INVESTIGATION OF HYBRID ELECTROCHEMICAL AND MAGNETIC FIELD ASSISTED ABRASIVE FLOW FINISHING PROCESS

A THESIS SUBMITTED IN FULFILMENT OF

THE REQUIREMENT FOR THE AWARD OF THE DEGREE

OF

DOCTOR OF PHILOSOPHY

IN

MECHANICAL ENGINEERING

BY

SACHIN DHULL

(ROLL NO- 2K14/Ph.D/ME/05)

GUIDED BY

Dr. QASIM MURTAZA                      Dr. R.S. WALIA                          Dr. M.S. NIRANJAN

(Professor)                                       (Professor)                                   (Associate Professor)

Mechanical Engineering Department

Delhi Technological University

Main Bawana Road, Shahabad Daulatpur, Delhi- 110042, India

CERTIFICATE

This is to certify that the work embedded in this thesis entitled, “Investigation of Hybrid Electrochemical and Magnetic Field Assisted Abrasive Flow Finishing Process” being submitted by Sachin Dhull (Roll No- 2k14/Ph.D/ME/05) for the award of Doctor of Philosophy Degree (Ph. D) in Mechanical Engineering at Delhi Technological University, Delhi is an authentic work carried out by him under our guidance and supervision.

It is further certified that the work is based on original research and the matter embodied in this thesis has not been submitted to any other university/institute for award of any degree to the best of our knowledge and belief.

Dr. Qasim Murtaza 	  Dr. R.S. Walia

Professor, 	                                                      Professor,

Department of Mechanical Engineering,         Head, Department of Production and Industrial Engineering,

Delhi Technological University,                      Punjab Engineering College (Deemed to be University),

Delhi- 110042                                                  Chandigarh

Dr. M.S. Niranjan

Associate Professor,

Department of Mechanical Engineering,

Delhi Technological University,

Delhi- 110042

ACKNOWLEDGEMENT

While bringing out this thesis to its final form, I came across a number of people whose contributions in various ways helped my field of research and they deserve special thanks. It is a pleasure to convey my gratitude to all of them.

First and foremost, I would like to express my deep sense of gratitude and indebtedness to my parents, brother, wife, Manjeet Singh, supervisors (Prof. Qasim Murtaza, Prof. R.S. Walia, Dr. M.S. Niranjan) and friends (Parvesh Ali, Jitender Kumar, Amrik Singh, Aman Verma) for their invaluable encouragement, suggestions and support from an early stage of this research and providing me extraordinary experiences throughout the work. I also thanks their support in my project research. I am also very thankful to Prof. R.S. Mishra for his valuable support and suggestions. Above all, their priceless and meticulous supervision at each and every phase of life inspired me in innumerable ways.

I specially acknowledge them for their advice, supervision, and the vital contribution as and when required during this research. Their involvement with originality has triggered and nourished my intellectual maturity that will help me for a long time to come. I am proud to record that I had the opportunity to work with an exceptionally experienced Professors like them.

Sachin Dhull

PREFACE

In this thesis the details regarding newly designed and fabricated electrochemo magneto rotational abrasive flow machining process setup have been given and the results of experimentation and mathematical models have been discussed. Further the details of in-house developed polymer media used for experimentation have been explained. The contents of the thesis are as follows:

Chapter 1 In this chapter the introduction to the non conventional machining processes has been given and the explanation of different types of abrasive flow machining (AFM) process is given. The different process parameters and the factors involved in AFM process are explained alongwith advantages, limitations and the applications of the process. Further polymer media, magnetorheological (MR) fluids used in the process are elaborated.

Chapter 2 The research conducted in the field of AFM process and its variants by various scientists and researchers has been analysed and written in a systematic documented form. The literature review of electrochemical assisted, magnetic field assisted, rotational force assisted AFM process and their combined form hybrid processes have been tabulated and the parameters, tools used have been discussed. In addition research done in the field of development of polymer media and MR fluids has been explained.

Chapter 3 The gaps in the research work in the field of hybrid AFM process were identified and based on that present research objectives have been set. In order to fulfil those objectives, a research methodology has been discussed and a sequence of events to be performed to complete the research work is planned.

Chapter 4 In this chapter firstly the hybrid electrochemo magneto rotational abrasive flow machining (EMR-AFM) machine setup fabricated has been explained with all the parts details and specifications. The polymer media developed for use in experimentation work has been detailed. Then the experimentation was performed in accordance with the design of experiments based on Taguchi method.

Chapter 5 The mathematical model was developed to explain the effects of magnetic field, electrochemistry and rotational force on the process. The computational flow dynamics was performed to study the effect of flow of polymer media through the fixture path during experimental work. The various rheological parameters were studied and the effect of temperature, pressure and velocity was also discussed. Further thermal, heat transfer and rigidity mechanics based models were developed to study in depth mechanisms of the process.

Chapter 6 The results of experimentation performed were discussed to know the effect of input parameters on the material removal and surface roughness of the workpiece obtained. Taguchi method based experimental results were studied in addition to Matlab fuzzy logic and grey relational optimization techniques. The characterization of developed media was done to deeply study the properties and their impact on the output results using XRD, FTIR images, etc.

Chapter 7 This chapter discusses the conclusions of the research work done both qualitatively and quantitatively. The mathematical results obtained were discussed and these can be compared with present setup used in industries and improvement can be done. Further the scope of future improvement and work that can be done is discussed.

CONTENTS

S.N.		Title 				                    Page No.

Certificate						         i

Acknowledgment						         ii

Preface						         iii-iv

List of Figures						         xi-xiv

List of Tables						         xv

Acronyms						         xvi

Abstract						         xvii-xxiii

1           CHAPTER 1 - INTRODUCTION						         1-6

1.1    Non Conventional Manufacturing Processes				         1

1.2    Abrasive Flow Machining (AFM) Process        		                     1

1.2.1    Basic Principle of AFM 						         2

1.2.2    AFM Technology						         2

1.2.3    Classification of AFM Process					         2

1.2.4    Applications of AFM Process					         3

1.3    Elements of AFM Process						         3

1.3.1    Fixture						         3

1.3.2    Abrasive Media						         3

1.3.3    Magnetorheological (MR) Fluids				         4

1.3.3.1    Properties of MR Fluids				         5

1.3.3.2    Disadvantages of Conventional MR Fluids		         5

1.3.3.3    Advantages of Bimodal MR Fluid over Conventional

MR Fluid						         5

1.3.3.4    Modes of MR Fluids					         5

1.3.4    Machine Setup						         6

1.5    AFM Process Variants						         6

2           CHAPTER 2 – LITERATURE REVIEW                                                         7-34

2.1    Non Conventional Manufacturing Processes				         7

2.1.1    Electrochemical Machining Process and its Variants		         7

2.1.1.1    ECM Using Mineral Water Electrolyte                              8

2.1.1.2    Electrochemical Micro Machining Process (ECMM)        8

2.1.1.3    Electrolytic Magnetic Abrasive Finishing Process and

Lorentz Force Study					         8

2.1.1.4    Electrochemical Discharge Machining (ECDM)               9

2.1.2    EDM and its Hybrid Processes					         9

2.1.2.1    Conventional and Micro EDM of WC		         9

2.1.2.2    Gas Film Study in ECDM				         9

2.1.2.3    Wire EDM						         9

2.1.2.4    Magnetic EDM						         10

2.2    Hybrid Conventional and Non Conventional Advanced Machining

Processes						         14

2.2.1    EDM and ECM/ECM Lapping					         14

2.2.2    Electrochemical Grinding (AECG)				         15

2.2.3    Rotary EDM with Ball Burnishing of Al2O3/6061 Al Composites   15

2.2.4    Modelling of Hybrid Electrochemical Turning Magnetic Abrasive

Finishing					                     15

2.3    Abrasive Flow Machining Process and its Variants			         15

2.3.1    Vibration Force Assisted AFM Process			         17

2.3.2    Abrasive Assisted Electrochemical Process			         17

2.3.3    Eletcrochemical and Centrifugal Force Assisted AFM	         17

2.3.4    AFM of Slit Fabricated by AFM				         18

2.3.5    Magnetic Field Assisted AFM Process and its Variants	         18

2.3.5.1    Magnetorheological AFM				         18

2.3.5.2    Ball End MR Finishing Process			         18

2.3.5.3    Double Disc Magnetic Abrasive Finishing of

Paramagnetic Materials				         18

2.3.5.4    MR Fluid Flow Behaviour				         18

2.3.5.5    Force Study in MAF					         19

2.3.6    Electrochemical Assisted AFM Process			         19

2.3.7    Helical AFM Process						         19

3           CHAPTER 3 – PROBLEM FORMULATION				         35-37

3.1    Research Gap						         35

3.2    Research Objectives						         36

3.3    Research Methodology						         36

4           CHAPTER 4 – EXPERIMENTAL INVESTIGATION OF EMR-AFM

PROCESS					                     38-73

4.1    Design and Analysis of Experimental Work				         38

4.1.1    Taguchi’s Method						         38

4.1.2    Taguchi Method Philosophy					         38

4.1.3    Taguchi Method DOE						         38

4.1.4    Strategy of DOE						         39

4.1.5    Loss Function and S/N Ratio					         39

4.2    Design and Fabrication of Magnetic Field Assisted Electrochemo

Abrasive Flow Finishing Setup						         39

4.2.1    Fixture Development and Fabrication Design			         44

4.2.1.1    Design Explanation					         45

4.2.1.2    Fixture Modelling					         45

4.2.2    Fixture and Electromagnet Design and Development		         46

4.3    Hybrid AFM Experimental Setup						         48

4.3.1    Working of the Hybrid Setup					         49

4.3.2    Principle Operation and Characteristics of the Magnetic Setup        51

4.3.2.1    Fixture and Electromagnet Design and Development        52

4.3.2.2    Development and Fabrication of Electromagnetic

Solenoid                                                                               52

4.3.2.3    Magnetic and Electrical Calculation of Electromagnetic

Solenoid and Experimental Setup			          53

4.3.2.4    Initial Readings on the Machine and Calculation of

Number of Turns						          53

4.3.3    Validation of the Concept of Electrochemistry Application in the

Removal of Material						         54

4.3.3.1    Electrolytic Assisted AFM Principle			         55

4.3.3.2    Decision of Cathode and Anode Selection		         55

4.3.3.3    Selection of Electrolyte				         56

4.3    4.3.4    Rotational AFM Setup						         56

4.3.4.1    Fabrication of Rotational AFM and its Effect on the

Efficiency of the Process				         57

4.4    Development of Polymer Media 						         58

4.4.1    Preparation of Polymers						         58

4.4.2    Preparation of Media						         58

4.4.3    Properties of Polymer Media					         60

4.4.4    In house Preparation of CNT Particles and their Role in

Material Removal Process						         61

4.4.4.1    Carbon Nano Tubes (CNTs) Synthesis		         62

4.5    Experimental Investigation						         63

4.5.1    Workpiece Preparation						         63

4.5.2    Measurements						         65

4.5.2.1    Weight						         65

4.5.2.2    Surface Roughness					         65

4.5.3    Sampling						         66

4.5.4    Observations						         66

4.5.5    Acquisition						         67

4.5.5.1    Justification for Selection of Material (Aluminium)	         67

4.5.5.2    Justification for Selection of Shape of Workpiece	         68

4.5.5.3    Pipe Purchase						         68

4.5.6    Procedure						         69

4.5.7    Experimental Design						         69

4.5.7.1    Plan of Experimentation				         70

5           CHAPTER 5 – MODELLING OF EMR-AFM PROCESS		         74-107

5.1    Mathematical and Computational Modelling of EMR-AFM Process	         74

5.1.1    Role of Computer Optimization Software and Algorithm in

AFM process Modelling						         74

5.1.2    Voltage and Magnetic Flux Calculations			         76

5.1.3    Effect of Time Derivatives on Magnetic Field			         78

5.1.4    Analysis of Flow of Media						         80

5.1.5    Computational Flow Analysis of Polymer Media in Hybrid

Magnetic Assisted Abrasive Flow Machine Fixture		         82

5.2    Heat Transfer, Flow and Velocity Analysis				         86

5.2.1    Heat Transfer During Media Flow Through Fixture		         86

5.2.2    Radial Heat Transfer Through the Brass Workpiece		         91

5.2.3    Governing Equations of the Flow Pattern 			         92

5.2.3.1    Continuity Equation					         92

5.2.3.2    Momentum Equation					         92

5.2.3.3    Constitutive Equation					         92

5.2.4    Flow Regime of Polymer Media Across the Inner Work Surface     93

5.2.5    Velocity Boundary Layer in Internal Flow of Media inside

Workpiece					                     94

5.3    Principle Operation and Characteristics of the Electrochemo-Magneto

AFM Setup						         95

5.3.1    Assumptions						         95

5.3.2    Magnetic Flux Intensity and Electrolytic Force Modelling	         96

5.3.3    Effect of Magnetic Field						         97

5.3.4    Analysis of Electrochemistry During Abrasive Flow

Machining Process						         98

5.3.4.1    Volume Removal Rate and Electrolytic Charge

Calculations						         99

5.3.4.2    Electrolytic Reactions Taking Place During

Machining						         100

5.4    Analysis on Abrasive Particles						         100

5.4.1    Force and Motion Analysis						         100

5.4.2    Hitting of Abrasive Grain Against Workpiece Surface	         102

5.4.2.1    Material Removal Time (tmr) Calculation		         102

5.4.3    Depth of Indentation and MR Calculation			        104

5.4.4    Stresses Acting on the Job						        105

5.4.5    Acceleration and Rotational Effects				        106

6           CHAPTER 6 – RESULTS AND DISCUSSION				        108-150

6.1    Effect of Process Parameters on MR					        108

6.2    Effect of Process Parameters on Ra					        116

6.3    Matlab Fuzzy Logic and Grey Relational Optimization of MR and

Ra Results						        117

6.4    Magnetic Field and Electrolytic Voltage Results			        120

6.4.1    Procedure of Experimental Work				        121

6.4.2    Result Output						        121

6.4.3    Introduction to RSM						        123

6.4.3.1    Procedure of RSM					        123

6.4.4    Effect of Electrolytic Force and Magnetic Assisted AFM

on MR						        125

6.4.4.1    Effect of ECM Voltage and Rod Size on MR	        125

6.4.4.2    Response Surface Methodology Results		        126

6.4.4.3    ANOVA Output and Fitted Line Plot Analysis	        126

6.3    Pareto and Contour Chart Detailed Explanation			        128

6.5    Experimental Results Based on Taguchi Analysis			        129

6.6    Experimental Results Based on ANOVA Analysis			        131

6.7    Experimental Results to Study the Effect of Magnetic Field		        133

6.7.1    Material Removal (MR)						        135

6.7.2    Confirmation Experiments						        135

6.8    Surface Roughness Calculation						        136

6.9    GRA and MPCI Output Results						        139

6.10  Characterization of Polymer Media					        145

6.10.1    X-Ray Diffraction Methods and Images			        147

6.10.1.1    Explanation of XRD Image Output Results	        147

6.10.1.2    Procedure of Polymer Media Analysis on

Brucker Machine				                    148

6.10.2    Prepared Media FTIR/TGA Image Discussion and Analysis       149

7           CHAPTER 7 – CONCLUSIONS AND FUTURE SCOPE OF WORK        151-152

7.1    Conclusions						       151

7.2    Future Scope of Work						       152

8          REFERENCES						       153-161

9          RESEARCH PUBLICATIONS						       162-165

LIST OF FIGURES

Figure 1.1    (a) One way AFM machine operation (b) Two way AFM machine operation,

(c) Orbital AFM machine operation  					                     2

Figure 1.2    (a) Behaviour of fluid flow in absence of magnetic field (b) the flow

pattern of fluid after application of magnetic field (c) microstructure of MR fluid

on application of shear strain rate 						         4

Figure 1.3    (a) valve mode (b) shear mode (c) squeeze mode				         5

Figure 2.1    (a) ECDM apparatus setup, (b) Electrochemical cell and polarization system	         7 Figure 2.2   (a) Machine tool system, (b) CFG rod and nylon fixture arrangement                      14

Figure 2.3    Three types of flows that in finishing zone (a) Flow Along Flute,

(b) Axial Flow Motion, (c) Scooping, (d) all the three motions			        20

Figure 4.1    (a) Top view of lower fixture, (b) Side view of fixture				        40

Figure 4.2    (a) 3D model of fixture, (b) Dimensional details of the fixture			        40

Figure 4.3    Different views of the fixture							        41

Figure 4.4    Electromagnet									        41

Figure 4.5    Bright bar cylindrical piece supporting workpiece			                    42

Figure 4.6    (a) AC power supply transformer, (b) voltmeter, (c) Ammeter			        42

Figure 4.7    AC to DC transformer supply							        43

Figure 4.8    Electrochemo magnetic fixture set up						        44

Figure.4.9    (a) Object free meshed in Ansys, (b) Fixture, (c) nylon fixture			        46

Figure 4.10.  Developed electrochemical and magnetic assisted AFM fixture		        47

Figure 4.11.  Top view of the fixture								        47

Figure 4.12.  Developed electromagnetic solenoid design					        48

Figure 4.13   Sketch of fixture incorporating electromagnet and ECM tool			        48

Figure 4.14   Hybrid EMR-AFM set up							        50

Figure 4.15   (a) Electromagnetic solenoid used in machine setup, (b) Media

characterization (a) FTIR, (b) SEM and TEM image				        51

Figure 4.16   (a) magnetic fixture setup installed on AFM machine, (b) AC-DC

Transformer									        53

Figure 4.17   (a) Machine showing the number of turns, (b) electromagnet attachment	        54

Figure 4.18   (a) AC-DC rectifier, (b) ECM rod, (c) drill bit ECM rod			        55

Figure 4.19    Working set-up, AC (220V) to DC (24V) transformer with 4

diodes: 3 for 3 electromagnet poles and 1 for electrolytic circuit		       56

Figure 4.20    Electrolytic fixture showing spring-loaded rotating contact for anode	       57

Figure 4.21    (a) Rotatioanal frequency meter, (b) Rotational AFM setup with fixture	       57

Figure 4.22    Natural Rubber based media							       59

Figure 4.23    Styrene Butadiene Rubber based media					       59

Figure 4.24    Nitrile rubber based media							       59

Figure 4.25    (a) Abrasive laden Media (carrier+Al2O3+CNT), (b) preparation

procedure, (c) fixture containing media					       61

Figure 4.26    (a) Optimised condition to synthesize Fe-filled CNTs, (b) Thermal CVD

Setup										       62

Figure 4.27    Currently used methods for CNTs synthesis 					       63

Figure 4.28    Schematic showing CVD method to develop CNT				       63

Figure 4.29    (a) Preparation of job on lathe, (b) Drilling operation on lathe machine	       64

Figure 4.30    (a) machine used for preparation, (b) Drilled brass pipes, (c) Filing of

Drilled brass workpieces							       64

Figure 4.31    (a) Weight measurement device, (b) roughness tester				       66

Figure 4.32    shows pipe flow profile							       68

Figure 4.33    shows roughness testing method						       69

Figure 5.1      (a) Flow-chart representing magnetic forces effect, (b) Neural network

approach in AFM								       75

Figure 5.2      Forces acting on abrasive particle inside the workpiece			       77

Figure 5.3     (a) Different forces acting on the workpiece, (b) Time derivatives

effect in magnetic field flow chart						       79

Figure 5.4     (a) Design of AFM fixture, (b) shear rate, (c) velocity of media flow and

(d) pressure variation								       82

Figure 5.5     (a) Top view of AFM, (b) Meshing of AFM, (c) Effect on temperature	       84

Figure 5.6     AFM Machine set-up block diagram: 1.Transformer, 2.Electromagnet,

3.Transformer oil tank, 4.Flow-sensor, 5.Pressure gauge, 6.Motorpump,

7.3-Phase motor, 8.Speed controller, 9.Fixture, 10.Lower media cylinder ram,

11.Lower machine cylinder pressure gauge, 12.Upper machine cylinder

pressure gauge, 13.Current reader, 14.Lower machine cylinder pressure

controller, 15.Upper machine cylinder pressure controller			      85

Figure 5.7    (a) top view of workpiece rotation, (b) media bulk motion inside fixture	      87

Figure 5.8    Heat transfer directions in cut section of workpiece				      88

Figure 5.9    Heat transfer circuit diagram							      89

Figure 5.10   Heat transfer vs media volume plot						      89

Figure 5.11   Different types of flow regime inside work surface				      93

Figure 5.12   Graphs showing fully developed media flow					      94

Figure 5.13   Electromagnetic setup configuration						      98

Figure 5.14 (a) initial shape of abrasive grain, (b) final shape of abrasive grain                        100

Figure 5.15   Rotational motion of bulk of abrasive grains					     101

Figure 5.16   Penetration of abrasive aprticle into work surface in successive

extrusion cycle provided by AFM machine					     103

Figure 6.1     3D Surface model (a) Type of media (surface view from top),

(b) Type of media (surface view from front), (c) Extrusion pressure (surface

view from top), (d) ) Extrusion pressure (surface view from front)       	      111

Figure 6.2.    S/N ratio and raw data output graphs of material removal rate vs

(a) Magnetic voltage, (b) ECM rod size, (c) ECM voltage respectively	      113

Figure 6.3     (a) MR vs rotational speed plot, (b) Power vs volume of material removal

Plot										      114

Figure 6.4     (a) Surface plot of MR vs magnetic voltage, (b) ANOVA interval plot

of MR vs rode size								      115

Figure 6.5     (a) Reduction in Ra vs (a) finishing time, (b) extrusion cycles, (c) media

pressure, (d) % abrasive concentration plot 					      117

Figure 6.6     Fuzzy logic operators alongwith membership plot and FIS variables		      120

Figure 6.7     surface plot of MR vs (a) ECM voltage and (b) magnetic voltage		      126

Figure 6.8    (a) ANOVA interval plot of MR vs rode size, (b) ANOVA interval plot

of MR vs voltage								      127

Figure 6.9     Fitted line plot of (a) MR vs rod size, (b) MR vs ECM voltage  		      127

Figure 6.10   (a) Pareto Chart of standardized effects, (b) Contour plot of MR

vs rod size and voltage								      128

Figure 6.11    (a) pareto chart of standardized effects, (b) interaction plot for material

Removal									    129

Figure 6.12    (a) Effect of different parameters on MRR, (b) Plot for the S/N ratio of

MRR										    130

Figure 6.13    (a) Plot for different process parameters effect on the mean Ra, (b) Plot

for different process parameters effect on the SN Ratio of Ra			    130

Figure 6.14    (a) One-way ANOVA: MRR versus (a) Pressure, (b) No. of Cycles,

(c) media								                131

Figure 6.15    (a) One-way ANOVA: Ra versus (a) pressure, (b) no. of cycles, (c)

Media										    131

Figure 6.16    (a) Effect of (a) cycles, (b) pressure, (c) CNTs on S/N ratio 			    131

Figure 6.17    Surface roughness versus pressure, number of cycle, magnetic field

strength (a) SN ratio, (b) means						    134

Figure 6.18    (a) Graph is plotted keeping magnetic field and number of cycles

at level 2, (b) magnetic field and pressure at level 2, (c) pressure and

number of cycles at level 2							    134

Figure 6.19    Profile curve									    136

Figure 6.20    R and  W motifs								    137

Figure 6.21    Rk calculation profiles								    137

Figure 6.22    Distance measurement								    137

Figure 6.23    Step height measurement							    138

Figure 6.24    (a) Abbot firestone curve, (b) Interactive abbot curve, (c) Fractal

analysis, (d) R and  W motifs							    138

Figure 6.25   (a) MPCI fuzzy controller, (b) scope display					    141

Figure 6.26   (a) Time series, (b) SN ratio data, (c) matrix plot				    143

Figure 6.27   (a) TEM image of CNTs, (b) SEM image of media, (c) FTIR graph

of the media									    146

Figure 6.28   FTIR image of the developed Nitrile rubber media				    146

Figure 6.30   X-Ray Diffraction image of  (a) Nitrile Rubber, (b) SBR			    147

Figure 6.31   Bruker X-Ray Diffraction Machine (D-8 Advance)				    149

LIST OF TABLES

Table 2.1    Electrical Discharge Machining and its variants					    10

Table 2.2.   Electrochemical force assisted AFM process and its variants			    11

Table 2.3.   Magnetic assisted finishing process and its variants				    13

Table 2.4.   Innovations in the field of AFM							    20

Table 2.5.   Conventional and hybrid AFM processes					    27

Table 2.6.   Output results obtained in various hybrid AFM processes			    32

Table 4.1    Machine parameters and units							    51

Table 4.2    Different types of media used and their properties				    60

Table 4.3    Initial reading of the prepared workpiece					    65

Table 4.4    Surface roughness values								    66

Table 4.5    Weight and roughness readings							    66

Table 4.6    Parameters and output MR results						    67

Table 4.7    Workpiece material specifications						    67

Table 4.8    Parameters with their levels used							    70

Table 4.9    Taguchi L 18 OA									    71

Table 4.10   Response characteristics i.e. material removal and % change

in surface roughness								    72

Table 5.1    Shear rate, pressure, velocity values at different locations during

media flow									    84

Table 6.1    Effect of different polymer media used on material removal			    109

Table 6.2    ANOVA table for material removal						    110

Table 6.3    Material removal and roughness output values					    112

Table 6.4    ANOVA table									    114

Table 6.5.   GRC and MPCI rank values corresponding to Taguchi L9 OA

Experimentation									    119

Table 6.6    Parameters and their level values							    120

Table 6.7   The L9 (34) OA parameters and response						    120

Table 6.8    Mean and variance of output results						    122

Table 6.9    S/N ratio table for response output						    122

Table 6.10  ANOVA Raw Data								    123

Table 6.11  Input variables									    123

Table 6.12  Values of factors and different points of cube					    124

Table 6.13  Design table in terms of actual factors						    124

Table 6.14  Statics control terminology							    125

Table 6.15  Taguchi Analysis: MRR versus pressure, no. of cycles, abrasive media                129

Table 6.16  Taguchi analysis: surface roughness versus pressure, no. of cycles, media            130

Table 6.17   Pooled ANOVA (Raw Data) (MR)						    132

Table 6.18   Pooled ANOVA (S/N Data) 							    132

Table 6.19   Average values and main effects: % improvement in Ra			    133

Table 6.20   Response table for SN ratio and means						    134

Table 6.21   Optimum values, ci and confirmation experiments				    136

Table 6.22   Output results corresponding different parameters combination		    139

Table 6.23   GRC based output results corresponding different combination of

Parameters									    141

Table 6.24.  Parameters and their level values						    143

Table 6.25   The L9 (34) OA parameters and response				                143

Table 6.26   Output results corresponding to input parameters				    144

Table 6.26   Input parameters and their levels and units					    145

ACRONYMS

Ra 		surface roughness of workpiece

Rcrt 		critical roughness

α		angle between magnetic field and plane of solenoid coil

Bp		peak magnetic field

ω 		angular frequency of current

M 		mutual induction

R		erosion rate of workpiece material

VA		volume removed by single particle

Fa		axial force

Fr		radial force

Ft		tangential force

m 		mass of abrasive particle

ρ 		density of abrasive material

r 		radius of iron oxide particle

p 		extrusion pressure

pm		magnetic pressure

τs   	            shear stress

V*		shear velocity

umax		maximum fluid velocity

dudy 	            velocity gradient of fluid

H28π 	 	magnetic pressure

B 		magnetic field

∅ 	 	magnetic flux

N	 	number of abrasive particles

S/N              	Signal to Noise Ratio

LN               	OA designation

fLN             	Total degree of freedom of an OA

R                	Number of repetitions

T                	Overall mean of the responses

A2 ,B2        	Average values of responses at the second level of parameters  A & B

CICE         	Confidence Interval of confirmation experiments

CIPOP       	Confidence Interval of Population

Fα             	The F-Ratio at the confidence level of (1- α) against DOF 1

fe               	Error DOF

AFM	 	Abrasive Flow Machining

EDM	 	Electric Discharge Machining

ECM	 	Electrochemical machining

MAF	 	Magnetic Abrasive Finishing

AECG	 	Abrasive Electro Chemical Grinding

UAAFM	Ultrasonic assisted abrasive flow machining

MRP 		Magneto Rheological Polishing

ECP/ECF	Electrochemical Polishing/Finishing

DOA	 	Dio-iso Octyl Adiabate

DOP		Dio-iso Octyl Pthalate

EMR-AFM	Electrochemical Magnetic Rotational AFM

RSM	 	Response Surface Methodology

ANOVA	 Analysis Of Variance

GRA	 	 Grey Relational Analysis

OA		 Orthogonal Array

GA		 Genetic Algorithm

MR		 Material Removal

SBR		 Styrene Butadiene Rubber

NR		 Natural Rubber

NTR		 Nitrile Rubber

PBS		 Polyborosiloxane

SLM		 Selective Laser Melting

SR		 Silicon Rubber

MS	 	 mild steel

ABSTRACT

The current scenario of industrialization requires need for higher productivity which is met by advanced material removal process, i.e., abrasive flow machining (AFM) in which the internal surfaces of the workpiece is machined to higher accuracy level with the help of abrasive laden media. In this paper, the conventional AFM setup has been made hybrid using electrolytic and magnetic force arrangement alongwith rotational effect in order to achieve better results in terms of material removal and surface roughness. The newly developed in-house polymer media were utilized in the process and the input parameters taken during experimentation were magnetic flux, electrolytic rod size and shape, rotational speed, polymer media, abrasive particles and extrusion pressure. It was found that the material removal and surface roughness improvement were more in electrochemo magneto rotational AFM process compared to conventional AFM process. The experimental values were in confirmation with those obtained in the optimization techniques applied, i.e., Taguchi L9 OA, Matlab fuzzy logic and GRA-PCA. In addition, the hybrid mathematical model was developed and effect of different forces occurring in the process and computational flow analysis of media have been explained. With advent of need for fast productivity in terms of material removal and surface roughness of the workpiece, abrasive flow machining (AFM) process is gaining rapid importance in the industries. In this process, the fine finishing of the internal surfaces is done that are difficult to reach spaces using abrasive laden polymer media. The media is extruded past the surface under high pressure with the help of two sets of extrusion piston cylinder arrangements. Further various innovations done in the field of abrasive flow machining have been studied in detail in a tabulated form. It included the applications of the process and the different variant forms of AFM process. Hence it can be concluded that this form of non conventional machining process is efficient both in terms of surface roughness and material removal. The SBR media resulted in maximum material removal during experimentation, i.e., 3.88 mg when input parameters, i.e., electrolytic voltage, number of extrusion cycles and pressure were taken as 18 V, 4 and 10 bar respectively. The NR, NTR and SR media had intermediate effect of material removal but minimum removal of material was achieved in case of PBS media, i.e., 2.39 mg at 6 V voltage, 6 number of cycles and 30 bar pressure. The material removal was first increased with higher rod size but afterwards its increase was lesser. The surface plots obtained from RSM technique showed that MR obtained was 2.25 mg at 21 bar pressure and 7 number of cycles. As compared to conventional AFM setup, it was found that in EMR-AFM setup, 34.5 % and 17.8 % improvement in % Ra and material removal, respectively, was obtained. It was found that MR was approximately 2.9 mg on an average when machining was done on traditional AFM process, while it increased upto 4.5 mg in prepared hybrid machine setup.

CHAPTER 1: INTRODUCTION

This chapter describes the basic principle of abrasive flow machining (AFM) process, its advantages, limitations and applications. Further, the different types of AFM process and the elements of the machine setup are explained in detail. The elements include machine setup, fixture, polymer media used, etc. The process parameters used by different researchers and the work done in the field of polymer media and magnetorheological fluids are discussed. In addition, the process hybrid forms are categorised and given a brief introduction.

1.1 Non Conventional Manufacturing Processes

There are two types of manufacturing processes i.e. conventional and non-conventional processes. In case of conventional process, there is job and tool contact and the tool must be harder than workpiece in order to achieve cutting. There is no direct tool and workpiece contact in unconventional machining processes and various types of energy is used to remove unwanted material and find uses in many of the industries, hard and brittle materials. The life of the tool is reduced and residual stresses are induced in the workpiece due to large cutting forces requirement and production of large amount of heat in the form of cutting chips off the workpiece.

1.2 Abrasive Flow Machining (AFM)

It is a process of polishing internal surfaces and producing controlled radii by the action of pressurised abrasive laden media against the workpiece surafce. The advantages of this process include more tolerance in terms of surface finish, finishing of more difficult to reach areas and faster finishing rates as compared to manual methods. Abrasive flow machine was first introduced in American based extrudes hone company in 1960s which is used for complex internal inaccessible cavity and shapes. AFM is a unique process developed for fine finishing, polishing by flowing an abrasive laden media. The hard and tough materials are machined because of the flexibility and mouldable properties of the media and it acts as deformable grinding media which is subjected to restricted flow passages.

The AFM process is mainly divided into three parts, i.e.

(a) Machine

(b) Tooling

(c) Process input parameters of AFM

Its applications can be diversified into pharmaceutical, chemical, production, automobile and aeronautics industry, etc.

1.2.1 Basic Principle of AFM

The basic machining mechanism of the process is by abrading the surface using high pressure extruded abrasive laden media against the surface. The location and intensity of abrasion can be controlled in AFM process by parameters and proper fixture design. The dozens of holes and passages can be machined easily with accurate results.

1.2.2 AFM Technology

In the AFM setup, pressure system employing two opposed cylinders is utilised to provide media pressure. The cutting tools are also flexible due to usage of self modulated medium having good viscosity and fluidity. When media enters and exits via restricted passages, the abrasion process occurs causing material removal. The combination of forward and backward strokes makes a complete cycle.

1.2.3 Classification of AFM Process

There are basically three categories of AFM process i.e. one way, two way and orbital. In one-way AFM process (Rhoades, 1989), as shown in figure 1.1 (a), the media is received and extruded through chamber un-directionally via surface of the workpiece that is hydraulically activated by reciprocating pistons.

(a)                                                 (b)                                        (c)

Figure 1.1 (a) One way AFM machine operation (Rhoades, 1989), (b) Two way AFM machine operation (Tzeng et al., 2007), (c) Orbital AFM machine operation

The two way AFM has two hydraulic cylinders and two medium cylinders (Tzeng et al., 2007). The mandrels and restrictors are used to finish blind cavities, recessed areas and counter bores, etc as shown in figure 1.1 (b). The orbital AFM process is shown in figure 1.1 (c).

1.2.4 Applications of AFM Process

The process applications include the finishing of critical parts, such as control parts, fuel spray nozzles and has numerous applications comprising aeronautical industry (the turbine blades thin layer coatings), medical technology (pharmaceutical machinery, surgical instruments requiring close incisions), automobile (complicated intersections like inlet manifolds of engines), aluminium dies, etc.

1.3 Elements of AFM Process

There are various elements included in the AFM process. The abrasive media determines the type abrasion occurring, the fixture determines its exact location and machine decides the extent of abrasion as the particles are responsible for direct MR action on the surface and fixture is responsible for holding the work piece against the flow of abrasive particles. The type of drill bit and the extrusion pressure of the machine decides the force by which abrasive particles strike the surface.

1.3.1 Fixture

The fixture is is used to hold workpiece and other process specific accessories, whose machining is to be carried out and its manufacturing is done based on the process. If AFM is used to process external edges or surfaces, the tooling contains the part in the flow passage, restricting the flow between the exterior of the part and the interior of the fixture. The uniform results are obtained in processing of parallel restriction on the process.

1.3.2 Abrasive Media

This technique uses polymer containing abrasive particles of Al2O3, SiC, boron carbide or diamond as the grinding medium and additives. The different mesh size abrasive particles, having limited life and generally the ratio of 2 to 12 is taken for abrasive particles and base material. In order to obtain the media rheological and flowability characteristics, the different additives are added. The lubrication purpose in polymer media is fulfilled by the hydrocarbon gel. Nanotubes find applications as additives to various structural materials so an attempt is made to use of nano particle (CNTs) as abrasive with the carrier and Al2O3 to machine the cast iron workpiece. Nano particles have extraordinary properties over available abrasives, so to enhance MR and surface finish nano particles can be used.

1.3.3 Magnetorheological (MR) Fluids

Magnetorheological (MR) fluids are defined as micron-sized magnetizable particles (like, iron) suspensions present in a nonmagnetic carrier fluid. The most essential characteristic of these fluid materials is that they can be reversibly and rapidly varied from a Newtonian-like fluid state to a stiff semisolid state under the  application of a moderately strong magnetic field. The columnar microstructure, in turn, dramatically results in the increment of its resistance due to applied shear strain shown in figure 1.2. This feature is the inspiration behind the design of new technology as well as various products such as brakes, clutches, semi active dampers, and numerous other robotic control systems. A typical MR fluid includes certain special additives like anti wear agents and surfactants that enhance its performance in the devices based on MR fluid. The magnetization non linear behavior and oscillation poses difficulties in giving information regarding magnetic properties of the particles.

Figure 1.2 (a) Behaviour of fluid flow in absence of magnetic field (b) the flow pattern of fluid after application of magnetic field (c) microstructure of MR fluid on application of shear strain rate (Simon et    al., 2001)

1.3.3.1 Properties of MR Fluids

The surfactants and stabilizers play a vital role in MR fluids, the suspended particles induced polarization is increased by surfactants adsorbed while their suspension results with the help of stabilizers. A number of additives (surfactants and stabilizers) are used for prevention of gravitational settling. The diameters of these magnetizable particles lie in the range of 3 to 5 microns. The approximately 30 nm diameter sized particles are generally stable because they are formed of MR fluid pigments.

1.3.3.2 Disadvantages of Conventional MR Fluids

There are some limitations of the use of conventional fluids. The large micron sizes of the particles are generally responsible for the settling due to gravity when the fluid is not in use for considerable time. However, use of small size of particles improves the colloidal stability. In order to overcome these disadvantages, the Bi-Modal MR fluids are used and the diffusion of small size micron sized magnetizable particles into the MR fluid is known as bi-model fluid.

1.3.3.3 Advantages of Bimodal MR Fluid over Conventional MR Fluid

The bimodal MR fluid has advantages over conventional fluids. The introduction of micron sized particles increases the dispersibility and decreases the sedimentation of the CIP particles. The viscosity of conventional MR fluid is found to be less than the bimodal fluid due to the aggregation of its CIP particles.

1.3.3.4 Modes of MR Fluids

There are three types of MR fluid modes, i.e. the valve mode, the shear mode and the squeeze mode, as shown in figure 1.3.

- (b)                                          (c)

Figure1.3 (a) valve mode (b) shear mode (c) squeeze mode

1.3.4 Machine Setup

All AFM machines regardless of size are positive displacement hydraulic systems, where work piece is clamped between two vertically opposed media cylinder. The media flow rate, abrasion limit and extrusion pressure are determined by the AFM machine. The clamping and unclamping of fixture and tool, media volume flow rate and hydraulic pressure controls are provided, in addition, for controlling temperature of media, viscosity, programmed microprocessors are installed on the machine setup. Several accessories such as part cleaning stations, automatic flow timers, automatic media lubricant replenishment, and media heat exchangers units may also be integrated to the conventional AFM systems.

1.5 AFM Process Variants

The process can be made hybrid by suitable arrangements and addition of external forces like rotation, magnetic and electrolytic force, etc. some hybrid forms of AFM process are discussed below. The different variants of AFM process include electrochemo magneto AFM, helical AFM, centrifugal force assisted AFM (CFA2FM), spiral AFM, magnetorheological AFM process, etc. These have an additional advantage of more material removal and better surface integrity.

Summary

- Abrasive flow machining process is the latest technique of non traditional machining in which high removal of material is obtained and is widely used in industries nowadays.

- There are basically three types of AFM process based on the direction of pressurised media flow.

- The various elements of the process includes machine setup, fixture, abrasive media, MR fluids, etc.

- The different variants comprises magnetic, centrifugal, electrochemical AFM processes, etc.

CHAPTER 2: LITERATURE REVIEW

This chapter describes the literature work done by various scientists and researchers in the field of non- conventional machining processes and abrasive flow machining (AFM) process and its hybrid forms. The different process parameters used, work output and input techniques used by researchers are tabulated and explained in detail. The electrolytic, magnetic and centrifugal force assisted AFM processes literature in addition to different polymer media used is analysed.

2.1 Non-Conventional Manufacturing Processes

In non conventional machining processes, the material removal of workpiece takes place without the necessary condition of tool being harder than workpiece. It can be of various kinds like electric discharge, electrochemical, ultrasonic, etc depending on the type of energy source. The various types of unconventional processes and their combination variant processes are explained.

2.1.1 Electrochemical Machining Process and its Variants

In electrochemical abrasive flow machining process, the abrasive media is mixed in electrolyte solution and extruded through the inner surface of workpiece assisted by electrolytic force. The workpiece is connected to positive, while tool is connected to negative terminal and the electrolysis occurs through electrolyte between anode and cathode. In a paper, the glass was micro machined by ECDM process used in various applications like micro reactors, micro fuel cells, etc., as shown in figure 2.1.

- (b)

Figure.2.1 (a) ECDM apparatus setup (Jui et al. 2013), (b) Electrochemical cell and polarization system (Yang et al. 2011)

It reduced overcut of hole and aspect ratio was improved (Jui et al 2013). A micro stage for feed with step size 0.1 µm, multimeter of resolution 0.01 mA, to control current supply was used. The cross innovation and modelling of ECM was done. ECF/ECP and its variants helped to achieve micro to nano range of surface finish, the parameters affecting the output results included electrolyte properties, position and motion of electrode, etc (Kumar et al 2013). A model was developed in which electrode gap was simulated and modelled and final micro tool diameter was predicted within the accuracy of 94% or 6% variation range to develop tungsten tools (Mathew et al 2012). Grey relational analysis was applies to study and analyse the output results obtained in ECM process (Liu et al 2012).

2.1.1.1 ECM Using Mineral Water Electrolyte

Green machining, low cost, high efficiency electrochemical process was explained, polarization cure was measured in potentiostat of 300 V, working electrode (WE) was workpiece i.e. SUS304, reference electrode (RE) is Ag/AgCl, counter electrode (CE) is tool i.e. WC rod of diameter 0.3mm, as shown in figure 2.1. The mineral water was used in the process. It was concluded that short pulsed supply was rapid than electrolyte NaNO3 (Yang et al 2011).

2.1.1.2 Electrochemical Micro Machining Process (ECMM)

Various types of profiles generated by sinking and milling methods using straight, conical, reverse taper tool was investigated. It was found that lesser the micro tool taper angle, lesser would be taper angle of profile generated during ECMM process. 14.5o taper angle of profile was generated by conical micro tool of 10.5o angle, while 5.14o angle was obtained by 4.34o angle tool (Ghoshal and Bhattacharya, 2015). If molarity value of electrolyte is less than 0.05 M, then electrolytic micro machining (EMM) does not give result, rather micro sparking removes material from the work surface.

2.1.1.3 Electrolytic Magnetic Abrasive Finishing Process and Lorentz Force Study

The effect of magnetic field on abrasive particles was studied. In case of both magnetic and electric fields, the oppositely charged ions move towards electrode in cycloidal path due to the action of Lorentz force. If approach angle of ions towards electrode is not proper, it resulted in poor electrolytic effect. Zinc stearate helped to stabilize steel grit movement, hence used for rough machining. High current and speed of rotation helped in more material removal and better surface finish (Taweel 2008).

2.1.1.4 Electrochemical Discharge Machining (ECDM)

Response surface methodology, i.e. RSM was used in ECDM process since material removal was non-linear. Aluminium frame was used for machine tool, worm and worm gear speed reduction of 25:1 was obtained, worm was attached to stepper motor shaft (Paul et al 2013). Taguchi method of optimization was used to obtain best result.

2.1.2 EDM and its Hybrid Processes

As compared to conventional Cu electrodes, Cu-ZrB2 electrodes showed more MRR, less tool wear. Since the difference between melting points of Cu and ZrB2 is there, the spark mainly passes through Cu, hence the erosion of ZrB2 decreases (Zhang et al 2009).

2.1.2.1 Conventional and Micro- EDM of WC

It is used where high dimensional accuracy is required in hard materials (Jahan et al 2011).

2.1.2.2 Gas Film Study in ECDM

Gas film plays a vital role in machining quality and efficiency. The electric supply affects the produced gas film, which further affects the electrolyte properties, hence the output material removal and surface finish of the workpiece varies (Jiang et al 2015). The development of bubble occurs and film thickness was in the range 17-29 mm. The advantage of gas bubble is that critical current as well as voltage gets decreased, hence overcutting problem in ECM is prevented.

2.1.2.3 Wire EDM

Addition of SiC abrasive particles in electrolyte improved wire EDM efficiency. The shape accuracy of workpiece was found to be significantly affected by wire vibration and introduction of bubbles in  the electrolyte. The advantage of addition of silicon carbide abrasive particles in the electrolyte is that it prevents the accumulation of bubbles, thereby decreasing the energy used in discharge. The expansion of slit and roughness value were 0.024 and 0.84 µm respectively (Yang et al 2006). The brass wire diameter 0.25 mm was put in contact with cathode and graphite was used as anode, hydrogen bubbles were produced when applied voltage exceeded critical voltage, as shown in figure 6. The temperature controller (401C) was used to control electrolyte properties, while the workpiece was driven by speed controlled motor. The bubbles formation occur more in KOH electrolyte.

2.1.2.4 Magnetic EDM

Gray relational analysis optimization technique applied in magnetic assisted EDM of SKD 61 workpiece (Lin and Lee 2009). Taguchi L18 was applied, parameters taken were machining polarity, high voltage auxiliary current (IH), servo reference voltage (SV). The machine set up comprised digital oscilloscope, current probe, passive voltage probe were used for monitoring discharge voltage and current waveforms. The various EDM process variants and the parameters, tool used in the particular process is given in table 2.1 and electrolytic process variants are explained in table 2.2.

Table 2.1 Electrical Discharge Machining and its variants

| Author, year, area of research/process | Workpiece | Tool | Electrolyte/media/particles | Parameters |
| --- | --- | --- | --- | --- |
| Zhang et al, 2009, EDM | Cu-ZrB2 shell electrodes | brass | Al2O3/6061 Al composites (toughness 29 MPa, yield strength 0.3 MPa, hardness 27-87 HRB, thermal conductivity 0.168-0.122) | Pulse off time 450 ms |
| Yan et al, 2000, Rotary EDM | Steel |  | Al2O3 vol. Fraction 0-20%, dielectric used was kerosene | current 1-15 A, pulse off time 1-650 ms, pressure 0-3 kg/cm2 |
| Yang et al, 2006, Wire-EDM | Graphite (+) | Brass wire (-) of 0.25 mm diameter | KOH electrolyte 300 g/L, SiC #200 abrasive | Non-load voltage 60-120 V |
| Lin and Lee, 2009, Magnetic-EDM | SKD 61 |  |  | frequency 100 Hz |

Table 2.2. Electrochemical force assisted AFM process and its variants

| Author, year, area of research/process | Workpiece | Tool used | Electrolyte/media/particles | Parameters |
| --- | --- | --- | --- | --- |
| Jui et al, 2013, ECDM | Glass of thickness 200 µm | Electrode: Anode: Steel of thickness 8 mm, cathode: WC rod of diameter 100-300 µm | NaOH of 0.1-7.5 M | Rotation speed:0-2500 RPM, feed with step size 0.1 µm, multimeter of resolution 0.01 mA |
| Yang et al, 2011, Eco-friendly ECM | working electrode (WE) was workpiece i.e. SUS304 | counter electrode (CE) is tool i.e. WC rod of diameter 0.3mm. |  |  |
| Kurita and Hattori, 2006, EDM and ECM/ECM lapping | EDM processed workpiece | machine tool size 557 x 604 x 655 mm, weight 80 kg |  | Power supply 0.75kVA, travel range 200 x 110 x 110 mm, feed rate 600 mm/s, resolution 0.1 fEm |
| Yan et al, 2003, Electrolytic MAF | SKD11, HRC61 |  | abrasive WA, 1.2 µm, 0.4 g, steel grit 180 µm, 3.6 g, unbounded magnetic abrasive 4 g. | magnetic flux 0.85 T, electrode gap 2-5 mm |
| Ghoshal and Bhattacharyya, 2015, ECMM |  | Micro tools 110 µm straight, conical 10.5o taper, reverse taper 2o | Sludge H2SO4 electrolyte of molarity 0.05-0.3 M | pulse frequency 5 MHz, duty ratio 35%. |
| Paul, 2013, RSM-ECDM | Graphite plate 50 mm x 30 mm x 5 mm | WC wire of 300 µm | 30 wt.% electrolyte, | MRR was found to be increased at high concentration and equal to 0.96 mg/hr at 25 wt% concentration and 60% duty cycle, whereas tool wear rate was minimum at high concentration i.e. 0.62 mg/hr. |
| Liu et al, 2015, ECM | TiAl intermetallic | electrode feed 2 mm/min | electrolytic pressure 0.8 MPa | 35 V |

The magnetic field assisted AFM process and its variants as well as magnetorheological finishing processes are explained in table 2.3 with details of tool, workpiece and dielectric media used.

Table 2.3. Magnetic assisted finishing process and its variants

| Author, year, area of research/process | Workpiece | Tool used | Electrolyte/media/particles | Parameters |
| --- | --- | --- | --- | --- |
| Sidpara and Jain, 2013, MR fluid based finishing [57] |  | permanent magnet attached to base of tool, N-Fe-B (N 50 grade) | CIPs size 6 mm, 40 vol%, diamond particles 6 mm, 3.5 vol%, 48.5 vol% water, 8 vol% glycerol. | 48-51 mega Gauss Oersted |
| Sidpara and Jain, 2012, MR fluid based finishing |  | permanent magnet sintered Nd-Fe-B N 48 grade | Particle diameter 2 mm, HS grade, 8 vol% glycerol |  |
| Niranajan and Jha, 2014, Ball-end MAF | M.S. workpiece | BEMRF tool | 55 vol% fluid, 16 and 4 vol% CIPs CS and HS grade respectively, 25 vol% abrasives. |  |
| Gorona et al, 2006, MAF | ferromagnetic alloy steel | ferromagnetic alloy steel | mixture of SiC (600# mesh) and ferromagnetic particles (300# mesh) in the ratio 1:4 by weight | magnetic flux 0-0.44 T, gap 1-2 mm |
| Singh et al, 2012, Bal-end MR finishing | ferromagnetic surfaces | electromagnetic coil is rotating core iron |  | Current 0.9999914 A, no. of turns 2000 |
| Singh and Shan, 2002, Magneto-AFM |  | Pole and yoke material Mild Steel 0.25% C, pole size 35 mm diameter, copper wire diameter 1.21 mm, number of turns 1500 |  | Magnetic flux 0.9 T, current 3.5 A. |

2.2 Hybrid Conventional and Non-Conventional Advanced Machining Processes

The following are the combination of traditional and non traditional processes.

2.2.1 EDM and ECM/ECM-Lapping

Same machine tool, same electrode i.e. copper and same machining liquid water were used the experiment was performed using formed electrode and simple shaped electrode. The EDM surface of Ra i.e. 1 mm was reduced to 0.2 mm by further ECM application.

(a)                                                                 (b)

Fig.2.2 (a) Machine tool system (Yoon et al. 2014), (b) CFG rod and nylon fixture arrangement (Vaishya et al. 2015)

If EDM and ECM lapping was used then surface roughness was improved upto 0.07 mm in 2 min (Kurita and Hattori 2006). The machine tool system of ECM-lapping process is shown in figure 2.2 (a). ECM is applied after EDM because it produce smooth, stress-free surface.

2.2.2 Electrochemical Grinding (AECG)

The electrochemical grinding of sintered carbides G20, titanium alloys WT31 was done and it was concluded that wear in conventional grinding was 6 times more as compared to AECG. The grinding of tool was 15 times lesser in AECG as compared to mechanical grinding (Zaborski et al 2004).

2.2.3 Rotary EDM with Ball-Burnishing of Al2O3/6061 Al Composites

The parameters were peak current, dielectric flushing pressure, electrode rotational speed, non-load voltage (Hwa et al 2000).

2.2.4 Modelling of Hybrid Electrochemical Turning Magnetic Abrasive Finishing

DC motor was used for rotating workpiece. Magnetic flux of 0-0.24 T, working gap 1.5 mm, copper wire diameter 1 mm, soft iron was used as magnetic pole and core since it has high magnetic permeability (Yan et al. 2003). The solenoid coils were connected in series. , feed 0.02-0.1 mm/min, voltage 8-24 V, electrolyte pressure 0.4 MPa, speed 125-750 RPM, flow rate 2 lit/min, machining time 1.5 min. The electrolytic ions path changed from linear to curved in the presence of magnetic field.

2.3 Abrasive Flow Machining Process and its Variants

Kenda et al. (2014) found that the AFM polishing process novelty study having movable mandrels in order to obtain improved performance of the product manufactured in the process. In the paper of AFM process, bevel gears are micro manufactured using special tools (Venketesh et al. 2014). The high temperature in the AFM process decreases the viscosity of the polymer media used for cutting action or finishing process (Uhlmann et al. 2009). The hybrid AFM process increases the efficiency of the conventional process (Jain 2008). The design of the optimum results, media and AFM setup has effect on the process (Zhang et al 2009). For extrusion pressure used in AFM, dies and molds are made of Al and steel that resulted in optimum output (Williams et al 2007). The AFM process used turbulent flow model and volume of fluid (VOF) model in case of zigzag channel to check the regularity of process (Tang et al 2010). In AFM process, the MRR was affected by various factors like abrasive grit size, pressure, etc (Williams and Melton 1998). The discussion of the pressure difference between entry and exit of the system was extensively done in case of steel pipe in AFM process that used copper and nylon fixture (Zhang et al 2009). The cleaning of the wall of steel tube in AFM process was discussed (Pengfei et al 2009). The cleaning technology helped to remove the material using the developed the mechanical model in lesser time to get accurate results in case of steel tubes (Pengfei and Jiazhi 2010). The Ansys and finite element analysis (FEA) software were used to obtain strength and rigidity of rail parts in AFM experiments (Li et al 2010). The abrasive particular move in such a way that it increase the hardness of workpiece and decrease the groove regime in AFM process, using 3-body abrasion (Fang et al 2009). The energy consumption and roughness was decreased, flow improved by increasing abrasive concentration, in case of extruding grinding which is affected by cycle time (Yang 2009). The SBR media was developed and used to finish different materials in AFF process (Sankar et al 2009). The force on abrasive grain was predicted and the depth of indentation was calculated to check the material deformation (Gorona et al 2006). The different parameter like workpiece modulus of elasticity, yield strength, load, grain size had effect on the amount of material removal (Yang and Kao 209). In the paper, abrasive electrochemical grinding (AECG), electrochemical honing and abrasive electrical discharge machining (AEDM) were studies (Kozaka et al 2001).

The optimum Ra was obtained when extrusion pressure was kept at 40 bar, while uniform roughness at 70 bar (Swata et al 2014). The different type of mechanical advanced machining process were discussed (Jain and Jain 2001). In AFM process the viscoelastic carrier affected the mixing that reduced the modulus of media by 10-86 % (Kar et al 2012). The non-Newtonian fluid is used as polymer media in AFM process that were affected by strain and temperature, the velocity of A-Silicone is 20 times lesser than P-Silicone (Wang et al 2007). The temperature change of workpiece was predicted by help of specific energy in AFM process i.e. 10-110 J/mm3 (Jain and Jain 2001). The surface integrity obtained by EDM process was enhanced by AFM process (Kenda et al 2011). The sustainability of manufacturing process was discussed in 3 sections, Type A, B, C, were denoted to explain the energy, material efficiency and materials or components used (Aurich et al 2013). The surface roughness was improved with the help of ball-shaped pole of magnetic brush that was flexible in nature (Lin et al 2007). The CFD method was used to study the flow of media in AFM process that concluded that shear rate affected media viscosity, and the working gap had the significant effect on the surface finish (Wang et al 2009). The simulation was done to reduce the cost and effort in process layout so that AFM process could be run smoothly (Uhlmann et al 2013). The twin flapper nozzle valve was used in AFM model to obtain high accuracy (Yang and Sha 2014). The section geometry, air supply in the way of workpiece in fluidized bed had been highlighted to study the process effect (Barletta 2009).

2.3.1 Vibration Force Assisted AFM Process

In the hybrid vibration abrasive flow machining process, the media is extruded to and fro through two media piston-cylinder arrangement and the process is assisted with the help of vibration force. In the paper, the workpiece was in vibration motion orthogonal in direction to media flow. The frequency is in the range 5-20 kHz. Responses were velocity, pressure of fluid, temperature, the pressure-velocity diagrams well explained the advantage of ultrasonic assisted abrasive flow machining over conventional AFM process. The temperature had no effect on the media stability (Gudipadu et al 2015). ANSYS FLUENT software was used to simulate the velocity, pressure and temperature distribution and CFD was used to study the path of flowing media.

2.3.2 Abrasive Assisted Electrochemical Process

Reinforcement particles has a significant effect in abrasive assisted ECM of Al-B-carbide graphite composite. Al composites are used in aerospace and automotive industries, boron absorbs neutron and graphite was added to improve tribology. In the paper, ECM was used and surfaces obtained were smoother as compared to that obtained by laser and electric discharge machining that produced het affected zone (Sankara and Babu 2014).  The abrasive particles in electrolyte solution increased the MRR.

2.3.3 Electrochemical and Centrifugal Force Assisted AFM

ANOVA was applied for significant parameters identification so that maximum material could be removed during machining process. The various input variable parameters selected were RPM, salt molal concentration, operating pressure, the pressure was kept at 6 MPa (Walia et al 2015).

2.3.4 AFM of Slit Fabricated by EDM

Analysis of variance (ANOVA) and signal to noise ratio (S/N) were used to identify significant combination of parameters so that optimum material removal and surface quality is obtained. After eliminating the recast layer produced by EDM, the optimum parameters were 150 µm, concentration of 50%, pressure 6.7 MPa and time of machining was 30 min (Tzeng et al 2007). If the concentration of media was high, the viscosity increased, thereby improving the surface finish of workpiece. The precision of surface was reduced due to high extrusion pressure.

2.3.5 Magnetic Field Assisted AFM Process and its Variants

2.3.5.1 Magnetorheological AFM

In this paper, applied magnetic field was used to calculate the normal force on abrasive grain, and microstructure of abrasive and magnetic particle was studied. The CIP chain around SiC abrasive particle was formed. The active abrasive particles actual participating in cutting action were calculated using developed model (Das et al 2008).  If the number of cycles and current was increased then surface roughness value was found to be decreased.

2.3.5.2 Ball-End MR Finishing Process

If MRP fluid was conditioned after several cycles of finishing operation, then it was forced to flow, otherwise the already stiffened ball end of fluid  continuously flow towards the tool tip (Singh et al 2012).

2.3.5.3 Double Disc Magnetic Abrasive Finishing of Paramagnetic Materials

Aluminium disc with 4 NdBFe magnets is used. Al is used as casing because permeability is 1, hence magnetic lines of force are not affected (Kala and Pandey 2015). The best surface finish results were obtained when working gap was 1 mm, 18% abrasive particles, speed 436 rpm for stainless steel, 36% by weight abrasives and 467 rpm speed. 1200 mesh size abrasives and feed 1mm/min resulted in best surface finish output.

2.3.5.4 MR Fluid Flow Behaviour

At different magnetic flux densities, the rheology graphs were plotted to analyse the flow pattern of the bidisperse fluid prepared (Niranjana and Jha 2014). The paper showed that bidisperse fluid has more yield strength and viscosity than monodisperse fluid.

2.3.5.5 Force Study in MAF

Ring dynamometer was designed and fabricated to experimentally study the forces acting during the finishing process. The material removal mechanism can be understood through this measurement. For recording the experimental data, Lab-view software was utilized (Singh et al 2006). If we increased the current supply to the prepared electromagnetic setup, the magnetic flux increased, subsequently the surface roughness and forces too decreased.  The machine setup was fixed on vertical milling machine. The Force study in magnetorheological fluid based finishing process was carried out. MRFF tool was mounted on CNC milling machine. Since the area of contact of MR fluid brush is high with curved work surface, hence the experimental values of forces measured were larger than theoretical ones (Sidpara and Jain 2013) [57]. The tangential and normal forces increased with increasing concentration of CIPs and abrasive particles Sidpara and Jain 2012).

2.3.6 Electrochemical Assisted AFM Process

In this process, viscoelastic polishing media is prepared containing NaCl as well as polishing abrasives. When the direct current supply is passed, the workpiece acts as a anode and the electrode is used a cathode. As per Faraday’s law of electrolysis, anodic dissolutuion of workpiece surface peaks takes place which softens the peaks of workpiece and mechanical abrasion takes place during the process.

2.3.7 Helical AFM Process

This is a slow process having low material removal rate and this limitation is overcome by the hybridization of the process, like Helical Abrasive Flow Machining process where drill bit is attached in the inner hole of work piece and held stationary. Lower and upper fixtures are tapered for proper media flow. The polymer media self deformability property affects the reshuffling and intermixing of the abrasive particles. The material removal is less due to small contact length covered by the abrasive particles flow. In hybrid process of helical AFM, further pressure from drill bit also makes the process more effective. There are three types of drill bits viz. splined, two and three start helical flute drill bit as shown in figure 2.3. The different flow patterns are observed like scooping flow, axial flow and flow along the flutes and this combination of flows result in removing the exact straight line path of movement of abrasive particles and increase the shearing of number of hard surfaces on the rough work to be machined and higher material removal is achieved.

(a)                              (b)                                 (c)                                   (d)

Figure 2.3 Three types of flows that in finishing zone (a) Flow Along Flute, (b) Axial Flow Motion, (c) Scooping, (d) all the three motions

The different innovations made in the field of AFM process are tabulated as shown in table 2.4.

Table 2.4. Innovations in the field of AFM

| S.No. | Topic | Work done |
| --- | --- | --- |
| 1 | Magnetorheological AFM (MRAFF) process (Jha et. al, 2007) | In this paper, principle of MRAFF process and the effect of extrusion pressure, number of finishing cycles on the Ra is studied. |
| 2 | Ellipsoidal particles’ pattern movements in AFM (Fang et al., 2009) | The ellipsoidal particles movement on the basis of equivalent circle is analysed. It includes sphere particle modelling, prediction of 2-D ellipsoidal particle in relation to rotating angle. Further oblate sphere approach alongwith particle in 3-body abrasion is analysed. |
| 3 | Bevel gears finishing (Venketesh et al., 2014) | For finishing bevel gears, AFM simulation is done and experimental procedure based on Taguchi analysis is done. Then effect of parameters on roughness is analysed followed by optimality check and surface morphology. |
| 4 | Magnetic pole arrangement study in Magnetic Abrasive Machining (Yoon et al., 2014) | Effect of surface finish w.r.t. abrasive mixing ratio, dry and wet processing conditions, spindle speed and magnetic pole arrangements is studied in detail. |
| 5 | MR fluid rheological characterization (Jha and Jain, 2009) | Magnetorheological polishing fluid rheological behaviour, characterization and experimentation alongwith capillary magnetorheometer design is done. The results of rheological properties’ variation with SiC mesh sizes and magnetic flux density are analysed in detail. |
| 6 | Surface roughness modelling and simulation in MRAFF process (Jha and Jain, 2006) | In this the chain structure and unit cell modelling is done, forces are analysed and surface roughness simulation is done. |
| 7 | Al/15% SiC-MMC finishing(Mali and Manna, 2010) | Here, response characteristics based parameters optimization, ANOVA for MR, Ra and decrease in Ra, development of mathematical models and SEM examination is done. |
| 8 | Micro channel surfaces finishing by AFM using self modulating abrasive medium (Tzeng et al., 2007) | In this paper, effect of media concentration, size, machining time on media viscosity is studied. In addition, abrasive mesh size, machining parameters, abrasive concentration, extrusion pressure, machining time effect on surface roughness is analysed. The wearing of abrasive on grain before and after AFM is done and shape precision is increased. |
| 9 | Temperature and specific energy determination in AFM (Jain and Jain, 2001) | The material removal mechanism, forces and specific energy, heat transfer in AFM process. |
| 10 | Steel pipe cleaning technology in AFM (Zhang et al., 2007) | Here cleaning of steel pipes was done using abrasive flow machining process. |
| 11 | Polymer abrasive gels development (Wang and Weng, 2007) | In this the effect of abrasive polymer gel properties, its effect during up and down cycles, abrasive concentration, mesh size is studied. Further, surface situation after AFM is studied and abrasive medium durable properties are analysed. |
| 12 | Micro-hole design and simulation in AFM (Li at al., 2009) | Here system designing is done, parts options, system power design is done. The process equipments key structure design including abrasive cylinder, common rail pipe fixture, AFM equipment overall structure design was done. Then finite element analysis of the components, common rail part modelling and simulation is achieved. Further entrance and exit condition exchange simulation, separate branch machining and four branch synchronous machining simulation is also done. |
| 13 | twin flapper nozzle valve injector nozzle prediction system in AFM (Yang and Sha, 2014) | Here processing parameters and quality interactional relationship including quality index, pressure, particle size, is analysed. The prediction model for injector nozzle, RBF network design, its training algorithm, sample data obtaining and pre-processing s done followed by network learning and system realization and experimental validation. |
| 14 | Laminated tooling conformal channels sealing and finishing using AFM (Williams et al., 1998) | In this PEL tooling, conformal cooling, its design specimen and then leak testing is done. Then material removal statistical analysis and 3-D surface profiling is done. |
| 15 | Nano-finishing of MMCs using AFF process (Shankar et al., 2009) | The effect of extrusion pressure, processing oil, number of cycles on Ra and MR is analysed. |
| 16 | Polishing and equipment study of AFM process (Yang and Zhao, 2007) | In this abrasive flow technology, polishing fluid, application and characteristics of abrasive flow, polishing equipment, micro hole flow polishing device is studied. In addition, polishing fluid preparation and micro hole surface roughness testing is done. |
| 17 | Mould softness structural surface machining using AFM (Tang et al., 2010) | The softness abrasive flow math model includes volume fraction equipment, additional scalar equation, turbulent kinetic transport equation, dissipation rate transport equation and boundary equation re studied. In addition, model calculation, initial conditions and grid division is studied. |
| 18 | Butyl rubber based media rheological characterization and performance evaluation for AFM process (Kar et al., 2009) | In this the experimental work included materials like abrasive, visco-elastic carrier, processing oil, metals used and the measurements include AFM setup, two-roll mill, pneumatic cutter, hydraulic press, AR 1000 rheometer and surface roughness tester. Then surface roughness was used to evaluate media, characterization of media and creep testing was done. |
| 19 | Rheology study of abrasive gel and its finishing behaviour in AFM (Wang et al., 2007) | In this paper, the finishing geometry is studied and coefficient of power law and simulation results of velocity, pressure, shear rate and shear forces is analysed in detail. |
| 20 | Complex holes uniform surface polishing (Wang et al., 2009) | In AFM process of complex holes, power law usage with and without mould core of chain hole, chain hole with two cylinders and chain hole with chain shape core is studied and analysed in detail. |
| 21 | AFM of micro slit fabricated by wire-EDM (Tzeng et al., 2007) | The machining time and media viscosity relation is analysed using signal to noise ratio, ANOVA and shape of surface and form of micro slit after wire EDM process is analysed. In addition, the effects of temperature, abrasive particle concentration and extrusion pressure on roughness of workpiece is studied. |
| 22 | Ultrasonic assisted AFM (UAAFM) process (Sharma et al., 2015) | Here material removal mechanism is understood in detail, alongwith machine setup, media and workpiece preparation, measurement and characterization. Then process parameters are selected for regression analysis and the finishing through AFM and UAAFM processes are compared. Afterwards X-ray diffraction analysis and SEM of machined surfaces is done. |
| 23 | AFM application in gas turbines (Perry and Stackhouse, 1989) | In this paper, it was found that abrading was highest where media velocity was greatest. The turbine applications included airfoil polishing, edge radiusing and removal of thermal recast surfaces. |
| 24 | Polygon holes helical passageways AFM study (Chen and Cheng, 2014) | Here, material property, internal helical motion, and simulation results including helical grooves different numbers, helical passageways on square, hexagonal, octagonal hole effects were studied and compared with the corresponding experimental results. |
| 25 | CFD simulation and process modelling in AFM (Wan et al., 2014) | In this, modelling methodology approach of media flow governing equation, abrasive media rheology model, material removal model, wall slip model are built and then extraction of model constants and the equations solutions are obtained. Then extracted models, experimental and simulated setup results are compared. |
| 26 | Ra and MR modelling (Jain et al., 1999) | Media flow modelling constituting basic continuity i.e. mass conservation equations, non dimensionalization, formulation of finite elements and boundary equations were generated. |
| 27 | Surface roughness prediction simulation in magnetic AFF process (Wani et al., 2007) | Here mathematical modelling including governing equation, modelling of machining pressure, material removal and surface roughness is done followed by experimental validation. |
| 28 | AFM process modelling on ceramic materials (Uhlman et al., 2009) | In this the technological investigation of the process in simple structures, complex structures surface formation and process model was developed. |
| 29 | AFM modelling and energy efficiency (Kenda et al., 2014) | The AFM of gear manufacturing, novel AFM upgrade to AFM mm was done followed by energy efficiency of both processes and geometrical and fatigue results. |
| 30 | AFF of stereolithography prototypes (Williams and Melton, 1998) | Here rapid prototyping of streolithography is done and flatness and other results were recorded alongwith scanning electron microscopy and data dependent system analysis. |
| 31 | New nozzle AFM machine tool (Bin et al., 2012) | Here the working mechanism of nozzle AFM tool and its control algorithm comprising flow coefficients, intelligent control algorithm, control system development platform and control system software is generated. |
| 32 | Small hole abrasive flow ultra precision polishing technology (Zhang et al., 2009) | In this study the AFM equipment and clamp was designed and media was prepared and the process parameters i.e. extruding pressure and extruding range and time were measured. |
| 33 | Micro hole AFM based on Delphi language (Li et al., 2009) | The motion control method of AFM was based on system design, software design and experimental test results. |
| 34 | Plastic gear matrix polishing using AFM (Kenda et al., 2014) | It included CFD analysis of process, and surface roughness experimental results included gear tooth face profile, prediction models, plastic gears lifespan tests and analysis. |
| 35 | Work efficiency monitoring using temperature in AFM (Fang et al., 2009) | Here data comparison between AFM machine and test rig was done and effect of number of cycles, media viscosity on MR and surface Ra was studied. |

The literature review related to electrochemical, centrifugal force and magnetic field assisted AFM process, modeling and simulation of these hybrid processes and different media used was done and explained in the table 2.5

Table 2.5. Conventional and hybrid AFM processes

| Author and Year | Research Work Done | Parameters Used | Output Results |
| --- | --- | --- | --- |
| 1. | Abrasive Flow Finishing Process |  |  |
| R.E.Williams et al., 1998 | AE power = a × MRR, where a is a proportionality constant depending on tool and workpiece properties. Root mean square RMS AE = a × f × Ac1/2 ,where f is feed rate, Ac is tool contact area. |  | - The primary AE signal had a frequency 160 kHz due to the type of work material and formation of AFM flow lines. |
| Wang et al., 2007 | Lower cost and effective abrasive media were developed to enhance the roughness of wire electric discharge machined (WEDM) surface. | Medium = P-Silcone, A-Silicone Workpiece = mold steel (SKD 11) | The surface roughness value will reach a minimum by utilizing high concentration medium, ex. The roughness value improvement will come to 84% only after 5 cycles by using A-Silicone with 60% concentration. |
| Bahre et al, 2012 | The goal is to improce surface quality and reduce stress concentrations at bore intersections due to abrasive deburring. | Medium : EM24640 Abrasive: Al2O3 Size : 300-600 µm | - The machined AISI 4140 workpieces showed a significant improvement in surface values Ra and Rz. |
| Chen & Chan, 2014 | Analytical model was developed to understand the abrasive media motion in different passageways using CFD-ACE software. | A-Silicone gel Abrasive: SiC Mesh size: 100# Weight %: 50 | Helical passageways can perform better than polygonal passageways even after polishing after only 5 cycles. |
| Ibrahim et al, 2014 | Taguchi concept, L-18 mixed orthogonal array is used to determine S/N ratio and optimize process parameters. | Workpiece: Al alloy Abrasive conc.: 25% Grain size: 355 µm Extrusion pressure: 8 MPa Number of cycle: 40 | - The optimim condition for maximum material removal is 140 mm stroke, 8 MPa pressure. |
| 2. | Electrochemical Assisted AFM |  |  |
| Jang et al, 2010 | An electrochemical polishing process using MR fluid was used to polish very hard materials like glassy carbon (GC). | Permanent magnet = Neodymium-iron alloy (NdFe) Flux density = 0.1-0.2 T) MR fluid = DI water based suspension of CI particles (42 vol%) | This process increased the MRR and improved the surface roughness by 14 times as compared to conventional process, which suggest that the oxidized layer was much softer and electrochemically more active than the bulk GC material. |
| Yang et al, 2011 | The paper presented a new electrochemical micromachining method that use mineral water as an electrolyte. The process is a green machining, high precision and low cost. | Electrolyte = mineral water Electric conductivity = 0.015 S/m pH = 7 Water hardness = 33.1 Voltage = 30V Workpiece = stainless steel (SUS304) Tool = WC | - The advantage of using mineral water as an electrolyte is that is unpolluted, low cost, no corrosion and wear of machine tool. - A WC micro pin with dia. 25µm is obtained from 300 µm dia. In 10 min. |
| Paul & Hiremath, 2013 | The effect of process parameters of ECDM on MRR is studied on borosilicate glass. As MRR is non linear, RSM is used for process parameters optimization. | Voltage = 50-70V Electrolytic concentration (% wt.) = 20-30 | - TWR decrease with increase in concentration - TWR increases with increase in voltage as most of heat will be dissipated through tool materials than through workpiece or electrolyte. |
| Brar et al, 2015 | The paper is about the development of novel hybrid of ECM and AFM, i.e. electrochemical- aided abrasive flow machining (ECA2FM) process. The various parameters have been optimized based on Taguchi method and using standard L27 orthogonal array (OA) | Voltage = 0-15V Salt molal concentration = 0.75-1.25 M Abrasive grain size = 100-200 mesh | - A fast ECA2FM process requires less number of cycles. |
| 3. | Magnetic Field Assisted Abrasive Flow Finishing |  |  |
| Sehijpal et al, 2002 | The paper reported the results of mixed factorial design experimental study to understand the MR and wear behavior, with the help of scanning electron microscopy (SEM). | Extrusion pressure = 15 bar Media flow rate = 450cm3/min Abrasive conc. = 1.5:1 | - The interaction magnetic field of no. of cycles is significant for Al but insignificant for brass. - The MRR from brass in AFM and MAAFM is higher than that for Al. |
| Taweel, 2008 | In the paper, integration of electrochemical turning (ECT) and magnetic abrasive finishing (MAF) was done that improved MRR and Ra. It also emphasized RSM model for correlating the influence of magnetic flux, voltage on MRR and Ra of 6061 Al/Al2O3. | Tool = brass Voltage = 8-24 V Electrolytic pressure = 0.4 MPa Electrolyte = 20% Na2NO3 Magnetic abrasives = Al2O3(1.5µm)+ steel (150µm) | ECT-MAF process resulted in material removal rate of 68 mg/min and surface quality less than 0.15µm. |
| Givi et al, 2012 | 3-level factorial method was used to investigate the gap between poles, cycles and magnetic abrasive powder on finishing of aluminium piece. | Magnetic abrasive powder mesh size: 100-140 # Weight of abrasive: 1-3 g | The higher rotational speed of poles improved the surface quality in MAF process, the ideal parameters to achieve optimum condition were 3 number of cycles, 1.5 mm of working gap and 2 g weight of magnetic abrasives. |
| Amineh et al, 2013 | The magnetic abrasive finishing (MAF) is used for removing recast layer. In addition, regression based equation is used to indicate relation between surface roughness and recast layer thickness. | Voltage: 110 V Pulse off time: 35 µs Servo: 30 V | - The recast layer removal and surface roughness improved by increasing abrasive particle size. |
| Judal & Yadava, 2013 | The objective of paper was to simulate cylindrical electro-chemical magnetic abrasive machining (C-EMAM) for magnetic stainless steel (AISI420). | Current to electromagnet = 0.5-2.5 T Electrolytic current = 0.5-2.5 T Electrolyte = 20% dilute Na2NO3. No. of turns = 2000 | - The normal and tangential cutting forces developed due to magnetic field are more at edges of magnetic poles. |
| Yamaguchi et al, 2014 | In this paper, it is shown that magnetic abrasive finishing (MAF) improved surface roughness with minimum material removal, while maintaining surface functionality. | Magnetic particles: steel grit (700 µm), iron particles (44-105µm), 0.5 g total Abrasive: 0-1 µm diamond paste, 40 mg. | Mixing large and small particles is best method to adjust magnetic force, and smoothing with minimal material removal is essential for coated tool finishing. |
| 4. | Centrifugal Force Assisted AFM |  |  |
| Walia et al, 2008 | The paper presented a mathematical model developed to calculate number of dynamically active particles participating in finishing operations in AFM and centrifugal force assisted AFM. | Extrusion pressure = 40 bar cycles = 3 Shape of CFG rod = rectangular Speed = 72 rpm | - Modification of distribution pattern of abrasives cause more particles taking part in abrasion. - Number of dynamically active grains in the media increase due to centrifugal effect. |
| 5. | Abrasive Laden Polymer Media Used in AFM |  |  |
| Tzeng & Yan, 2007 | SiC | Stainless steel (SUS 304) | Silicone oil Polymer, wax medium |

In table 2.6, the output results in case of various hybrid abrasive flow machining processes  are explained clearly.

Table 2.6. Output results obtained in various hybrid AFM processes

| S.No. | Author, year, area of research/ process | Output results |
| --- | --- | --- |
| 1 | Jui et al, 2013, ECDM [35] | The surface roughness less than 100 µm was achieved during machining on glass. If the concentration of electrolyte was decreased, tool wear and hole taper were decreased by 39% and 18% respectively. |
| 2 | Yang et al, 2011, Eco-friendly ECM [36] | Production of micro pins of size 20-30 µm from pin of 300 µm using ECMM was done in 10 min. |
| 3 | Kurita and Hattori, 2006, EDM and ECM/ECM lapping [4] | surface roughness was improved upto 0.07 mm |
| 4 | Mathew and Sundaram, 2012, Pulsed ECM [38] | High aspect ratio of 280-450 was achieved when fabrication of tools was done. |
| 5 | Walia et al, 2015, EC2A2FM [33] | The time of machining was reduced by 70%, hence the cost was largely reduced, maximizing the production rate and profitability. The obtained Ra was in the range 0.5-0.6 Ra. |
| 6 | Singh et al, 2012, Bal-end MR finishing [53] | The surface roughness was reduced upto 16.6-123.7 nm for 60 passes of finishing on ferromagnetic surfaces. |
| 7 | Singh and Shan, 2002, Magneto-AFM [59] | It was found that material removal increased more with magnetic flux as compared to improvement in surface quality. |
| 8 | Taweel, 2008, EC turning MAF [46] | surface roughness of 0.15 µm was achieved. |

Summary

- The electrolytic process is explained alongwith electrolyte used and Lorentz force study.

- The electric discharge process including micro EDM, wire EDM and magnetic EDM processes are studied in detail.

- Various hybrid conventional and non conventional processes included electrical grinding, centrifugal EDM, electrochemical turning processes, etc.

- Further the variants of AFM process included the use of vibrational force, magnetic force and magnetorheological AFM processes are studied.

CHAPTER 3: PROBLEM FORMULATION

This chapter deals with the formulation of problem and research objective after thoroughly finding the gaps in the past research. Further the research methodology i.e. the steps of working is detailed. The present investigation of hybrid AFM process both experimentally and mathematically is successfully done and the results are briefed in the following chapters.

3.1 Research Gap

- On thorough scrutiny of the published research work on magnetic field assisted abrasive flow machining (AFM) and electrolytic finishing processes, it has been observed that the finishing forces during processing has not been controlled by external means. Hence, material removal as well as surface roughness has not been controlled during processing. So, sufficient efforts are required towards the study of combined electrochemical and magnetic field assisted abrasive flow machining (AFM).

- The parameters that affect ECM are poor source characteristics, electrolyte properties, electrodes, their relative positions. It is observed that individual as well as collective effects of several parameters are still not fully understood.

- Several mathematical and empirical models have been developed pertaining to prediction of material removal and surface finish, however most of them are specific and can’t be generalized. Hence, comprehensive modeling and simulation of ECM is necessary.

- The enhancement of performance of ECM in terms of surface finish and material removal using magnetic field have been demonstrated but many of them need complete exploration.

- The parameters related to electrolyte and work/tool characteristics are responsible for the surface generated, hence elaborate studies are needed on them.

3.2 Research Objectives

In light of the above-mentioned gaps, the present investigation aims to analyze electrolytic and magnetic field assisted abrasive flow finishing with the following objectives:

- Design and development of the magnetic field assisted electrochemo abrasive flow finishing (MFAECAFF) set up.

- Development of new abrasive laden polymer media and study their rheology.

- To study the effect of variation of various process parameters (i.e. magnetic field, concentration and type of electrolyte, type of media, extrusion pressure and No of cycles etc)  on the response such as material removal and surface roughness.

- Multi-response optimization various process parameters of developed Hybrid MFAECAFF process.

- To model and simulate the design of magnetic field assisted electrochemo abrasive flow finishing (MRAECAFF) process.

3.3 Research Methodology

- In the present research, the authors have fabricated hybrid electrochemo magneto rotational abrasive flow machining setup and experimentation was done using newly developed polymer media based on SBR, natural, nitrile, PBS and silicone rubber.

- RSM technology was employed to arrive at the result that which of the developed media suits best in terms of material removal. Then experimentation design was developed based on Taguchi L9 OA and experiments were performed on the developed hybrid machine setup.

- Then the output results, i.e., MR and Ra were analysed in detail, i.e., effect of magnetic flux, ECM rod size and voltage on output results were analysed graphically.

- Further, Matlab fuzzy logic optimization, gray relational analysis approach were also utilized and the results were compared so as to arrive at the best optimized result.

- Apart from experimentation, the mathematical and computational modeling of the developed EMR-AFM setup is also done in detail.

- The voltage, magnetic flux, flow parameters and cutting forces are calculated and computational flow dynamics of developed EMR-AFM fixture is also done, alongwith various physical models and algorithms.

CHAPTER 4: EXPERIMENTAL INVESTIGATION OF EMR-AFM PROCESS

In this chapter the hybrid experimental machine setup is described in detail and then experimental design is elaborated based on which the experiments were conducted. The different type of polymer media preparation and characterization is also described. The rigorous experiments were conducted on different hybrid AFM machining parameters and the data collected in terms of material removal and surface roughness were analysed in extensive manner.

4.1 Design and Analysis of Experimental Work

In experimental design i.e. Design of experiments (DOE), the control of experimental work is there and experiments are performed in planned manner. This was invented in 1920 by Ronald and analysis of variance technique was applied to increase crop yield and the orthogonal array (OA) was used mostly by Taguchi.

4.1.1 Taguchi’s Method

The process variation by robust experimental work was studied in Taguchi method to fulfil the aim of high production. The Japanese scientist Taguchi developed the effect of parameters on mean and variance and decided the levels of parameters that allowed the data collection for minimum number of experiments to obtain best results.

### 4.1.2 Taguchi Method Philosophy

In any product, quality is an important criteria and parameter design play a vital role in deciding product quality levels and quality is increased by minimizing the deviations from set goal. The signal to noise ratio should be high and the cost of quality will be the measure of deviations.

### 4.1.3 Taguchi Method DOE

Firstly, process objective is defined i.e. maximum or minimum, the parameters affecting the process are defined. Those may be fixed or variable and their levels are decided so that orthogonal arrays are created for the same. Then the experiments are conducted for data collection and analysis of data is done for determining parameters effect on the output process response.

4.1.4 Strategy of DOE

The parameters are interactions are assigned to the suitable OA in the columns using triangular tables and linear graphs. The main effects of all the parameters are studied and analysed to arrive at the optimum condition and the contribution of every parameter is considered. The percentage contribution of each parameter is decided by analysis of variance (ANOVA). There are two methods adopted and suggested by Taguchi i.e. two routes one single run experiments, their average taken and main effects studied through ANOVA and raw data analysis. The other route is multiple runs using signal to noise (S/N) ratio principle.

4.1.5 Loss Function and S/N Ratio

The quality loss is defined by loss function by Taguchi. The Taylor series expansion was used to calculate loss function which is calculated as

Lo(z) = k(z-n)2

In case of mass production, Lo(z) = [k(z1-n)2 + k(z2-n)2 + .......... + k(zn-n)2]

where z1, z2,...,zn are characteristic values for 1,2,...n units respectively, n are number of units.

The above equation can be written as Lo = k. MSD,

where MSD is average of square of all deviations.

4.2 Design and Fabrication of Magnetic Field Assisted Electrochemo Abrasive Flow Finishing Setup

The set up comprises of a nylon fixture that supports three pole electromagnet arranged with their poles arranged at an angle of 120° with one another. The different elements of the designed set up are:

- Fixture: The fixture was designed and fabricated in such a way that it can hold the workpiece properly inside the bright bar and the poles of the electromagnet are arranged at the outer periphery of the bright bar cylindrical piece. The fixture is made in two parts upper and lower part. The material of fixture is nylon. The top view and side view of the fixture is as shown in figure 4.1(a), (b).

(a)                                                                    (b)

Figure 4.1(a) Top view of lower fixture, (b) Side view of fixture

The 3D model of the fixture, i.e. solidworks model is as shown in figure 4.2 (a) while the dimensional details are shown in figure 4.2 (b).

- (b)

Figure 4.2 (a) 3D model of fixture, (b) Dimensional details of the fixture

The different view of the fixture are as shown in figure 4.3.

Figure 4.3 Different views of the fixture

- Poles: The poles of magnet are made of soft iron. More the thickness of the pole, more is the capability of retaining magnetic flux. The thickness of each pole is 18 mm (figure 4.4).

- Solenoid: The solenoid is made of copper wire (19 gauge). More is the gauge of wire, lesser is its diameter. The optimum wire gauge to produce maximum magnetic field is 19 gauge, if lesser than 19 gauge wire is used, the current will be high and it will cause heating and the efficiency of electromagnet will be used. The number of turns on each electromagnet is 2200. The three electromagnets are arranged in such a way that they point at the center of the fixture and the magnetic field is focused at the centre towards the workpiece. The developed electromagnet is shown in figure 4.4.

pole

19 gauge Cu wiring (2000 turns)

Figure 4.4 electromagnet

- Workpiece holder: It is made of bright bar material that has high magnetic susceptibility and it has the property to retain the magnetic field, hence the losses are less. It is shown in figure 4.5.

Brass workpiece

Bright bar material to hold workpiece

Figure 4.5 Bright bar cylindrical piece supporting workpiece

This material helps the magnetic field produced inside the electromagnet to properly get focussed on to the workpiece.

- AC Transformer: The AC transformer supply (shown in figure 4.6) is provided to give variable supply to the electromagnet so that variable magnetic flux density is obtained. The various output voltages at the transformer are set at 40, 65, 98, 130, 167, 200 V.

- (b)                                      (c)

0-200 V

Figure 4.6 (a) AC power supply transformer, (b) voltmeter, (c) Ammeter

- Electrode: In order to achieve electrochemical reaction, workpiece is made anode, while cathode is retained inside the workpiece. This electrode is made of aluminium, as shown in fig.4, it is permanently fixed i.e. welded on one side of the fixture in the axial direction, while it is screw-tightened on another side with the help of mild steel thin stripper plates.

- AC to DC transformer:  This transformer is used to supply DC current to electrolytic set up, the anode. i.e. workpiece is given positive connection while the electrode is connected to the negative terminal. The different output voltages provided on this transformer are 6V, 12V, 18V and 24V (figure 4.7).

18 V

12 V

6 V

Common terminal

Figure 4.7 AC to DC transformer supply

- Voltmeter (Amco SR-72 P.T.R.) =  0-300 V. it is connected in parallel to check the voltage.

- Ammeter (Priya 23 V.K.) = 0-20 A. it is connected in series for current measurement. The voltmeter and ammeter are shown in figure 4.7 (b), (c).

- The set up consists of three solenoid electromagnets as shown in figure 4.8. The starting ends of these three electromagnets are attached to each other and this node 1 is connected to a wire whose other

Nylon fixture

electromagnets

Stripper plate acting as cathode for ECM assisted AFM

Figure 4.8 Electrochemo magnetic fixture set up

4.2.1 Fixture Development and Fabrication Design

The fixture was designed and fabricated in such a way that it can hold the workpiece properly inside the bright bar and the poles of the electromagnet are arranged at the outer periphery of the bright bar cylindrical piece. The fixture is made in two parts- upper and lower part. The material of fixture is nylon. The proper selection of material for fixture manufacture is the first and foremost step in AFM process. A number of materials were tested and analyzed for its proper working, the materials were 6061 Aluminum, 7075 Aluminum, POM (AKA Polyoxymethylene, Accetal and Delrin), Turcite, Nylon, High density polyethylene, G10 (AKA Garolite) Machinist wax, Stainless steel, Teflon. The choosing of material for test and production processes fixtures is a vital process. 6061 Aluminum has best balance between cost, machinability and strength, easy to work and machining. POM, Acetal and delrin absorbs little moisture and chemically resistant to every material, hence not used. Turcite is a form of teflon, it has low coefficient friction it is preferable to use over teflon due to hugh rigidity properties. Out of these materials Nylon 66 was selected for manufacturing for workpiece fixture. It absorbs high amount of moisture. Nylon can easily be bonded, this property makes it worth as compared to other materials.

      - Design Explanation

The top view of the fixture clearly indicates the location of bright bar and the seat of workpiece inside the hollow slot given in the nylon fixture, three additional holes provided at the periphery of the fixture are provided to attach more than one fixture to each other using screws, so as to provide proper rigidity to the clamped fixtures and job. In the side view of fixture, two fixtures are clearly shown attached to each other, the upper fixture thickness is lesser as compared to lower fixture. In the lower fixture, three 18 mm through holes are drilled at the periphery at 120o to each other. The upper fixture is made to fix into the media cylinder of AFM setup, for this purpose, 7 mm height surface of diameter 70 mm is provided so as to tightly clamp inside it. The abrasive laden polymer media is given extrusion force by the reciprocating piston cylinder arrangement of AFM setup, that ultimately pushes the media through the inner walls of workpiece. The media first enters the upper fixture, for that a tapered hole of 29o is provided upto the depth of 15 mm so that a jerk is not experienced by the workpiece and hence efficient finishing process is obtained.  The 3D model of the fixture, i.e. SolidWorks model is as shown in fig.2 (b). The model of fixture was prepared on the SolidWorks software before starting the manufacturing of fixture in workshop. The different machines used were lathe, milling, drilling, power hackshaw, CNC, etc. The different operations utilized were slotting, knurling, cutting, turning, facing, centering the drilling, reaming, boring, finishing, etc. The different tools used were single and multi-point cutting tool, boring tool, different sized drill-bits, hackshaw blade, milling cutters, various holding devices and accessories, collets, etc. Since before manufacturing, proper design of fixture is required after complete testing, hit and trial methods, hence accurate design software selection was essential. All the design work was done on SolidWorks software, it took lesser time and gave accurate and better results and was comfortable to use. Initially the central axis was selected and then all dimensions were applied and rotation command was implemented so as to obtain the design of circular fixture required.

4.2.1.2 Fixture Modelling

The Ansys software was utilized for simulation so as to solve the problem of compliance of clamping workpiece under dynamic forces acting during the extrusion forces in abrasive flow machining. The aim of developing model was solved in order to optimize results. Load capacity of fixture was tested during experimental test run on the AFM setup. In addition, industrial application like fixture reliability was checked. The geometrical design of nylon fixture was taken and subjected to impact forces and deformation during testing, shown in figure 4.9. Operations included meshing and deformation using methods like Finite Element Analysis.  For creating magnetic pull at the inner surface of the workpiece permanent magnets of cylindrical shape hacing dimensions of 10x10 are used.

- (b)                                                           (c)

Figure.4.9(a) Object free meshed in Ansys, (b) Fixture, (c) nylon fixture

Drill bit attachment for centrifugal force. For creating centrifugal force inside the workpiece a drill bit of dia.4mm is used and is modified to erect it accurately inside the workpiece. The electrochemical based magnetic field assisted abrasive flow machining set up consists of three fixtures, made of nylon material. Dimensional analysis of the working AFM set up: the distance travelled by magnetic force lines = workpiece thickness, A = 1 mm, the angle between the three solenoid electromagnets = 120o. The pole material is made of soft silicon iron, having better magnetic properties. It is cylindrical in shape.

4.2.2 Fixture and Electromagnet Design and Development

The electromagnetic and magnetic assisted AFM process utilizes fixture to hold workpiece that results in improved material removal, which are shown in figure 4.10 to 4.12.

Figure 4.10. Developed electrochemical and magnetic assisted AFM fixture

Figure 4.11. Top view of the fixture

Figure 4.12. Developed electromagnetic solenoid design

4.3 Hybrid AFM Experimental Setup

The set up comprises of a nylon fixture that supports three pole electromagnet arranged with their poles arranged at an angle of 120° with one another.

Figure 4.13 Sketch of fixture incorporating electromagnet and ECM tool

In figure 4.13 hybrid fixture sketch is shown and the hybrid AFM setup as shown in figure 4.14 comprises of a pair of extrusion machine piston cylinder arrangement and a pair of media cylinders in which prepared abrasive laden polymer is filled and fixture alongwith electromagnetic coils in between is shown. The transformer for electricity supply to the magnetic system is also arranged in the machine setup. The ammeter and voltmeter for current and voltage output readings respectively are connected. The ammeter is connected in series while voltmeter is connected in parallel in circuit diagram.

Similarly, the ending points of all the three electromagnets are connected to each other to form node 2, this node is connected to a wire whose other end can be connected to any of the six output voltage terminals viz. 45-200V so as to receive different magnitude of magnetic flux on the electromagnets. Further, node 1 and the output port of the transformer are connected to the mains AC 220V supply. The full system including ECM working and effect of magnetic current in the fixture holding workpiece i.e. brass, Al, C.I., M.S., etc. is shown in figure 4.14. The electromagnetic solenoid is shown clearly on the left part of the drawing, these are three in number, circumferentially placed at equal angles to one another with their unwrapped part inside the nylon fixture and the copper wire portion outside. The bright bar which is paramagnetic in nature is fixed around the workpiece. The thickness of pole of solenoid is 18 mm, the copper turns are upto the thickness 58 mm from the axis, situated at a distance of 60 mm from the top surface of fixture and the tapered portion of the fixture is upto the depth of 35 mm from the surface that fixes into the media cylinder.

4.3.1 Working of the Hybrid Setup

During working the following parameters were kept variable: Workpiece: Brass, Abrasive: SiC, Grain mesh size: 300#, Extrusion pressure: 45 bar, Volume of media used: 192.3 cm3. The constant parameters are chosen such that their values does not change and have not any significant effect, here workpiece, quantity of media, piston force, abrasive and its size are selected. The other factors that were kept variable are cycles, flux density, shape and size of rod, voltage and media. To analyze effect of these parameters it is important to select which type of table must be chosen in Minitab Taguchi software to get the best possible optimized output results in terms of material removal rate and surface integrity. A number of orthogonal array were studied for different number of parameter taken and their number of levels. The brass rod is taken firstly and then this rod is taken to Anand Parbat market, Delhi where industrial area lies and big machinery is installed. The rod is somehow clamped between supports on lathe machine and through boring is done and simultaneously cut into piece of size 16 mm. Since the internal surface of the prepared piece is not so smooth and requires post finishing process, hence the non-traditional machining process i.e. abrasive flow finishing (AFF) process is done on the prepared machine setup in Precision engineering laboratory, that will produce highly finished surface as compared to traditional machining process applied earlier that included drilling, boring and reaming. The large number of workpieces of brass material were obtained, out of this lot, selection of nearly equal surface roughness value pieces are selected for AFM experimentation. In the present experimental work, 18 workpieces are selected on which hybrid AFM has to be performed, their initial surface roughness value tested on roughness tester machine was found to be in the range 1.65 µm to 1.99 µm, the initial weight measured were in the range 3.7684 gm to 3.949 gm. After performing machining, the roughness values obtained were in the range 0.90 µm to 1.92 µm, while the final reduce weight obtained was in the range 3.6921 gm to 3.7491 gm.

(a)

(b)

(a), (b) ECM-Rotation fixture

(1)

(2)

(3)

Media used (1) NR, (2) SBR, (3) NT

Stripper plate acting as cathode for ECM assisted AFM

Transformer

Media cylinder

Electromagnet

Nylon fixture

Extrusion cylinder

Figure 4.14 Hybrid EMR-AFM set up

- (b)

(b)

(a)

100

128

80

28

70

10

10

18

Copper wire

Iron core

Wood

White plaster

78

Figure 4.15 (a) Electromagnetic solenoid used in machine setup       (b) Media characterization 									           (a) FTIR, (b) SEM and TEM image

The dimensions of electromagnetic solenoid is explained in detail in figure 4.15 (a) and particulars of media used is as depicted in figure 4.15 (b). the machine in-built parameters that are fixed are given in table 4.1.

Table 4.1 Machine parameters and units

| Machine process parameter | Unit | value |
| --- | --- | --- |
| Extrusion cycles | No’s | 1-9 |
| Temperature | oC | 30-35 |
| Pressure | kg/cm2 | 200 |
| Machine capacity | tonnage | 25 |
| Hydraulic cylinder bore | mm | 125 |
| Maximum pressure | MPa | 40 |
| Media volume | cc | 300 |
| Extrusion cycles | No’s | 1-9 |

4.3.2 Principle Operation and Characteristics of the Magnetic Setup

During the working operation, the magnetic lines of forces act towards the workpiece whose internal wall surface has to be machined. In order to provide more focusing magnetic force towards the centre, the workpiece is placed inside the hollow cylindrical piece made of paramagnetic material, usually known as bright bar. The main aim of our model is to achieve high material removal and better morphological characteristics, which requires the development of electro-magnetic model. As the current supply to the developed solenoid arrangement is varied, the magnetic force gets changed. Taking all the parameters in electrochemical and magnetic force assisted AFM into account, the following assumptions are taken while writing mathematical equations. The magnetic field domain inside the workpiece is symmetrical about the axis. Both cathode (cylindrical rod) and anode (workpiece) are conducting in nature. The supply of current in the solenoid coils is assumed to be constant. The magnetic abrasive particles are considered spherical- shaped. According to British standard wire gauge: 19 gauge = 0.040 inch = 1.016 mm diameter. Resistance of 19 gauge wire = 0.0264 ohm/m, at 20 ‘C. Copper density = 8.96 g/cm3 or 0.324 lb/in3.

4.3.2.1 Fixture and Electromagnet Design and Development

The electromagnetic and magnetic assisted AFM utilizes fixture to hold workpiece that results in improved material removal. The nylon fixture has been manufactured on lathe machine, shaper machine, milling, drilling machine. The size, shape and specification of the fixture is decided on the basis of requirement for setting up the job and the abrasive flow finishing requirement. The developed electro chemical and magnetic assisted AFM fixture different views have been shown in figure 4.13. The upper fixture when seen from the front side has length 90 mm, height 18 mm. This fixture when seen from top has outer diameter 90 mm whereas inner diameter 35 mm. The middle fixture has length 90 mm and height 58 mm, the hole of diameter 18 mm has been bored at height 8 mm from bottom surface of the fixture. Inside the fixture, ECM road of varying diameter i.e. 4, 5, 6 mm inside the hollow bright bar of 35 mm diameter. The brass workpiece of outer diameter 10 mm and inner diameter 8 mm is fixed in the bright bar seat. On the top of the first fixture a metal strip of thickness 3 mm, length 50 mm and width 16 mm is fixed with the help of two bolted joints.

4.3.2.2 Development and Fabrication of Electromagnetic Solenoid

The developed electromagnetic solenoid design is shown in figure 4.16 It consists of ferromagnetic iron bar of diameter 18 mm and length 128 mm, having enameled copper wire of 19 gauge specification  wound around the bar upto length 100 mm and white tape is surrounded so that copper wire does not come in connect with any external material for safety purpose. The copper wire wound with the help of machine. A lot of problems were encountered while preparing solenoids. The electromagnet was prepared on different machines and the number of copper turns played a major role in magnetic field generation. It includes following steps. The fixing of wooden frame over the soft iron core.

- (b)

Figure 4.16 (a) magnetic fixture setup installed on AFM machine, (b) AC-DC transformer

4.3.2.3 Magnetic and Electrical Calculation of Electromagnetic Solenoid and Experimental Setup

Three ceramic capacitors of 104 pico farad, Capacitors of 470µF, 16V. Step-down transformer 12012, denoting 12V, 0,12V, 5408- 4 diodes used to build bridge rectifier, having filter capacitor (2200µF, 50V). Voltage regulator 7812 I.C. having 3 pins, 1st pin is input 24V, 2nd pin is ground, 3rd pin is output 12V Capacitors of 470µF, 25V, 555 I.C. (It needs 12V, othervise it will burn). Voltage/ Magnetic field sensor, Capacitor of 1000µF, 25V, Voltage regulator 7805, 05 denotes 5V output.

4.3.2.4 Initial Readings on the Machine and Calculation of Number of Turns

The 27 gauge copper wire turns are greater than that of 25 gauge in the prepared electromagnetic setup, higher the gauge number lesser is the thickness of wire and lesser will be the current carrying capacity and less will be the magnetic flux density. The copper wire is uniformly wound over the iron bar over a pre-decided length and number of turns is approximated because it is a vital factor in increasing the magnitude of magnetic field. 27 gauge copper wire electromagnet: No. of turns= 6720, 25 gauge copper wire electromagnet: No. of turns= 5800. Length of pole over which copper winding is done = 8 cm. Average number of turns on one layer= 128, total number of layers= 26. 1st layer: 8 turns made with the 1 foot(30 cm) length of copper wire, i.e. 0.2667 turns per cm, 2nd layer: 8 turns/ foot, i.e. 0.2667 turns per cm and so  on. Total no. of turns= no. of layers × no. of turns = 26 × 128 = 3328 turns. Total length of copper wire= 305.75 m. Voltage and Current Readings: The electromagnet showed 200V at 250 mA and 260V at 500mA, Copper wire resistivity= 1.7 micro-ohm cm.

(a) 			                         (b)

Figure 4.17 (a) Machine showing the number of turns, (b) electromagnet attachment

The circular views of fixture are explained and dimensioned. The ECM rod of variable diameter 4, 5, 6 mm is at the center, which is enclosed by bright bar of diameter 35 mm in which rod is centrally fixed. In another view, a 50 mm strip of width 20 mm having 5 mm holes on both sides in longitudinal direction. As shown in figure 4.17, the electromagnetic solenoid is fabricated inside a wooden frame. The size of iron bar is 128 mm long and 18 mm diameter. The portion of iron bar that was inside the fixture is of length 28 mm, this portion comes in direct contact with bright bar that holds the workpiece. The copper wire which is wound around the bar has 3300 number of turns that extends upto diameter 70 mm, the white plaster tape is finally wrapped around the copper wire.

4.3.3 Validation of the Concept of Electrochemistry Application in the Removal of Material

In the traditional methods, the electrolysis or electro-chemical action was utilized for electroplating purposes such as Zn plating or galvanizing process. According to this process, faraday introduced the concept of electrolysis that utilizes the flow of current and maintaining the closed circuit among anode, cathode and the electrolyte solution. In this method, the ions exchange occurs which causes the removal of material from one material and addition of the same on the other electrode. For this system, DC power source is required as shown in figure 4.18 (a). Present setup utilizes the above principle in reverse manner. The electrode set up has been fabricated in-house and separate power source i.e. transformer supply voltage 6V, 12V, 18V.

- (b)                                      (c)

Figure 4.18 (a) AC-DC rectifier, (b) ECM rod, (c) drill bit ECM rod

The alternating current that reverses direction periodically is converted into direct current flowing in only one direction using rectifier device. In motor generated set the AC motor shaft is coupled to DC generator. The multi phase alternating current is produced in armature windings, commutator on the armature converts it into direct output current. A transformer contains two magnetically coupled windings, the primary winding is driven by input AC supply, while the secondary winding give supply to AC-DC converter.

4.3.3.1 Electrolytic Assisted AFM Principle

In this process, the flow of polymer media mixed with electrolyte, inside the gap between cathode rod and the internal wall of hollow cylindrical job gets interacted with the electrochemical action between anode and cathode. The workpiece is made anode i.e. connected to positive terminal of DC supply, while the rod inside the workpiece is connected to negative terminal.

4.3.3.2 Decision of Cathode and Anode Selection

Since 65% heat is generated at cathode and 35% at cathode in DC power source, therefore the workpiece is selected as anode as more heat will be generated and the requirement of material removal from the workpiece is achieved. Since less heat is generated at cathode, hence the rod is connected to the negative terminal.  Cathode material: bright bar, mild steel. Anode material: brass, cast iron, aluminium, mild steel, Al-composite.

4.3.3.3 Selection of Electrolyte

The normal kitchen salt is taken as electrolyte in the molal concentration ratio 1:1. The electrolyte is taken in such a way that the material is removed only from the workpiece surface, and no material removal takes place from cathode rod. The electrolyte is non-toxic, ecofriendly and has good compatibility with the work and cathode materials.

4.3.4 Rotational AFM Setup

The working setup of rotational AFM system is clearly indicated in figure 4.19 and explained in details in further section. The two nylon fixtures are attached above and below the motor with the help of rotating bearings and through bore was done in the motor and nylon fixture in the form of hollow pipe is fixed inside it. This long hollow pipe is split into two parts so as to provide seat to the workpiece and this pipe rotates when the motor is started. The separate speed and frequency controller is installed in which the variable button is provided which can change the speed of rotation of motor and hence we can obtain another variable factor in the form of speed in RPM. These different factors are controllable and we use them in optimization software.

Fabricated structure to hold the motor

3-phase motor

Fixture supporting electromagnets

Figure 4.19 Working set-up, AC (220V) to DC (24V) transformer with 4 diodes: 3 for 3 electromagnet poles and 1 for electrolytic circuit

4.3.4.1 Fabrication of Rotational AFM and its Effect on the Efficiency of the Process

The motor is placed on the AFM machine setup to provide rotational effect on the machining process, on both sides of the motor the newly developed and fabricated fixtures are attached.

Figure 4.20 Electrolytic fixture showing spring-loaded rotating contact for anode

The electrolytic fixture is used to obtain electrochemical machining in which the workpiece is connected to positive terminal while the tool i.e. ECM rod is connected to negative terminal, i.e. work is anode and tool is cathode.

(a)                                            (b)

Figure 4.21 (a) Rotatioanal frequency meter, (b) Rotational AFM setup with fixture

Since we have employed rotational setup that will disturb the bright bar arrangement i.e. it is in continuous motion hence continuous contact should be maintained. For this spring-loaded attachment was prepared and through the spring, a conducting wire is passed and this is made to contact with bright bar with the help of C-shaped strip for proper connection as shown in figure 4.20. In figure 4.21 both rotational fixture and frequency meter installed is depicted.

4.4 Development of Polymer Media

The media available for commercial use is not cheap enough for experimentation, hence to achieve cost effective process, we need lower cost AFM media. This is prepared by mixing base polymer, plasticizer to make viscoelastic carrier

4.4.1 Preparation of Polymers

The preparation of all the polymers was done at “Two roll mill machine” facility in Shriram institute of industrial research, New Delhi. For preparing the flexible polymers mass, a fixed quantity of polymer is taken first and an appropriate quantity of plasticizer is added into it. This plasticizer is not added just all in once, rather it is added slowly and it is only added during the crushing and rolling of solid polymer in two roll mill machines. In order to prepare natural rubber polymer, 100 gm natural rubber is weighted. This natural rubber is available in the form of sheet.

4.4.2 Preparation of Media

Take 300 gram of polymer and 80 gram of gel and then it is mixed by hand properly. Then add 400 gram of Silicon Carbide and it is properly mixed with it. Thus the media is prepared. Other media i,e Natural Rubber, SBR Rubber, Nitrile Rubber and Natural Rubber are also prepared in similar manner, as shown in figure 4.22, 4.23. 4.24 respectively.

Figure 4.22 Natural Rubber based media

Figure 4.23 Styrene Butadiene Rubber based media

Figure 4.24 Nitrile rubber based media

4.4.3 Properties of Polymer Media

The media should have desirable properties i.e. it should not be sticky in nature and should not damage workpiece surface during high flow velocity and there should not be drasticchange in weight and roughness values. The media should be bouncy and should become spherical ball shape, further should have high temperature withstanding capacity during processing. The different types of media used have been explained in table 4.2.

Table 4.2 Different types of media used and their properties

| NR | SBR | SR | Plasticizers |
| --- | --- | --- | --- |
| Natural rubber or India rubber has viscoelastic property has isoprene plus organic impurities of water, isoprene i.e. diene 1,4 due to which is unsaturated. It vulcanizes with sulphur and has high tensile strength and used in heavy duty tyres, footwears, foam, etc. | Styrene Butadiene Rubber (SBR) is of two types i.e. emulsion based and solution based, ESBR and SSBR that depends upon the manufacturing process employed. It is used in making tyres as its is cost effective. | Silicone rubber (SR) is non reactive to difficult conditions, and can resist temperature upto 500 oC. During its preparation it passes through two stage manufacturing process to obtain shape and then cured and injection moulding is done. Hence due to its ease of getting shaped, it is used in food storage and automobile industries. | Plasticizers are added to polymer and they form polar attractive forces and chains. Its misxing is done in the ratio 10:27 and the plasticizers used are Dio iso Octyl Pthalate (DOP) and Dio iso Octyl Adiabate (DOA) |

4.4.4 In-house Preparation of CNT Particles and their Role in Material Removal Process

The characterization of CNTs that are iron filled is done through transmission electron microscope (TEM) is done after thorough study and synthesis and a new media is developed made of mixture of alumina, CNT and base carrier. Then chemical vapor deposition (CVD) is used to synthesize ferromagnetic particles and various characteristics are studied.

- (b)                                               (c)

Figure 4.25 (a) Abrasive laden Media (carrier+Al2O3+CNT), (b) preparation procedure, (c) fixture containing media

The newly developed abrasive media , hydrocarbon gel, aluminium oxide grain, polymer are mixed in specific quantity, the ratio of polymer to abrasive varied between 1 to 1.15. Then CNT particles in the form of additives in the weight ranging from 1 to 8 gram is added, particle having viscosity 800 Pas. In CVD process of ferromagnetic particles, ferrocene and toluene are mixed in an oven in the ratio 1:5 at temperature 900oC in the presence of argon gas. The media performance evaluation was done in precision Engineering Laboratory on abrasive flow machining setup. The three media were developed for experimentation, first media contained abrasive, polymer and gel, while in second and third media, 3 and 6 grams of CNTs were added as shown in figure 4.25. The SEM images shows that after addition of CNTs the sharp alumina edges of abrasive grain are clearly visible. These sharp edges are nothing bu cutting edges responsible for material removal from workpiece during machining process. When we do machining of cast iron workpiece then CNTs addition in media shows positive results in terms of material removal since CNT particles are more hard than alumina particles. When 3 gram CNT particles are added, roughness improvement is fair but further addition of CNT particle upto 6 gram drastically improve surface roughness of workpiece.

4.4.4.1 Carbon Nano Tubes (CNTs) Synthesis

Carbon nanotubes (CNTs) are carbon allotropes of cylindrical shape and Chemical Vapour Deposition technique is used to synthesze Fe-filled CNT shown in figure 4.26 (a) by heating the solution of  Ferrocene (5gm) and Toluene (25ml) in the oven, maintaining the oven temperature around 800oC and argon gas (100 sccm) is passed to get inert atmosphere, then  800oC temperature is maintained to completly vaporise the solution of  Fererocene and Toluene, as shown in the setup figure 4.26 (b). As solution vaporise completley the oven temperature is lowered by 25oC

- (b)

Figure 4.26 (a) Optimised condition to synthesize Fe-filled CNTs, (b) Thermal CVD Setup

As oven reached 775oC - 875oC carbon start dissociating and carbon layers get stick on quartz tube with sp2 bond. Then cooling is done slowly which takes aproximately 3hrs. After this the developed CNT layers is brushed and collected.The collected sample is tested for its magnetic nature by bar magnet, N & S  north and south pole respectively showing the deposited film having pole characterisitic means the botoom layer of film having N Pole while top layer of deposited film having S Pole. The methods used for synthesis is depicted in figure 4.27 and the CVD method is shown in figure 4.28.

Figure 4.27 Currently used methods for CNTs synthesis

Figure 4.28 Schematic showing CVD method to develop CNT

4.5 Experimental Investigation

4.5.1 Workpiece Preparation

Brass workpiece have been used in this research work for calculating the final output results. The workpiece taken is of outside diameter of 10 mm and length of 16 mm. The problems while preparation of workpieces and the strategy applied are shown in figure 4.29.

- (b)

Figure 4.29 (a) Preparation of job on lathe, (b) Drilling operation on lathe machine

Workpiece is prepared by first of all drilling of 7 mm drill bit and after that 1mm diameter is removed by the boring operation so that there will be clear boring tool mark, which is our aim to remove by finishing operation. The workpiece has internal diameter of 8 mm. The workpiece taken is of outside diameter of 10 mm and length of 16 mm. Workpiece is prepared by first of all drilling of 7 mm drill bit and after that 1mm diameter is removed by the boring operation so that there will be clear boring tool mark, which is our aim to remove by finishing operation. The workpiece has internal diameter of 8 mm. the machine used for preparing workpiece is as shown in figure 4.30.

- (b)                                         (c)

Figure 4.30 (a) machine used for preparation, (b) Drilled brass pipes, (c) Filing of Drilled brass workpieces

In this context, filing was done on the two circumferences of the tube-shaped pieces shown in figure 4.30 (c). Filing was carried out in all the hundred pieces just before weighing process. This was done in order to ensure removal of unwanted projections and deburring. As the pieces were cut from a single long tube using a hacksaw, surface irregularities tend to be present, which would have contributed to the weight. In order to get the accurate quantitative results, filing was carried out to smoothen the surfaces and chip off the irregularities. The measurement of weight and roughness of surface of workpiece was undertaken after suitable workpiece acquisition and preparation, which was followed by sampling to get fair 9 workpieces and were machined on AFM setup.

4.5.2 Measurements

Measurement in this project involved assigning quantitative values to the parameters of weight and surface roughness of all the 27 pieces chosen as explained earlier. The measurements will be later used for the sampling process. The device is shown in figure 4.31 (a).

4.5.2.1 Weight

Weight of each of the 27 pieces was measured using a digital weighing balance. Least Count of balance = 0.0001 gram. The initial readings are shown in table 4.3.

Table 4.3 Initial reading of the prepared workpiece

| Piece | Weight | Piece | Weight | Piece | Weight | Piece | Weight |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.027 | 8 | 1.054 | 15 | 1.129 | 22 | 1.115 |
| 2 | 1.136 | 9 | 1.082 | 16 | 1.033 | 23 | 1.092 |
| 3 | 1.062 | 10 | 1.041 | 17 | 1.059 | 24 | 1.134 |
| 4 | 1.114 | 11 | 1.006 | 18 | 1.114 | 25 | 1.083 |
| 5 | 1.187 | 12 | 1.143 | 19 | 1.088 | 26 | 1.257 |
| 6 | 1.179 | 13 | 1.102 | 20 | 1.146 | 27 | 1.045 |
| 7 | 1.078 | 14 | 1.070 | 21 | 1.247 |

4.5.2.2 Surface Roughness

The device used was Taylor Hobson Surface Roughness Tester as shown in figure 4.31(b). The surface roughness of each piece of the 27 pieces was measured three times and then averages to rule out fluctuations and errors in measurements. The roughness values are listed in table 4.4.

(a)                                             (b)

Figure 4.31 (a) Weight measurement device, (b) roughness tester

Table 4.4 Surface roughness values

| Piece | Ra-1 | Ra-2 | Mean | Piece | Ra-1 | Ra-2 | Mean | Piece | Ra-1 | Ra-2 | Mean |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 2.82 | 3.10 | 3.16 | 10 | 2.14 | 2.33 | 2.44 | 19 | 1.22 | 1.22 | 1.32 |
| 2 | 2.79 | 2.55 | 2.82 | 11 | 0.62 | 0.70 | 0.78 | 20 | 1.44 | 1.32 | 1.54 |
| 3 | 1.11 | 1.34 | 1.23 | 12 | 2.25 | 2.34 | 2.33 | 21 | 1.47 | 1.22 | 1.45 |
| 4 | 1.09 | 0.67 | 0.88 | 13 | 1.40 | 1.67 | 1.66 | 22 | 1.38 | 1.55 | 1.56 |
| 5 | 1.45 | 1.39 | 1.43 | 14 | 1.11 | 0.89 | 1.29 | 23 | 1.50 | 1.66 | 1.57 |
| 6 | 0.55 | 0.85 | 0.81 | 15 | 1.09 | 1.23 | 1.23 | 24 | 1.67 | 1.56 | 1.59 |
| 7 | 1.11 | 1.40 | 1.33 | 16 | 1.27 | 1.09 | 1.23 | 25 | 1.66 | 1.65 | 1.66 |
| 8 | 1.44 | 1.58 | 1.48 | 17 | 1.67 | 1.44 | 1.77 | 26 | 1.67 | 1.54 | 1.74 |
| 9 | 1.62 | 1.31 | 1.49 | 18 | 1.90 | 1.67 | 1.86 | 27 | 1.45 | 1.55 | 1.64 |

4.5.3 Sampling

Sampling is done to select a subset from the entire lot. 9 pieces hovering around the mean with minimum deviation from the mean were selected. Surface Roughness = 1.50 µm. the sampled pieces readings are shown in table 4.5.

Table 4.5 Weight and roughness readings

| Piece No. | Ra (µm) | Weight (gm) | Piece No. |  | Ra (µm) | Weight (gm) | Piece No. | Ra (µm) | Weight (gm) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3 | 1.23 | 1.062 | 9 | 1.49 |  | 1.082 | 13 | 1.66 | 1.102 |
| 4 | 0.88 | 1.114 | 11 | 0.78 |  | 1.006 | 15 | 1.23 | 1.129 |
| 6 | 0.81 | 1.179 | 12 | 2.33 |  | 1.143 | 16 | 1.23 | 1.033 |

4.5.4 Observations

The observations for each workpiece with respect to the parameters are listed. The workpiece material removal and surface roughness are calculated by using weighing machine and Taylor Hobson tester respectively. The workpiece number given in the table 4.6 shows the serial number of workpiece taken for experimentation purpose.

Table 4.6 Parameters and output MR results

| Exp. No. | Workpiece No. | Parameter Trial Conditions |  |  | Final Surface Roughness (um) | Final Weight (grams) | Material Removal (mg) |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Pressure (bar) | Extrusion cycles | Media to grit ratio |  |  |  |
| 1 | 3 | 10 | 2 | 1.15:1 | 0.64 | 1.067 | 2.6 |
| 2 | 4 | 10 | 4 | 1:1 | 1.08 | 1.077 | 2.8 |
| 3 | 6 | 10 | 6 | 1:1.15 | 1.11 | 1.054 | 2.6 |
| 4 | 13 | 20 | 2 | 1:1 | 0.74 | 1.034 | 2.5 |
| 5 | 9 | 20 | 4 | 1:1.15 | 1.22 | 1.144 | 2.9 |
| 6 | 11 | 20 | 6 | 1.15:1 | 0.67 | 1.134 | 2.6 |
| 7 | 12 | 30 | 2 | 1:1.15 | 0.45 | 1.187 | 2.7 |
| 8 | 15 | 30 | 4 | 1.15:1 | 0.02 | 1.003 | 2.8 |
| 9 | 16 | 30 | 6 | 1:1 | 0.23 | 1.104 | 2.8 |

4.5.5 Acquisition

The workpiece of specific size and specifications were to be acquired and prepared before experimental work and here aluminium workpiece material was selected for experimentation.

4.5.5.1 Justification for Selection of Material (Aluminium)

The work material details ae shown in table 4.7.

Table 4.7 Workpiece material specifications

| S.No. | Workpiece material | details |
| --- | --- | --- |
| 1 | Light weight | Specific weight 2.7 g/cc, its use reduces dead weight in vehicles |
| 2 | Corrosion resistance | Used in surface treatments like anodising, painting, etc |
| 3 | Electrical and thermal conductivity | Excellent, twice as good as copper with respect to its weight |
| 4 | Reflectivity | Good, used in rescue blankets |
| 5 | Ductility | Easily formed into close to product design |
| 6 | Impermeable and odourless | Can be rolled upto 0.007 mm thickness |
| 7 | Recyclability | 100%, its remelting requires 5% of energy required to produce primary product |

4.5.5.2 Justification of Selection of Shape of Workpiece

In AFM process, the media is extruded through the internal surface of workpiece under high pressure and the abrasion of material from surface depends on abrasive particle velocity. The cross section needs to be uniform throughout to obtain uniform machining. Hence the shape of workpiece needs to be hollow cylindrical piece, diameters taken as 10 and 8 mm outer and inner respectively shown in figure 4.32. Further the circular shape doesn’t offer much constriction of media challenge, hence the flow is smooth.

Internal obstructions are present

Velocity and flow is uniform

Figure 4.32 shows pipe flow profile

4.5.5.3 Pipe Purchase

The Aluminium pipes were Acquired from Chawri Bazaar, New Delhi from Shop No. 1, Ragunath Market. The age of the Aluminium pipes in the shop was around 4 weeks with very mild corrosion on the outer surface. Total length of pipe acquired was 9.5 feet cut into three smaller pieces. This signal may be displayed on both graph and screen outputs, together with numerical values that characterize the surface texture shown in figure 4.33.

Figure 4.33 shows roughness testing method

The surface roughness of each piece of the 27 pieces was measured three times and then averages to rule out fluctuations and errors in measurements.

4.5.6 Procedure

- The first three workpieces are machined at low pressure. Firstly, we fill the media into one of the cylinders of the two way AFM.

- Placing the workpiece between the two-piece fixture, we fix both the fixtures on the upper and lower jig such that they fit into the groove of the jig.

- We then fix this jig onto the AFM setup such that the cylinders are in line with the pistons with the help of the nut and bolt provision given.

- Subsequently, we set the pressure manually by using the handle for both the upper and lower side.

- After the pressure has been set, we manually operate the pistons with the help of the operating levers in accordance with the number of cycles required.

- After the machining is done, we unclamp and dismantle the fixture. We then remove the workpiece, clean it with cloth and give it an acetone bath and the surface roughness and weight is measured. The difference in weight gives us the material removal.

- For the rest of the six pieces, we repeat steps a) to f). The pressure and no of cycles are changed

- Clean setup after experimentation. Tabulate and analyse observations to get results.

4.5.7 Experimental design

In the advanced machining processes, various optimization techniques are applied, in order to get the optimized output response. In the present investigation, obtaining the higher material removal and lower surface roughness is the primary target of the designed hybrid electrochemical and magnetic force assisted abrasive flow machining set up. The controllable variable input parameters taken are electrochemical voltage, magnetic flux, shape and size of the electrochemical rod and the polymer media used. The workpiece, abrasive mesh size, number of cycles, extrusion pressure are kept constant.  Mixed-element Orthogonal Array OA L-18 (2'x3') method contains saturated OA, replacement of column and different matrices.

4.5.7.1 Plan of Experimentation

Taguchi L 18 orthogonal array was adopted for the experimentation to optimize the results. Six parameters were controlled in order to optimize results. The six parameters and their three levels are listed in the table 4.8. The parameters that were kept constant are:

- Workpiece: Brass

- Abrasive: SiC

- Grain mesh size: 300#

- Extrusion pressure: 45 bar

- Volume of media used: 192.3 cm3

The constant parameters are chosen such that their values does not change and have not any significant effect, here workpiece, quantity of media, piston force, abrasive and its size are selected. The other factors that were kept variable are cycles, flux density, shape and size of rod, voltage and media. To analyze effect of these parameters it is important to select which type of table must be chosen in Minitab Taguchi software to get the best possible optimized output results. A number of orthogonal array were studied for different number of parameter taken and their number of levels. For getting best result in case of the variable parameters taken, we reached to the conclusion that L-18 orthogonal array must be applied.

Table 4.8 Parameters with their levels used

| Parameters | Level 1 | Level 2 | Level 3 |
| --- | --- | --- | --- |
| - ECM rod shape | Drill bit | square | _ |
| - Size of ECM rod (mm) | 4 | 5 | 6 |
| - ECM voltage (volts) | 6 | 12 | 18 |
| - Magnetic field (in terms of volts) | 50 | 125 | 200 |
| - Type of polymer media | Natural | SBR | Nitrile |
| - No. of cycles | 3 | 6 | 9 |

In Taguchi L 18 OA, the number of experiments to be performed was 18 and first 9 experiments were conducted using drill bit shaped ECM rod placed concentrically inside the hollow workpiece and the size was kept 4, 5, 6 mm in 3 runs respectively. The electrolytic voltage was changed in the form of 6, 12, 18 V in each run respectively while magnetic voltage was kept at 50, 125, 200 V and media selected at each run was natural rubber (NR), styrene butadiene rubber (SBR) and nitrile rubber (NTR). The upper and lower piston cylinder arrangement were utilized to provide required extrusion pressure and their repetition cycles were 3, 6 and 9. Taguchi L18 OA is shown in table 4.9 and the output responses are listed in table 4.10.

Table 4.9 Taguchi L 18 OA

| Experiment number | ECM rod shape | Size of ECM rod (mm) | ECM voltage (volts) | Magnetic field (in terms of volts) | Type of polymer media | No. of cycles |
| --- | --- | --- | --- | --- | --- | --- |
| 1. | Drill bit | 4 | 6 | 50 | Natural | 3 |
| 2. | Drill bit | 4 | 12 | 125 | SBR | 6 |
| 3. | Drill bit | 4 | 18 | 200 | Nitrile | 9 |
| 4. | Drill bit | 5 | 6 | 50 | SBR | 9 |
| 5. | Drill bit | 5 | 12 | 125 | Nitrile | 3 |
| 6. | Drill bit | 5 | 18 | 200 | Natural | 6 |
| 7. | Drill bit | 6 | 6 | 125 | Natural | 9 |
| 8. | Drill bit | 6 | 12 | 200 | SBR | 3 |
| 9. | Drill bit | 6 | 18 | 50 | Nitrile | 6 |
| 10. | Square | 4 | 6 | 200 | Nitrile | 3 |
| 11. | Square | 4 | 12 | 50 | Natural | 6 |
| 12. | Square | 4 | 18 | 125 | SBR | 9 |
| 13. | Square | 5 | 6 | 125 | Nitrile | 6 |
| 14. | Square | 5 | 12 | 200 | Natural | 9 |
| 15. | Square | 5 | 18 | 50 | SBR | 3 |
| 16. | Square | 6 | 6 | 200 | SBR | 6 |
| 17. | Square | 6 | 12 | 50 | Nitrile | 9 |
| 18. | Square | 6 | 18 | 125 | Natural | 3 |

Table 4.10 Response characteristics i.e. material removal and % change in surface roughness

| Experiment number | Run order | Initial weight (gm) | Final weight (gm) | Material removal (gm) | Initial surface roughness(µm) | Final surface roughness (µm) | % change in surface roughness |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | 1. | 3.9490 | 3.7491 | 0.1999 | 1.87 | 1.16 | 37.96 |
| 2. | 2. | 3.9390 | 3.7436 | 0.1954 | 1.78 | 1.12 | 37.07 |
| 3. | 3. | 3.8995 | 3.7226 | 0.1769 | 1.88 | 0.90 | 52.12 |
| 4. | 4. | 3.8456 | 3.7314 | 0.1142 | 1.80 | 1.74 | 3.33 |
| 5. | 5. | 3.9995 | 3.7288 | 0.2707 | 1.78 | 1.64 | 7.86 |
| 6. | 6. | 3.8001 | 3.7424 | 0.0577 | 1.84 | 1.18 | 35.86 |
| 7. | 7. | 3.8746 | 3.6921 | 0.1825 | 1.77 | 1.18 | 33.33 |
| 8. | 8. | 3.7684 | 3.7323 | 0.0361 | 1.65 | 1.22 | 26.06 |
| 9. | 9. | 3.8845 | 3.7350 | 0.1495 | 1.45 | 1.10 | 24.14 |
| 10. | 10. | 3.8720 | 3.7184 | 0.1536 | 1.80 | 1.52 | 15.55 |
| 11. | 11. | 3.8841 | 3.7333 | 0.1508 | 1.80 | 1.72 | 4.44 |
| 12. | 12. | 3.8234 | 3.7204 | 0.1030 | 1.99 | 1.94 | 2.51 |
| 13. | 13. | 3.9290 | 3.7154 | 0.2136 | 1.77 | 1.56 | 11.86 |
| 14. | 14. | 3.9990 | 3.7216 | 0.2774 | 1.99 | 1.92 | 3.51 |
| 15. | 15. | 3.9347 | 3.7280 | 0.2067 | 1.82 | 1.48 | 18.68 |
| 16. | 16. | 3.8765 | 3.7453 | 0.1303 | 1.75 | 1.38 | 21.14 |
| 17. | 17. | 3.9008 | 3.7330 | 0.1678 | 1.56 | 1.52 | 2.56 |
| 18. | 18. | 3.8848 | 3.7350 | 0.1498 | 1.81 | 1.12 | 61.6 |

The brass rod is taken firstly and then this rod is taken to Anand Parbat market, Delhi where industrial area lies and big machinery is installed. The rod is somehow clamped between supports on lathe machine and through boring is done and simultaneously cut into piece of size 16 mm. Since the internal surface of the prepared piece is not so smooth and requires post finishing process, hence the non-traditional machining process i.e. abrasive flow finishing (AFF) process is done on the prepared machine setup in Precision engineering laboratory, that will produce highly finished surface as compared to traditional machining process applied earlier that included drilling, boring and reaming. The large number of workpieces of brass material were obtained, out of this lot, selection of nearly equal surface roughness value pieces are selected for AFM experimentation. In the present experimental work, 18 workpieces are selected on which hybrid AFM has to be performed, their initial surface roughness value tested on roughness tester machine was found to be in the range 1.65 µm to 1.99 µm, the initial weight measured were in the range 3.7684 gm to 3.949 gm. After performing machining, the roughness values obtained were in the range 0.90 µm to 1.92 µm, while the final reduce weight obtained was in the range 3.6921 gm to 3.7491 gm. As shown in table 4.10.

Summary

- Design and analysis of experimental work based on Taguchi and ANOVA analysis is done and magnetic field assisted electrochemo abrasive flow machining setup was fabricated.

- Further the experiments were performed to validate electrochemical and rotational motion effect on the workpiece during AFM process.

- The parameters selection was done in such a way that individual effect of machine, magnetic field, electrolytic and rotational based parameters can be analysed on MR and Ra results.

CHAPTER 5: MODELLING OF EMR-AFM PROCESS

This chapter deals with the modelling of the developed hybrid AFM setup in which all the external forces attachments are first mathematically modelled to recognise the effect of the process. Then based on the developed model the fabrication of fixture is accomplished and experimentation was performed. Further computational flow dynamics of media flow through fixture path was studied using Solidworks software. Different mathematical models were built to study media flow behaviour, strength of magnetic field used and electrochemical effect and the overall combined hybrid setup was modelled.

5.1 Mathematical and Computational Modelling of EMR-AFM Process

The modelling of the hybrid EMR-AFM process is done which includes voltage, cutting forces and magnetic flux calculations in elecrochemo magnetic AFM process, analysis of flow of media, i.e., shear rate, velocity, pressure calculations, etc., the role of computer neural network and algorithms in AFM process is analysed. Further, the computational flow analysis of the flow of media through the newly designed and fabricated EMR-AFM machine fixture is done using Ansys software.

5.1.1 Role of Computer Optimization Software and Algorithm in AFM Process Modelling

The demands of cost feasible products led to the development of advanced non conventional finishing processes like abrasive flow finishing process. In AFM process, abrasive media is extruded across the surface to be finished in single direction or two-way or orbital. Chryssolouris and Guillot (1990) modelled a machining process using neural network and multi-regression method. The neural network approach has been extensively used in abrasive flow machining. Jain et al (2000) developed the equations for material removal rate (MRR) and surface roughness (Ra) by multi variable regression and corresponding coefficients were evaluated using least squares method. For modeling the process in such a way that it perform like human being, we have to apply neural network method. It has three features, i.e. topology, functionality and learning. The back propagation neural network is shown in figure 5.1(b). Petri et al (1998) used the neural network model to predict the surface finish in abrasive flow machining. The developed to set machine parameters of AFM, by pairing with meta-heuristics, which assisted neural network model in extrapolating. The response of node of hidden layer,

hj = f ∑wjixi 										           (1)

for output layer,

ri = f ∑vijhj 										       (2)

where w is weight of connection to hidden layer as shown in eq. (1) and (2). The function f is transfer function given by eq. (3).

f(t) = (1+e-t)-1 										       (3)

Shinmura and Aizawa (1986) developed a simulation to study on magnetic assisted abrasive finishing process. A set up was fabricated in which the input current to the solenoids was changed and accordingly the magnetic pressure was controlled. After analysis of the results of magnetic finishing the simulation results showed that the magnetic flux between north and south poles is maximum when the air gap between the poles is minimum. It was also concluded that the magnetic pressure between the poles attained maximum value at 1.2 Tesla flux density. The experimental and simulation results matched exactly at lower values of flux density. Figure 5.1(a) clearly explains the flow chart and step by step simulation of magnetic assisted finishing process. Jain and Jain [40] simulated the surface profile in abrasive flow machining by assuming the random distribution of abrasive grains in media.

(a)                                                                       (b)

X1

X2

X3

H1

H2

I1

W21

W13

W11

W12

W23

W22

Start

Input(data,process)

Calculate magnetic field strength

and permeability

Calculate machining pressure

Ra≤Rcrt

Ra≤Ravg

End

Change input solenoidal current

YES

NO

Figure 5.1(a) Flow-chart representing magnetic forces effect, (b) Neural network approach in AFM

Uhlmann et al (2015) applied Maxwell model to polymer media by CFD simulation of abrasive flow machining process.

Relaxation time, t = z/c  							                   (4)

C/ (w) = C0 + ∑ Ck. (wtk)2/[1+ (wtk)2]  						        (5)

The relaxation time calculation is given in eq. (4), while spring stiffness calculation for next series is done in eq. (5). Jain and Jain (2000) used back-propagation neural network model to optimize abrasive flow machining process.

The genetic algorithm (GA) approach used for process optimization started with formulation of constrained optimization problem. Initialization of GA parameters, i.e. population size, string length, crossover, mutation probability and maximum number of genes is done. Put generation number = 0. Now, initial feasible random population is obtained. If the generation number > maximum number of genes, then the program is terminated, else again we have to evaluate fitness of each individual and the program is run in the similar manner. Silva and Geough (2000) have done a lot of work on computer applications in unconventional machining.

5.1.2 Voltage and Magnetic Flux Calculations

A model was developed in which electrode gap was simulated and modelled and final micro tool diameter was predicted within the accuracy of 94% or 6% variation range to develop tungsten tools by Mathew et al (2000). In magnetic field assisted AFM process, the active abrasive particles actual participating in cutting action were calculated using developed model by Das et al (2008).  If the number of cycles and current was increased then surface roughness value was found to be decreased. The magnetic force used in the experimental work played a vital role in enhancing material removal. The calculation of magnetic force and the removal of material is the prime focus which resulted in the need of a mathematical model. Hence model was generated by assuming a magnetic particle of radius r and mass m and is of spherical shape. We apply continuity eq. (6), based on mass conservation principle.

43πr3 = 1/ρ       									       (6)

differentiating we get  ∂∂m43πr3δr = - δρρ2

where ρ is the density of magnetic particles. The abrasive particle equation of motion is given by eq. (7). In eq.(8), the pressure calculation is shown.

∂2r∂t2 = - 2πr∂P∂m - 2Gmr 								                   (7)

The total pressure P = p+ H28π   								       (8)

Differentiating the above equation, we get the solution from eq. (9),

δP = δp + HδH4π

∂2r∂t2 = - 2πr∂∂m δP + 4Gmr2δr  								       (9)

The magnetic field B is calculated as in eq.(10).

B = µo2.NIx2x2+z23/2  									     (10)

= 10 Gauss.

Piston downward extrusion pressure force

Electromagnet-2

Magnetic current direction

Polymer media (abrasive +iron particles)

Magnetic field lines				field orientation

Electromagnet-1

Electromagnet-3

Eddy currents

Electrolytic current flow direction

Input and output terminals

Workpiece(+)

Electrode (-)

Magnetic and electric

field lines are mutually

perpendicular to each other

Piston upward extrusion pressure force

Figure 5.2 Forces acting on abrasive particle inside the workpiece

The magnetic flux is calculated as given in eq.(11).

φ = ABcosα                                                                              			     (11)

= π × 4.52 × 10 × cos60o = 308 G/A

According to Faraday’s law of induction as shown in eq. (12),

V = -Ndφdt 							         			     (12)

= -3200 × 4.52 × cos60o × 10/120 = 2784 V

B = 0.5 BPcosωt        									     (13)

ω = 100.5×40000 = 0.75 rad/s

where ω is angular frequency of alternating current., which is calculated from eq.(13).

Hence V = 0.5 ωNABPcosα.sinωt  								     (14)

V = Mdidt 										     (15)

The eq.(14) and (15) are used for calculating voltage using current gradient.

The erosion is given by eq. (16), which denotes the rate of removal of metal from the work surface.

R = dmdAm  											     (16)

M = kρwVAN 											     (17)

In eq.(17), mutual induction expression is shown.

Figure 5.2 shows a schematic drawing in which an active particle is subjected to a number of external forces. The direction of current is shown by fingers curling orientation of the right hand. It is seen that the different kinds of forces viz. magnetic, electrolytic and centrifugal force act on the abrasive particle. The piston cylinder arrangement above and below the fixture containing workpiece provide the required driving force to the media. This gives extrusion pressure to the abrasive laden polymer media which results in material removal from the surface of the job. The different forces incorporated in the system are as shown in figure 5.3(a), i.e., driving force transferred by the pressure of the media and normal force mainly produced by cylinder total pressure.

5.1.3 Effect of Time Derivatives on Magnetic Field

The approximation of different derivates in case of different field values with finite differences in Maxwell’s equations is explained in detail. We calculate these terms before iteration to speed the process of simulation. The algorithm for calculation of H and e field values is generated which is shown as in figure 5.3(b). The algorithm in which H and corresponding e values are calculated using iteration principle is generated. Initially H|t- ∆t/2 = 0 and e|t = 0. In the first iteration, e|t→ H|t- ∆t/2. This suggests that the e field value at time t changes to H field value at half time step more than initial time value. Similarly the corresponding e and H values after every half time step value are explained.

(a)                                                                                               (b)

Brass workpiece

M.S. tool

Diverging negative field lines

Converging field lines

Cylinder extrusion pressure force

Abrasive grain (R)

Workpiece wall surface

FN

FR

Material pile up

Resistance force

Driving force

Initialize Fields to Zero e = H = 0

Finish

Done?

Update H from e

H|t+ ∆t/2 = H|t- ∆t/2 - ∆te∇×e|t

Update e from H

e|t+ ∆t/2 = e|t + ∆te∇×H|t+ ∆t/2

Yes

No

Figure 5.3(a) Different forces acting on the workpiece, (b) Time derivatives effect in magnetic field flow chart

In the following iterations, H|t + ∆t/2→e|t H|t + 3∆t/2 → e|t+2∆t and so on. The modeling included different laws i.e. Maxwell, Gauss, Faraday and Ampere law, etc. the above equations were utilized during modeling. The electric field generated during the operation of magnetic field in hybrid AFM setup diverges from positive charges whereas convergence occurs in case of negative charges. Figure 5.3(a) shows the workpiece and tool electric field charge directions that are either converging or diverging in nature. If we stop the supply of current, there are no charges and hence loops are formed. The magnetic field produced during the working of prepared electromagnetic setup in hybrid AFM process always form closed loops. The magnetic field strength was calculated and was upto 1 Tesla. This magnetic field causes the magnetic abrasive particles mixed in polymer media to attract towards the magnetized poles and hence hit the inner walls of brass workpiece, consequently improving the machining efficiency. The varying magnetic field with time is due to circulating electric field whereas the time varying magnetic fields induce circulating electric fields. The time derivative effect has been shown in figure 5.3(b) in the form of a flowchart.

5.1.4 Analysis of Flow of Media

When the abrasive laden polymer media is reciprocated between upper and lower cylinders, and hit the work surface, it exerts force and this force can be divided into different components like axial i.e. along the centerline axis, along the radius of circular job and also perpendicular to the radius i.e. tangential components. Let k =1, y = distance moved by media per stroke of machining = 650 mm, time/ stroke = 6 sec.

hence, µo = 1× 65060.8-1 = 0.3917.

Let Fa, Fr and Ft are the axial, radial and tangential forces exerted by the polymer media on the abrasive particle, shown in eq.(18). Extrusion pressure at which AFM machine is set = 30 bar = 30 × 105 Pa

Fa = p.A = 30 × 105 × 100.53/106 = 301.6 N

Fr = pm.A = 2 × 105 × 100.53/106 = 20.106 N

Ft = Fa.cos45o = 213.3 N							                 (18)

where pm is magnetic pressure = 2 Tesla = 2 × 105 Gauss. It can be seen that axial force is about 15 times the radial force, and 1.5 times the tangential force.

The cutting force, Fc  is given in eq. (19) and shear force is given by eq (20)

Fc = Fa2+Fr2+Ft2,					                                         (19)

= 301.62+20.12+213.32 = 369.42 N

Fs = τs.A  										     (20)

where Fs is the strength of workpiece and A is the projected area. For brass material, τs = 234 MPa

Fs = 234 × 100.5/106 = 0.0235 N

For positive condition of AFM action to occur, shear force must be lesser in magnitude as compared to cutting force. Since Fc ≥ Fs, hence cutting occurs. The flow of semi-paste polymer media inside the workpiece is assumed as turbulent flow. The shear stress is given by eq. (21) and (22).

τ = n dudy + µdudy  			                                                                             (21) τ = 0.9 108.33650 + 48108.33650 = 8.05 MPa.

u1 = v1 = 43.2 mm/s

τ = 1.1 × 10-3 × 43.22 = 2052.86 MPa

τ = ρl2dudy2										     (22)

= 1.1 × 10-3 × 2602 × 0.1662 = 2.05 MPa

τρ = l dudy     (23)

dudy = 2.051.1/1000/0.26 = 183.35 s-1

Shear velocity, V* = 0.4 y dudy    						                  (23) = 19.06 mm/s

2.5 V* dyy = du

2.5 V* lny = u + c

Boundary conditions: at y = R, u = umax

umax-uV* = 5.75 log10Ry   					  				     (24) At y = R, umax = u = 43.2 mm/s

The above eq. (24) is based on Prandtl velocity defect equation.

5.1.5 Computational Flow Analysis of Polymer Media in Hybrid Magnetic Assisted Abrasive Flow Machine Fixture

First of all, the nylon fixture for hybrid AFM process setup alongwith electromagnets was designed as shown in figure 5.4(a), then modeling simulation and analysis of the flow of media was done. It included velocity, pressure, shear rate calculation, etc. There is constant density of media during operation. The density of abrasive laden polymer media is 740 kg/m3. There is no effect on the density, it remains constant throughout the working operation. The shear rate variation with the flow passage is shown clearly in the figure 5.4(b), alongwith scale on the left side ranging from 2638 to 12006.74/s. As shown in the fixture, the shear rate value at entrance and exit lies between 1336.42/s to 2670.22/s, while all along the flow path the value was changing from 2638/s to 1336.42/s and the minimum shear rate value ranges from 2670.22/s to 4004.006/s which occurs at the junction of tapered portion of fixture and at the centre of workpiece location inside the fixture. This is due to the reason that the abrupt change in velocity occurs at this stage. The pressure value ranges from -297880 Pa to 1.22 e +07 Pa as shown in the scale in figure 5.4(d).

(a)                                                                     (b)

(c)

(d)

Figure 5.4(a) Design of AFM fixture, (b) shear rate, (c) velocity of media flow and (d) pressure variation

The maximum pressure value is at the centre and gradually decreases upto the exit cross section of the fixture and similarly this pressure change is seen from opposite side of the fixture, now the exit becomes the entrance of the fixture. The pressure value at the centre is 5277112 Pa.

(a)                       (b)                                                                     (c)

.

Figure 5.5 (a) Top view of AFM, (b) Meshing of AFM, (c) Effect on temperature

Table 5.1 Shear rate, pressure, velocity values at different locations during media flow

| S. No. | X (m) | Y (m) | Z (m) | Velocity VZ (m/s) | Shear rate (1/s) | Pressure (Pa) | Shear stress (Pa) | Temp. of fluid (K) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1. | 0.00069 | 0.0657 | 0.0046 | 1.93 | 2037 | 11.76 | 0.04 | 293.19 |
| 2. | 0.00069 | 0.0636 | 0.0046 | 2.00 | 1168 | 11.73 | 0.06 | 293.29 |
| 3. | 0.00070 | 0.0657 | 0.0046 | 1.87 | 1957 | 11.71 | 0.04 | 293.19 |
| 4. | 0.00070 | 0.0636 | 0.0046 | 1.90 | 1057 | 11.70 | 0.06 | 293.28 |
| 5. | 0.00067 | 0.0615 | 0.0046 | 2.00 | 1578 | 11.41 | 0.07 | 293.40 |
| 6. | 0.00067 | 0.0594 | 0.0046 | 1.99 | 2035 | 11.10 | 0.09 | 293.54 |
| 7. | 0.00070 | 0.0615 | 0.0046 | 1.88 | 1478 | 11.39 | 0.07 | 293.40 |
| 8. | 0.00070 | 0.0594 | 0.0046 | 1.86 | 1958 | 11.08 | 0.09 | 293.54 |
| 9. | 0.00942 | 0.0501 | 0.0094 | 0.00 | 11.63 | 67.53 | 0.07 | 294.06 |
| 10. | 0.00702 | 0.0501 | 0.0114 | 0.00 | 6.155 | 67.48 | 0.03 | 293.76 |

Hydraulic oil supply to upper ram

Machine column structure

Supporting frame for media cylinders

Steel rod to support motor

Electromagnetic solenoid

Electrolytic variable supply

Cooling water tank

Water out

Water in

(3)

(1)

0-200 V

Variable

Supply

(5)

(4)

(2)

Electrolyte tank

(6)

(Magnetic field supply set-up)

(13)

(12)

(11)

(14)			       (15)

Hydraulic Power Pack

(Electrochemical set up)

Downward and upward

movement of machine ram

Machine base/ foundation

Upper ram

(9)

(7)	       (8)

(10)

Lower ram

Figure 5.6 AFM Machine set-up block diagram: 1.Transformer, 2.Electromagnet, 3.Transformer oil tank, 4.Flow-sensor, 5.Pressure gauge, 6.Motorpump, 7.3-Phase motor, 8.Speed controller, 9.Fixture, 10.Lower media cylinder ram, 11.Lower machine cylinder pressure gauge, 12.Upper machine cylinder pressure gauge, 13.Current reader, 14.Lower machine cylinder pressure controller, 15.Upper machine cylinder pressure controller

The temperature variation is negligible during the media flow through the workpiece along the fixture path. It varies in the range 293.2 to 301.43 K. According to global coordinate system, the velocity of media variation is clearly depicted in the figure 5.4(c), ranging from -3.55 m/s to + 3.543 m/s, maximum being at the cross-section changes in the fixture and second most near the workpiece location. According to continuity equation of flow, as the cross section area increases, velocity of flow decreases and vice-versa, the minimum velocity being at the inlet and exit of the fixture. Further, the top view of the machine fixture showing the inlet and outlet of the media flow, meshing and effect on temperature is shown in figure 5.5(c). It can be clearly inferred that temperature is nearly constant when polymer media laden with abrasive particles pass through machine fixture. The value of temperature is given in table 5.1. Before analyzing the effect of different parameters, i.e., temperature, pressure, shear rate, velocity, etc., the meshing of the flow of media between upper and lower extrusion cylinders is essential, as shown in figure 5.5(b).

A small element is taken on the flow field and values of various factors such as location, velocity, temperature, pressure, shear stress and shear rate are given in the table 5.1. It can easily be seen that temperature of media during its flow in the experimentation remains nearly constant, i.e., 293 K to 294 K. The velocity of flow of media varies from 0 to 2.008 m/s, this value obtained is nearly equal to that obtained from mathematical calculations. The shear rate changes from 6.155 s-1 to 2037 s-1, the drastic change may be due to the fact that firstly when media enters the fixture, the shear rate is low but when it comes in contact with workpiece surface, the shear rate value drastically increases due to the force exerted by solid surface onto the semi-solid of liquid layer of media. The pressure ranges from 11 to 67.5 Pa, which depends on machine parameter, i.e., extrusion pressure. AFM machine setup block diagram is as explained in figure 5.6.

5.2 Heat Transfer, Flow and Velocity Analysis

5.2.1 Heat Transfer During Media Flow Through Fixture

Assumptions:

- The energy flow is assumed to be one dimensional

- There is no heat generation due to any other source

- Unsteady state of conduction

The amount of heat conducted through the work surface is given by eq.(25)

qcond = -KA(dtdx) watt 										     (25)

where q is conduction rate in watt, K is thermal conductivity in W/m2K and (dtdx) is temperature gradient i.e. rate of change of temperature with thickness dx of workpiece. The media motion is shown in figure 5.7 (b).

- (b)

AS

θ

Media motion (bulk motion)

fixture

workpiece

Vouter

Vinner

Workpiece rotation

dx

Figure 5.7(a) top view of workpiece rotation, (b) media bulk motion inside fixture

Due to extra rotational force provided to the workpiece with the help of motor, there is outer and inner surface velocity differential. Since the angular velocity is constant but radius of internal and external surface varies, hence peripheral velocities are different.

Vinner > Vouter (since RO > RI, and V = ωR)

where ω is angular velocity of motor, RO, RI are outer and inner radii of workpiece.

Now, we know the heat gets conducted through both workpiece surface and the adjacent polymer media. The heat conduction is in axial direction due to the two and fro motion of media due to extrusion pressure applied in upper and lower strokes. It is azimuthal in direction because of motor rotation, it glides along the peripheral surface of inner wall.

When the media flows in upward and downward stroke as a bulk movement, then due to macro motion, extrusion pressure energy of piston cylinder is transferred into thermal energy of media, which is given as in eq.(26).

qconv/trans = hAS(TS-Tf,m) 									     (26)

where AS is surface area of workpiece, TS is surface temperature of workpiece, Tf,m is fluid or media temperature. The different directions of heat transfer is shown in figure 5.8.

rd∅

Z

dz

qr

qr+dr

r

dr

qpiston extrusion pressure force

qrotation and magnetism

∅

d∅

Figure 5.8 Heat transfer directions in cut section of workpiece

Applying energy conservation principle we get

Ein – Eout + Egen = Est 						     (27)

where Ein is energy input, Eout is output energy, Egen is energy generated and Est is static energy.

Using Taylor’s expansion series

(Ein – Eout)r = qr – qr+dr = qr – (qr + ∂∂r qrdr + .....)

= - ∂∂r qrdr = - ∂∂r(-K.r.d.∅dz. ∂T∂r)dr

= 1r∂∂r(Kr∂T∂r).V 									     (28)

where qr is radial heat entering workpiece material, qr+dr is outgoing radial heat transfer, 
∅ is azimuthal angle, Z is height or length of workpiece.

Hence

1r∂∂r(K∂T∂r) + qg = ρCp. ∂T∂t                                                                                                               (29)

where α is ratio of heat conducted in workpiece material to heat stored in polymer media.

T∞

T1

ln(R2/R1)/2πKL

1/hoAo

T2

Figure 5.9 Heat transfer circuit diagram

From equation (31) and (32), we get

(T1 – T2)ln(R2/R1)/2πKL = T1 - T∞1/hoAo 						     (33)

qmax

qw/o media

RO

Rpolymer media

Rtotal

q

rmax

rc

Rconv

Rth

0

Assume media

No media

ro

Tf

Tcentre

T2

T1

Figure 5.10 Heat transfer vs media volume plot

The above equation represents heat diffusion equation in cylindrical coordinates in radial direction. The figure 5.10 shows effect of radius on heat transfer and thermal resistance. The media gets heated because of fast motion due to extrusion pressure applied by two sets of piston-cylinder arrangements. The assumptions taken during the modelling includes 1-D radial heat flux, non heat generation, constant thermal conductivity of the material and steady state conditions.

Now the temperature at any location in the workpiece is given by eq.(34).

T = (qq.R2/4K).[1 – r2/R2] + Ts 								     (34)

where qg is heat generated, R is radius of workpiece, r is radial distance at which temperature is to be calculated and Ts is static temperature. The heat transfer is given by the eq.(35)

q = (T1 – T2)ln(R2/R1)/2πKL                                                                                                                                         (35)

where T1, T2 are workpiece inner and outer wall temperature respectively.

qconv = T1 - T∞1/hoAo 											     (36)

where T∞ is media temperature, ho is convective heat transfer coefficient of media, Ao is inner surface area of workpiece. The circuit diagram is as shown in figure 5.9.

The polymer media is assumed to fully cover or envelop the inner surface area of workpiece. Hence it is analogous to insulating the cylindrical workpiece internally, thereby acting as a temperature insulator. In the figure, the variation of thermal resistance with increase in volume of polymer media.

rc = Kiho,

where KI is the conductivity of polymer media material (KI or Km). The temperature varies across the thickness of workpiece. The temperature of fluid or media is Tf, the centreline temperature is maximum which gradually decreases outwards hyperbolically as shown in figure. The thermal resistances of polymer media, convection and total resistance curves are depicted in figure. It is shown that thermal resistance of media increases as we move outwards across workpiece, while convective resistance i.e. heat transfer coefficient from media to work surface decreases at a constant rate. The total resistance is minimum at critical radius value while heat transfer rate is maximum at this instant.

As the number of extrusion cycles on AFM increases, the workpiece and media temperature changes and hence we can assume lumped heat transfer. Let at the end of first cycle,

T = Ti

where T is work temperature, Ti is initial temperature.

Let TI = TM,

where TM is polymer media temperature.

Applying energy balance in ‘n’ number of extrusion cycles, we get

Decrease in internal energy of workpiece in ‘n’ number of cycles = amount of heta rejected to media by convection

i.e. –m.c.dT = h.As.(T-TM).n 									     (37)

where m, c, h are mass, specific heat capacity, convective transfer rate of media material, As is work surface area.

Hence, T-TMTi-TM = e-n/t, 									     (38)

where t is time constant.

t  = ρVchAs

5.2.2 Radial Heat Transfer Through the Brass Workpiece

Assume one- dimensional, radial heat transfer s shown in eq (39) and (40)

q = TG-T1Rth  											     (39)

q = UiAi∆T = UoAo∆T   									     (40)

where Ai = 2πriL, Ao = 2πroL

the extrusion pressure inside the workpiece is assumed as the forced convection heat transfer in semi-liquid paste having convective heat transfer coefficient hi = 1200 W/m2K and the outside free convective heat transfer coefficient ho in gas = 375 W/m2K. the thermal conductivity of brass, k = 109 W/mK at 25oC.

Rth = 1hi2πriL + lnr2/r12πKL + 1ho2πroL =  11200 × 2π × 0.004 × 0.016 + ln5/42π × 109 × 0.016 + 1375 × 2π ×0.005 × 0.016 = 7.47 K/W

During machining, the temperature of media reaches, TG = 145oC = 418 K.

Ambient air temperature, T1 = 32oC = 305 K.

Hence, q = 418-3057.47 =15.13 W.

The overall heat transfer coefficient, Ui = 15.132π ×0.004 ×0.016 × (415-305) = 342.05  W/m2K

UO = 15.132π ×0.005 ×0.016 × (415-305) = 273.63 W/m2K.

5.2.3 Governing Equations of the Flow Pattern

The media used in AFM is composed of semisolid carrier mixed with abrasives which exhibits linear viscous flow property. The media is isotropic and homogeneous. Since cylindrical workpiece is considered, media flow is taken as axi-symmetric. The media flow is steady.

5.2.3.1 Continuity Equation

The condition of volume conservation can be expressed as,

∈θθ + ∈rr + ∈zz = 0		     (41)

where, ∈θθ, ∈rr and ∈zzare components of strain rate tensor in azimuthal, radial and axial directions respectively.

5.2.3.2 Momentum Equation

ρvr∂vr∂r+vz∂vr∂z+∂p∂r-1r∂(rτrr)∂r-τθθr+∂τrz∂z = 0		     (42)

where, ρ is density of media, p is pressure (hydrostatic stress).

5.2.3.3 Constitutive Equation

The media behaves as a Newtonian fluid with shear stress being the linear function of shear

rate.The total stress tensor:-

σij= -pδij+τij

= -pδij + μa∈ij		     (43)

where μa is apparent viscosity and δij is identity tensor.

5.2.4 Flow Regime of Polymer Media Across the Inner Work Surface

Trailing edge

Turbulent

transition

laminar

Leading edge

Up and down stroke

U(r)

T∞

Fully developed flow

V is non zero

Abrasive particle

V = 0 (no slip condition)

x

Figure 5.11 Different types of flow regime inside work surface

In figure 5.11 flow regime of polymer media is shown. At ‘x’ distance,

Local Reynold number of the flowing media is given by

Rex = u∞.xv 									     (44)

where u∞, x, v are the free media velocity, distance of workpiece cross section from trailing edge, kinematic viscosity of media respectively.

Local heat flux, q = h(Ts - T∞)

= -Kf.(dTdy)y=0 								     (45)

where Kf is media conductivity, (dTdy)y=0 is wall temperature gradient.

The elemental media mass flowing through any work cross section is given by eq.(46)

dm = ρ.dAc.u(r)									     (46)

total mass is

M = 2π ρ0Rr.urdr 									     (47)

But me know that

M = ρ πR2.u(m) 									     (48)

Hence from above equations we get

U(m) = 2R20Rr.urdr 									     (49)

where u(m) is the mean flow velocity of media.

5.2.5 Velocity Boundary Layer in Internal Flow of Media inside Workpiece

Outside velocity boundary layer i.e. irrotational flow

Hydrodynamically developed flow i.e. u = f(r) only

Figure 5.12 Graphs showing fully developed media flow

Mean temperature or bulk mean temperature of media is the temperature when the flow is fully developed.

Energy of media is given by

E = 2ρ πcp0Rr.urTmrdr 									     (50)

Also, E = ρ πR2.u(m)cpTbm									        (51)

From above two equations we get

Bulk mean temperature,

Tbm = 2u(m)R20Rr.urTmrdr 								     (52)

5.3 Principle Operation and Characteristics of the Electrochemo-Magneto AFM Setup

During the working operation, the magnetic lines of forces act towards the workpiece whose internal wall surface has to be machined. In order to provide more focusing magnetic force towards the centre, the workpiece is placed inside the hollow cylindrical piece made of paramagnetic material, usually known as bright bar. The main aim of our model is to achieve high material removal and better morphological characteristics, which requires the development of electro-magnetic model. As the current supply to the developed solenoid arrangement is varied, the magnetic force gets changed. The following mathematical equations will predict the performance of abrasive flow finishing process.

5.3.1 Assumptions

Taking all the parameters in electrochemical and magnetic force assisted AFM into account, the following assumptions are taken while writing mathematical equations:

- The workpiece material is homogeneous and isotropic.

- The magnetic field domain inside the workpiece is symmetrical about the axis.

- Both cathode (cylindrical rod) and anode (workpiece) are conducting in nature.

- The supply of current in the solenoid coils is assumed to be constant.

- The magnetic abrasive particles are considered spherical- shaped.

5.3.2 Magnetic Flux Intensity and Electrolytic Force Modeling

The Maxwell equation (53) is used to determine electromagnetic forces and the direction of the magnetic lines. The equation can be denoted mathematically as:

∇.B = 0 											     (53)

where B is the magnetic flux density.

1r ddrrdφdr + d2φdz2 = 0                                                                                                                   (54)

where φ is the azimuthal angle, z is the height of the workpiece where the effect of magnetic field is produced.

According to British standard wire gauge: 19 gauge = 0.040 inch = 1.016 mm diameter

Resistance of 19 gauge wire = 0.0264 ohm/m, at 20 ‘C.

Copper density = 8.96 g/cm3 or 0.324 lb/in3

Maxwell’s Equation:

(a) Gauss’ Law

∇.S = θ

∇.S = ∂Sx∂x +∂Sy∂y +∂Sz∂z 										     (55)

The electric field generated during the operation of magnetic field in hybrid AFM setup diverges from positive charges whereas convergence occurs in case of negative charges.

∇.B = 0

∇.B = ∂Bx∂x +∂By∂y +∂Bz∂z                                                                                                                                   (56)

The magnetic field produced during the working of prepared electromagnetic setup in hybrid AFM process always form closed loops. The magnetic field strength was calculated and was upto 1 Tesla. This magnetic field causes the magnetic abrasive particles mixed in polymer media to attract towards the magnetized poles and hence hit the inner walls of brass workpiece, consequently improving the machining efficiency.

(b) Faraday’s Law

∇×e = -∂B∂t

∇×e = ∂ex∂y- ∂ey∂zbx + ∂ey∂z- ∂ez∂xby+ ∂ey∂x- ∂ez∂ybz                                                         (57)

The varying magnetic field with time is due to circulating electric field whereas the time varying magnetic fields induce circulating electric fields.

(c) According to Ampere’s law,

∇×H = i+ ∂S∂t 										     (58)

Where i is the current density. The above eq.1 shows that a circulating H field induces change in S field at the center of circulation. The circulating magnetic fields induce currents and time varying electric fields, whereas currents and time varying electric fields induce circulating magnetic fields.

A B field induces an H field which is directly proportional to the permeability, as shown in eq.1.

B(t) = [µ(t)]. H(t) 										     (59)

Where µ is the permeability index of the medium.

S(t) = [e1(t)]. e(t) 										     (60)

The above eq.1 denotes the induction of e field due to S field which is proportional to permittivity e1.

5.3.3 Effect of Magnetic Field

Let heat flux entering due to magnetic flux be qconv, magnetic.

Applying steady flow energy equation on control volume, we get

qconv, magnetic = m.cp(Tb,o- Tb,i) watt 								     (61)

ω1i

Iron particles

ω3i

n1

ω2i

n3

Magnetic lines of force

n2

Iron pole

Copper windings

1

2

3

Figure 5.13 Electromagnetic setup configuration

ω1i, ω2i, ω3i are the solid angles between iron particles and electromagnet pole 1, 2 and 3 respectively. The configuration of magnetic field is shown in figure 5.13.

n1, n2 and n3 are normal vectors on poles 1, 2 and 3.

α1, α2 and α3 are angles made by normal vectors with longitudinal axis of workpiece.

Magnetic flux Ie = qe, ij Aicosθiωji 									     (62)

5.3.4 Analysis of Electrochemistry During Abrasive Flow Machining Process

The electrochemical equivalent of alloy:

Anode is alloy brass (Cu + Zn)

Let Cu = 1 and Zn = 2

where 1,2 are the elements in the alloy.

5.3.4.1 Volume Removal Rate and Electrolytic Charge Calculations

Let m1 and m2 are atomic weights of the elements i.e. 29 and 30 respectively, V1 and V2 are the valencies i.e. 2 each, x1 and x2 are percentage fraction of the element in the alloy, i.e. 0.7 and 0.3 respectively and ρ1 and ρ2 are the densities i.e. 8.96 and 7.13 g/cm3 respectively.

The initial weight of brass workpiece = 3.753 g

Final weight = 3.5531 g

Change in weight = 0.1999 g

Let Va is the volume of material that goes into the electrolytic or media solution in given time t.

Volume removed, V = 0.1999/8.70 = 0.0229 cm3

The weight of copper = Va100ρ1 x1 								     (63)

= 0.0229100×8.9× 0.7 = 1.4266 × 10-3 g

Weight of zinc = Va100ρ2 x2 = 0.0229100×7.13× 0.3 = 4.89 × 10-3 g

The charge taken by copper Q1 = w1Fv1/29 = 1.4266 × 10-3× 96500×2/100 = 9.48 C

The charge taken by zinc Q2 = w2Fv2/30 = 31.46 C

The total charge required for removing all the elements from the alloy will be

Q = Q1 + Q2  											     (64)

= 40.9 C

The volumetric material removal rate VM per unit charge

VM = Va/Vtotal = 6.3 × 10-3/ 0.0229 = 0.275 mm3/C

If the current I flows for time t, the total charge and MRR are given by eq (65) and (66)

Qtoatal = I.t  											     (65)

MRR = Va/t  											     (66)

Diameter of ECM rod = 4 mm

Inner diameter of workpiece = 8 mm

Hence dh = 4 mm

The weight dissolved dW = 1.431 g

where dh is the gap between anode and cathode and t the time of machining per piece.

I = V/R 											     (67)

where R is the resistance of electrolyte.

5.3.4.2 Electrolytic Reactions Taking Place During Machining

The electrochemical reactions taking taking place during the operation are given in eq (68-70)

NaCl(s) = Na+(aq) + Cl-(aq) 									     (68)

Cathode: 2H2O + 2e- → 2OH- + H2↑ 								     (69)

Anode: 2NaCl → 2Na+ + Cl2↑ + 2e- 								     (70)

5.4 Analysis on Abrasive Particles

5.4.1 Force and Motion Analysis

Abrasive particle is assumed to be under the action of three external forces:

- Shear effects

- Rotational or centrifugal effects

- Torsional effects

Assumption: the analysis is done on 2-D surface of abrasive grain.

When abrasive particle is under motion due to force provided by the piston, it is under the ction of various shear stresses as shown in figure 5.14.

Abrasive grain

τxy

τyx

∅xy/2

Figure 5.14 (a) initial shape of abrasive grain, (b) final shape of abrasive grain

Total shear strain in X-Y plane = ∅xy = total angular deformation of abrasive particle.

Suppose abrasive particle is acted upon by three directional forces due to external pressure of piston, magnetic pull of solenoid and rotational motion provided by induction motor as shown in figure 5.15.

σz

σx

σy

z

x

y

x

dx

D

ω

Bunch of abrasive particles

Figure 5.15 Rotational motion of bulk of abrasive grains

Therefore volumetric stress on particle is given by

∈v = change in volume of abrasive particle due to forcesinitial volume = ∆VV 					     (71)

= (σx+σy+σzE).(1-2µ)

where σx, σy, σz are stresses due to magnetic pull, centrifugal force and extrusion force of piston respectively.

Let ω is rotational speed of workpiece (rad/s).

Let us take a bunch of abrasive particles at distance x from longitudinal axis of workpiece. Due to centrifugal action, there is tendency that this bunch gets pushed outwards.

Let outward movement = d∆ = Fx.dxAE = (ρAx).(L-x/2).ω2.dx/AE 				     (72)

There total movement = ∆ = ρ ω2.L3/3E

In addition to above, abrasive grain is under torsional effect. The rhombohedral shape of particle can be assumed as circular shape.

T = τdA.r

= 2πτr2dr 											     (73)

where T is torque applied to abrasive particle due to motor rpm.

Due to rotation effect, the centrifugal action occurs on polymer media which leads to the tightening of media volume against the wall surface of workpiece.

Total axial movement of polymer media = [elastic contraction of workpiece] + [elastic expansion of media after release of centrifugal force]

n.p = [σwEwLw] + [σmEmLm] 			     (74)

where w, m subscripts represents workpiece and media respectively, σ is axial normal stress, E is Young’s modulus and L is length of workpiece.

5.4.2 Hitting of Abrasive Grain Against Workpiece Surface

When abrasive grain hits the surface, it produces impact force since it hits with high velocity from a certain distance. Let δmax be maximum or dynamic deflection of the elastic workpiece material on impact of abrasive grain.

Loss of energy of abrasive particles = gain in strain energy of workpiece surface

mg(h+ δmax) = σmax22EAL 			     (75)

Hence, σmax = WA[1+1+2hWL/AE] 			     (76)

where W is weight of abrasive particle hitting the work surface, A, E are the area of cross section and Young’s modulus of work material.

The linear motion of abrasive particle hitting the work surface is assumed to be moving with feed velocity f and the workpiece is in constant rotational motion N rpm. The feed is f mm motion of abrasive grain/ revolution of workpiece and fN is feed velocity in mm/min. The abrasive particles result in abrasion of work surface and the material gets removed.

5.4.2.1 Material Removal Time (tmr) Calculation

Velocity of abrasive particle motion, V = πDN1000 m/min 			     (77)

Speed in revolutions per minute, N = V×1000/πD rpm

Hence cutting time, tmr = LefN 			     (78)

where Le is the effective work surface length machined.

Hence material removal rate, MRR = π/4(Do2-Di2)×LwLw/fN 			     (79)

= π4(Do2- Di2)fN

ω/N

abrasive

feed

AB

D

x

α

Figure 5.16 Penetration of abrasive aprticle into work surface in successive extrusion cycle provided by AFM machine

Depth of penetration (as shown in figure 5.16),

X = D2tanα/2 			     (80)

Where D is workpiece diameter in mm, α is angle subtended by abrasive particle during indentation. Since workpiece is in continuous rotational motion,

AB = [Dw – D2-Da2] 								     (81)

where Dw is workpiece diameter and Da is abrasive grain diameter.

Wear of inner work surface:

The wear is generally radial wear and the volume of material removed = l×b×d

= Vi-Vf

= π4(Di2- Df2)L            (82)

Where Di is initial diameter, Df is final diameter and L is work length.

5.4.3 Depth of Indentation and MR Calculation

When material removal occurs due to impingement of abrasive grain onto the surface or inner wall of workpiece, due to external force, there is indentation upto some particular depth and this depth is in microns. For different materials of job and different nature of abrasive grain used, this depth varies in magnitude. If harder and coarse grain is used then depth is more while fine and smoother grain results in better surface quality and lesser depth of indentation. The harder workpiece are affected to lesser extent.

Ap = πdgh 											     (83)

where Ap is the projected area, dg is the diameter of the embedded grain and h is the depth of penetration. dg is abrasive diameter corresponding to 300 mesh size = 0.051 mm (from Sigma Aldrica particle size conversion table)

brass density, ρ = 8.70 g/cm3

initial weight of brass workpiece, wi = 3.753 g

final weight, wf = 3.5533 g

decrease in weight after finishing process, ∆w = 0.1999 g

volume of hollow cylindrical brass workpiece, V = π4 (102 – 82).16 = 452.4 mm2

hence, volume of material removed, ∆V = 0.19998.70  = 0.0229 cm3

hence, h = 0.0229 × 1032π ×16 ×4 = 0.0569 mm

5.4.4  Stresses Acting on the Job

Sooraj and Radhakrishnan in 2004 gave the expression for calculation of radial stress by eq (84)

Pr = ϑea1-ϑea Pa, where Pr, Pa and ϑea are radial stress, axial stress and poisson ratio of elastic abrasive respectively. 										     (84)

Pa = 30 × 105 Pa

poisson ratio of elastic abrasive, ϑea = 0.21

Pr = 0.211-0.21 × 30 × 105 = 797.468 kPa.

According to Hertzian contact theory, the elastic deformation of elastic abrasive in axial direction is given by eq (85)

δ = 3Fea4Eeq.1Rea122/3   										     (85)

where Fa(ea) = PaπRea2   									     (86)

Rea = 0.025 mm

The equivalent Young’s modulus is given by eq (87)

1Eeq = 1-ϑea2Eea + 1-ϑw2Ew , where ϑw is the poisson ratio of workpiece material.                              (87)

1Eeq = 1-0.212280 + 1-0.332345 = 5.99/1000

δ = 3 ×301.6666.6.125122/3 = 0.419 mm

Let the brass workpiece taken be assumed as thick cylinder as it fulfills the condition Dt≤20

In the present case Dt = 10/2 = 5 i.e. ≤20.

During machining, the workpice is subjected to both external pressure i.e. magnetic flux and internal pressure i.e. extrusion pressure exerted by polymer media.

Pp is the extrusion pressure exerted by polymer media given by eq (88) and Pm is magnetic pressure given by eq (89)

At x = Ri=8 mm, px = pp = 30 × 105 Pa

x = Ro=10 mm, px = pm = 2 × 105 Pa

pp = -a + bRi2    											     (88)

pm = -a + bRo2   											     (89)

30 × 105 = -a + 15625 b

2 × 105 = -a + 10000 b

a = 4777777

b = 497.77

The hoop stress and radial stress are given by eq (90) and (91)

therefore (σh)x = a + bx2   									     (90)

(σr)x = a - bx2   											     (91)

At x = 8 mm, (σh)x = (σr)x = 47.77 MPa

5.4.5 Acceleration and Rotational Effects

Acceleration of abrasive particle through media: is given by eq (92)

a = axi + ayj +azk  										     (92)

ax = dxdt = ∂u∂xdxdt + ∂u∂ydydt + ∂u∂zdzdt+ ∂u∂t

= u∂u∂x + v∂u∂y + w∂u∂z + ∂u∂t = 43.2 × 43.2650.33 + 86 × 43.26 + 0 = 12.47 mm/s2

ay = dydt = u∂v∂x + v∂v∂y + w∂v∂z + ∂v∂t = 2.307 mm/s2

az = dzdt = u∂w∂x + v∂w∂y + w∂w∂z + ∂w∂t = 0

hence a = 12.68 mm/s2.

In flow field, the rotational components are as under:  given in eq (93) and rotation is given in eq (94)

tandα = ∂v∂xdxdxdt 										     (93)

hence dαdt = ∂v∂x 											     (94)

similarly dβdt = ∂u∂y

rotation wz = 0.5  dαdt-dβdt = 0.5∂v∂x-∂u∂y = 3.59 s-1

w =0.5 i jk∂∂x∂∂y∂∂zuvw 										     (95)		The vertical force exerted by the fluid on the workpiece = dFv = weight of fluid of the above surface = ρghdAcosθ = 0

where hdAcosθ is the volume of the media above the surface.

dFv = 1.1 × 10-3 × 9800 × (650/2) × 3.14 × 8 × 16 × (1/1.14) = 1235.2 kN.

The horizontal force acting on the workpiece = dFh = ρghdAsinθ = 0.

where dAsinθ is the projected area.

Summary

- Firstly mathematical and computational modelling of EMR-AFM process was done.

- Heat transfer, flow, velocity analysis model was prepared and effect of magnetic field and electrochemistry was studied.

- The model based on forces and MR calculation based on abrasive particles was prepared and analysed.

- CFD analysis of media flow through the fixture path was done and rheological properties were studied and analysed.

CHAPTER 6: RESULTS AND DISCUSSION

In this chapter the output results of both mathematical and experimental investigation are discussed and analysed. The experimental values obtained on developed EMR-AFM setup in terms of material removal and roughness of surface were analysed and the developed polymer media results were compared. These values were compared with the results obtained through mathematical models and the results from fuzzy logic optimization and grey relational analysis were tabulated and discussed. Further the computational flow dynamics of the polymer media was done using Solidworks software and various rheological properties were studied.

The results and discussion section is the main output of the experimental and analytical research carried out by the researchers in the present study. It comprises the output results, i.e., material removal and roughness behavior with respect to input parameters taken on the hybrid EMR-AFM setup. Further the mathematical and computational modelling of the process alongwith Taguchi L9 OA, fuzzy logic, GRA optimization technique results are also discussed in details.

6.1 Effect of Process Parameters on MR

In this section, the output material removal (MR) results obtained during AFM is analysed considering the effect of input parameters taken. Firstly, the different polymer media that were prepared were utilized in the process and their effect was calculated. It can be found out in the literature that material removal or wear was achieved in more amount by using hard abrasive particles based tools. Hence, the role of abrasive particles is very high in material removal from the work surface. The experiments were performed based on Taguchi L9 OA, by taking first three parameters, i.e., electrolytic voltage, number of cycles and pressure as variables and rest parameters as constant, as shown in table 6.1. The five different types of prepared media are used to check the best usable media in AFM process. The table 2 consists values of material removed during AFM process in case of different media viz. SBR, NTR, SR, SR, NR and PBS, used. The MR was found to be minimum in PBS, i.e., 2.39 mg, maximum in SBR, i.e., 3.88 mg and intermediate results were obtained in NTR, NR and SR media, as given in table 3. It can be concluded that maximum MR occurs in case of SBR media usage, i.e., 4.9 mg at electrolytic voltage 18 V, number of cycles 4 and extrusion pressure 10 bar. But when voltage taken was 6 V, number of cycle 6 and pressure 30 bar, MR was found to be minimum, i.e., 1.7 mg in case of PBS media usage. The reason may be the poor flow ability of PBS and due to lesser input voltage. Hence, it is proven that SBR results in more removal of material as compared to PBS, further, electrolytic voltage increases the MR, whereas pressure and number of cycles effect on MR is lesser as compared to that of voltage.

Table 6.1 Effect of different polymer media used on material removal

| Exp. No. | Material removal (MR) (mg) |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | SBR | NTR | SR | PBS | NR |
| 1 | 3.6 | 3.6 | 3.9 | 2.5 | 2.3 |
| 2 | 4.4 | 3.8 | 3.8 | 2.1 | 2.3 |
| 3 | 4.0 | 3.1 | 3.9 | 1.7 | 2.3 |
| 4 | 3.0 | 3.7 | 3.5 | 3.2 | 3.1 |
| 5 | 4.9 | 2.5 | 3.3 | 2.4 | 2.4 |
| 6 | 3.4 | 2.5 | 3.1 | 2.1 | 3.8 |
| 7 | 3.6 | 2.3 | 4.0 | 2.9 | 3.33 |
| 8 | 4.9 | 3.8 | 3.2 | 2.0 | 3.0 |
| 9 | 3.5 | 3.1 | 3.8 | 2.6 | 3.3 |
| Avg. | 3.8 | 3.1 | 3.6 | 2.3 | 2.8 |

In table 6.2, ANOVA technique applied shows that model is significant including media, pressure, number of cycles and volume of media, denoted by letters A,B,C, and D, respectively. The equation in terms of coded factors can be used to make predictions about the response for given levels of each factor. As seen from table 3, which is based on analysis of variance for the workpiece material removal, clearly indicates that the model is significant and the lack of fit is found to be insignificant. The P-values of the parameters, i.e., A, B, C and D are also significant alongwith their combination sets, i.e., AB, BC, etc., and their square values, the model degree of freedom being 14. The input parameters taken were in 4 levels, i.e. A (1. NR, 2. NTR, 3. SBR, 4. PBS), B (1. 15, 2. 20, 3. 25, 4. 30), C (1. 6, 2. 7, 3. 8, 4. 9) and D (1. 200, 2. 215, 3. 230, 4. 245), the units of A, B, C and D being dimensionless, bar, number and ml respectively. The surface plots obtained showing output material removal results in the RSM technique are as shown in figure 6. the input variables, i.e., A, B, C and D are taken on horizontal plane, i.e. X1 and X2 axis, while output variable, i.e., MR is taken on Y axis.

Table 6.2 ANOVA table for material removal

| Source | Sum of squares | DOF | Mean square | F-value | P-value Prob.>F |  |
| --- | --- | --- | --- | --- | --- | --- |
| Model | 10.09 | 14 | 0.72 | 5.68 | 0.0009 | Significant |
| A-Type of media | 0.41 | 1 | 0.41 | 3.27 | 0.0006 |  |
| B-Extrusion pressure | 6.023E-003 | 1 | 6.023E-003 | 0.047 | 0.0004 |  |
| C-No. of cycle | 0.029 | 1 | 0.029 | 0.23 | 0.0072 |  |
| D-Vol. of media | 0.90 | 1 | 0.90 | 7.07 | 0.0079 |  |
| AB | 4.977E-003 | 1 | 4.977E-003 | 0.039 | 0.0056 |  |
| AC | 0.058 | 1 | 0.058 | 0.46 | 0.0092 |  |
| AD | 0.072 | 1 | 0.072 | 0.56 | 0.0041 |  |
| BC | 0.15 | 1 | 0.15 | 1.20 | 0.0099 |  |
| BD | 0.026 | 1 | 0.026 | 0.21 | 0.0044 |  |
| CD | 0.073 | 1 | 0.073 | 0.58 | 0.0096 |  |
| A2 | 3.30 | 1 | 3.30 | 25.98 | 0.0001 |  |
| B2 | 4.67 | 1 | 4.67 | 36.83 | <0.0001 |  |
| C2 | 2.52 | 1 | 2.52 | 19.84 | 0.0005 |  |
| D2 | 0.062 | 1 | 0.062 | 0.49 | 0.0037 |  |
| Residual | 1.90 | 15 | 0.13 |  |  |  |
| Lack of fit | 1.54 | 10 | 0.15 | 2.14 | 0.2075 | Not significant |
| Pure error | 0.36 | 5 | 0.072 |  |  |  |
| Cor total | 12.00 | 29 |  |  |  |  |

The figure 6.1(a) and 6.1(b) shows top and front view respectively, that are based on constant type of media parameter used in which the input parameters combination set AB and AC was used rexpectively. It can be inferred from the figure 6.1(a) and 6.1(b) that MR value lies between 1.5 mg to 1.9 mg, maximum being at extrusion pressure 21 bar and number of cycles 7. In figure 6.1(c) and 6.1(d), the output MR results are based on constant extrusion pressure used in which top and front view surface plots are plotted to analyse the MR results based on BC and AD input parameters combination sets. The MR was nearly 2.25 mg, i.e. more removal of material occurs at constant pressure, maximum being at volume of media 225 ml and during usage of media number 3, i.e. SBR.

The hybrid electromagneto rotational abrasive flow machining (EMR-AFM) setup resulted in higher material removal and better surface integrity. For calculating the effect of magnetic field on the hybrid AFM set-up , the three input parameter i.e. magnetic voltage or flux, ECM rod size and voltage were taken and it was found that both electric and magnetic lines of force caused increased velocity of particle hitting the work surface. The rod size first increases the metal removal and then its effect is negligible. The Taguchi L-9 OA is applied to optimise the result in which 9 experiments have been performed using different combination of 3 input parameters, the results shown in table 6.3.

- (b)

2.5						    2.5

MR 1.5					              MR 1.5

0.5						        0.5

2.5			            23			 2.5				    9

3			    21			             3			           8

A 	  3.5                    19	      B 			          A         3.5                     7      C

4  17                   					  4    6

X1 = A, X2 = B						X1 = A, X2 = C

Actual factors: C = 8, D = 225				Actual factors: B = 20, D = 225

(c)  							   (d)

3						     3

2.5						   2.5

2						       2

MR 1.5					              MR 1.5

1						         1

2						         15

2.5						              17

3			         250		             B      21			                10

A	     3.5		      225   	D			          25                            8	  C

4   	   200	                                              			     6

X1 = A, X2 = D						X1 = B, X2 = C

Actual factors: B = 20, C = 8				Actual factors: A = 3, D = 225

A: Type of media, B: Extrusion pressure, C: No. of cycles, D: Vol. of media

Figure 6.1 3D Surface model (a) Type of media (surface view from top), (b) Type of media (surface view from front), (c) Extrusion pressure (surface view from top), (d) ) Extrusion pressure (surface view from front)

Abrasive type (at), abrasive mesh size (am), electric voltage (ev), rotational speed (rs), magnetic voltage (mv), workpiece type (wt), number of cylces (nc), extrusion pressure (ep) i.e. machine parameters used are shown in table 6.3. The combination of input parameters for experiments using Taguchi L9 OA technique, is made in a scientific manner so as to understand the overall effect of abrasive particles, voltage and workpiece used, etc. The first combination, i.e., (at, am, ar), signifies the importance of abrasive particle, its size and the mixing ration in the machining efficiency. The second combination (ev, rs, mv) is based on the hybrid EMR-AFM machine setup fabricated, so as to analyse the effect of different types of forces on the output finishing results. The third combination, i.e., (wt, ep, nc) gives us the data of conventional machine parameters effect on MR and Ra results.

Table 6.3 Material removal and roughness output values

| Parameters | at, am, ar |  | ev, rs, mv |  | wt, ep, nc |  |
| --- | --- | --- | --- | --- | --- | --- |
| Exp. No. | MR | Ra% | MR | Ra% | MR | Ra% |
| 1 | 5.8 | 24.01 | 7.8 | 34.01 | 6.8 | 24.4 |
| 2 | 5.03 | 16.4 | 7.3 | 26.4 | 6.03 | 17.9 |
| 3 | 4.86 | 30 | 6.9 | 30 | 5.86 | 30.9 |
| 4 | 6.64 | 18.8 | 6.9 | 28.8 | 5.64 | 18.2 |
| 5 | 9.19 | 14.33 | 9.2 | 24.33 | 8.19 | 14.69 |
| 6 | 8.14 | 13.1 | 9.5 | 23.1 | 8.14 | 13.98 |
| 7 | 7.1 | 25 | 10.1 | 35 | 8.1 | 25.91 |
| 8 | 6.5 | 8.9 | 10.5 | 9.9 | 8..5 | 8.9 |
| 9 | 10.5 | 10.9 | 12.9 | 10.9 | 11.5 | 10.99 |
| Avg. | 7.06 | 18.1 | 9.02 | 24.75 | 7.64 | 18.41 |

It can be inferred from output results, as shown in table 6.3, that the second combination set results in overall increase in MR and percentage decrease in Ra value as compared to conventional AFM machine used for experimental purpose. Hence the hybrid machine setup used by the authors resulted in 34.5 % and 17.8 % rise in % Ra improvement and MR respectively, as compared to traditional setup, the average output results data is as shown in table 6.3.

- (b)

(c)

S/N ratio data, --------- raw data

Figure 6.2. S/N ratio and raw data output graphs of material removal rate vs (a) Magnetic voltage, (b) ECM rod size, (c) ECM voltage respectively

The applied magnetic field at starting increases material removal at slower rate but afterwards its increase is high, as shown in figure 6.2(a). In figure 6.2(b), it is clear that the MR rate value increases from 0.2 mm3/min to 3.0 mm3/min when ECM rod size of diameter 6 mm is put inside the workpiece instead of rod of 4 mm diameter size. This indicates that by increasing the diameter or decreasing the gap between anode and cathode from 6 mm to 4 mm, the more MR occurs. Afterwards, using thick thick ECM rods greater than 6 mm results in very less improvement in removal of material. The approximately same trend is shown in figure 6.2(c), in case of electrolytic voltage, in which MR increases at fast rate when electrolytic voltage increases from 6 V to 12 V, but further increase in voltage increases MR at slower rate.

Table 6.4 ANOVA table

| Source | Sum of Square | Degrees of Freedom | P | V | F-value | Pool |
| --- | --- | --- | --- | --- | --- | --- |
| Electrolytic rod | 630.33 | 2 | 81.24 | 80.50 | 19 | No(significant) |
| ECM Voltage | 120.44 | 2 | 16.14 | 300.12 | 19 | No(significant) |
| Magnetic Flux | 33.22 | 2 | 4.46 | 15.54 | 19 | No(significant) |
| Error | 2.03 | 2 |  |  |  | No(significant) |

The ANOVA calculations for S/N ratio is as shown in table 6.4. The three experimental runs of material removal of each workpiece is shown alongwith mean, variance and sum of squares. It is found that all the three input parameters taken are significant, their degree of freedom being 2 each.

Figure 6.3 (a) MR vs rotational speed plot, (b) Power vs volume of material removal plot

The material removal effect with and without rotational effect is clearly depicted in figure 6.3(a) in which 1600 rpm speed resulted in maximum removal of material. When rotational force in not employed in AFM process, then on an average 2.9 mg material gets removed, while using rotational setup results in removal of material upto 4.5 mg. As shown in figure 6.3(b), it is clear that when speed of rotation is increased from 800 to 1600 rpm, the MR value drastically increased from 2.5 µm to 4.5 µm. The power consumption of the machine vs volume of material removal in case of different polymer media developed is shown in figure 6.3(b), where it was found that natural rubber based media required more power as compared to nitrile and SBR for same volume of material removed. The power consumption in EMR-AFM process got reduced from 0.65 kW to 0.1 kW when NR media was used, while SBR media usage resulted in constant power consumption of about 0.5 kW with increase in MR of workpiece. The material removal volume was calculated by calculating change in weights of the workpiece at the start and end of process.

The proper validation has been done for both experimental and analytical output results; so that we can obtain best optimized result i.e. higher material removal and lower surface roughness value. In figure 6.4(a), material removal effect on magnetic voltage and number of extrusion cycles is explained. The increase in number of cycles from 4 to 8 gradually increased the MR as seen from the surface plot and material removal first increased and then decreased by increasing the magnetic voltage. The analytical methods, ie., surface and interval plots were applied so that the complete overview of the various input parameters’ effect on output responses can be understood. In the interval plot as shown in in figure 6.4(b), the 3 intervals of rod size taken at 4, 5, 6 mm, the MR results obtained are about 0.17 gm at 4 and 5 mm rod size, while 0.125 gm at 6 mm rod size.

(a) 						(b)

Figure 6.4 (a) Surface plot of MR vs magnetic voltage, (b) ANOVA interval plot of MR vs rode size

From this data, we can easily infer that the MR increases when we use ECM rod of size more than 4 mm and the same inference was drawn in the previous section. Hence, it is concluded that in both cases, i.e., Taguchi L9 OA output results and the interval plots, the results are nearly same.

6.2 Effect of Input Parameters on Surface Roughness (Ra)

In this section, the Ra improvement is analysed and the effect of various input parameters is understood in details. Various authors have obtained significant results in surface roughness reduction. Firstly, their brief work is introduced in the section and then the output results obtained by the present author in doing experiments on EMR-AFM setup are discussed in detail. If EDM and ECM lapping was used, then surface roughness was improved upto 0.07 mm in 2 min. In double disc magnetic abrasive finishing of paramagnetic materials, Al disc with 4 NdBFe magnets is used. Al is used as casing because permeability is one, hence magnetic lines of force are not affected. The best surface finish results were obtained when working gap was 1 mm, 18% by weight abrasive particles, speed 436 rpm for stainless steel while for Cu alloy when working gap 2.3 mm, 36% by weight abrasives and 467 rpm speed.

In case of finishing of workpiece material, the utmost requirement is that surface obtained should be of very fine finish and integrity. Hence, the input parameters are controlled in such a wayso as to get nano-level fine finished products. These products are used in precision instruments where high degree of accuracy is needed, in medical and surgical dentures where medical care has to be done in a very safe environment since the life and health of an individual is considered. The effect of finishing time of workpiece, extrusion cycles, machining pressure on the output Ra response was analysed graphically. The matrix of mold injection surface of initial Ra value 0.65 µm was polished till Ra reached 0.07 µm in 1500 seconds in abrasive flow machining (Jain et al. 1999). In the prepared machine setup, the surface roughness was reduced from initial Ra value of 1.4 to 0.07 µm in 1200 seconds, i.e. 40 % more roughness reduction in 20% lesser time in contrast to conventional AFM process, comparison shown in figure 6.5(a). The finishing time was calculated with the help stopwatch setting on during the number of extrusion cycles of finishing the workpiece. The finishing time ranges from 5 min to 25 min per workpiece and it was found that maximum cutting of workpiece material occurred in first 10 min and afterwards the surface roughness improvement was negligible.

- (b)

(c)      		                                     		        (d)

Figure 6.5(a) Reduction in Ra vs (a) finishing time, (b) extrusion cycles, (c) media pressure, (d) % abrasive concentration plot

The Ra decrease was obtained and compared with the input parameters viz. vibration amplitude, pressure and time of machining the temperature and viscosity of media taken was 300 K and 730 poise respectively as shown in (Venketesh et al. 2015) while initial Ra kept between 1.2-1.4 µm and concentration of abrasive in media by weight was 60:40.  The parameters taken during operations include volume flow rate in the range 7000-16000 mm/s and piston stroke length per cycle 4 × 50 and 200 mm on the 50CrMo4 material. The surface roughness value was reduced from 0.8 µm to 0.2 µm in rotary ultrasonic machining. the surface roughness value was drastically reduced from 1.4 µm to 0.11 µm in the present working set up, as shown in figure 6.5(b). The roughness value decrease with number of extrusion cycles as shown. It can be inferred from figure 6.5(b), that the number of machine extrusion cycles requirement is decreased from 15 to 8 in the present hybrid setup utilized in experimentation. The conventional setup resulted in roughness reduction from 1.25 µm to 0.6 µm,  while the hybrid setup decreased Ra from 1.5 µm to 0.2 µm, i.e., 53.8 % more improvement in roughness. The main aim is to achieve high material removal, better surface finish, reduced sub-surface damage. In figure 6.5(c) and (d), the surface roughness percentage improvement is more in hybrid electrolytic magneto rotational AFM setup as compared to conventional AFM process. In case of conventional AFM process, when 20 % abrasive particles and when no abrasive particle is used, then Ra value get reduced from 0.3 µm to 0.12 µm at gradual rate with increase of media pressure and roughness value increased with increase of pressure respectively. As shown in figure 6.5(c), it is clear that in EMR-AFM setup, the roughness value got reduced from 0.7 µm to 0.19 µm at 50 bar extrusion pressure value. Hence it is concluded that more decrease in surface roughness can be achieved in hybrid machine setup at half the extrusion pressure value. It can be inferred from figure 6.5(d), that 10 % more improvement in roughness value results in case of hybrid AFM setup as compared to conventional AFM process when percentage abrasive concentration is increased in polymer media.

6.3 Matlab Fuzzy Logic and Grey Relational Optimization of Material Removal and Surface Roughness Results

Grey relational analysis optimization technique was used by Lin and Lee (2009). After getting the output optimized results of MR and Ra values in Taguchi L9 OA and RSM technique, the results are optimized in multi objective fuzzy logic optimization and grey relational analysis and then compared and to get to a conclusion that which technique is best. In fuzzy logic optimization process, first of all the membership functions were defined i.e. very low to very high in 5 levels, shown in figure 6.6. Highest MPCI value corresponds to lowest rank as shown in table 6. In GRA, firstly, the normalization of data is done, then for various experiments the grey relational coefficients are calculated, as shown in table 6.5. These values range from 0 to 1. At last grey relational grade is calculated. The eq. (1) is used for calculating GRC value.

GRC = dmin+e.dmaxdk+ e.dmax  									      (1)

where d is the value corresponding to the experiment run ranging from k =1-9, e is value taken corresponding to the number of output responses taken.

Table 6.5. GRC and MPCI rank values corresponding to Taguchi L9 OA experimentation

| Exp. No. | % Ra | Normalised (N) | Deviation (D) | GRC | MR | N | D | GRC | MPCI | Rank |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 (111) | 20.37 | 0.09 | 0.81 | 0.38 | 4.2 | 0.00 | 1.00 | 0.33 | 0.06 | 9 |
| 2 (122) | 16.4 | 0.00 | 1.00 | 0.33 | 10.8 | 0.43 | 0.57 | 0.46 | 0.25 | 8 |
| 3 (133) | 50.8 | 0.75 | 0.25 | 0.66 | 12.4 | 0.53 | 0.47 | 0.51 | 0.55 | 3 |
| 4 (212) | 30.3 | 0.30 | 0.70 | 0.41 | 14.4 | 0.66 | 0.34 | 0.59 | 0.42 | 6 |
| 5 (223) | 38.1 | 0.47 | 0.53 | 0.48 | 19.6 | 1.00 | 0.00 | 1.00 | 0.65 | 1 |
| 6 (231) | 62.4 | 1.00 | 0.00 | 1.00 | 10.2 | 0.39 | 0.61 | 0.45 | 0.64 | 2 |
| 7 (313) | 36.5 | 0.44 | 0.56 | 0.47 | 7.2 | 0.19 | 0.81 | 0.38 | 0.31 | 7 |
| 8 (321) | 50.4 | 0.74 | 0.36 | 0.58 | 8.2 | 0.26 | 0.74 | 0.40 | 0.45 | 5 |
| 9 (332) | 53.9 | 0.82 | 0.28 | 0.64 | 9.8 | 0.36 | 0.64 | 0.43 | 0.54 | 4 |

The three input variables taken were magnetic flux, electrolytic voltage and rotational speed and each parameter has 3 levels. As it is clear from table 6.5, rank 1 corresponds to the condition of magnetic flux of 0.75 Tesla corresponding to 125 V magnetic voltage, 12 V electrochemical voltage and 160 RPM rotational speed. In table 6.5, the final output results in terms of MR and Ra are listed for both fuzzy logic and grey relational analysis. The GRC values range from 0.0 to 1.0 in case of material removal of 4.2 µm to 19.6 µm respectively, while it range from 0.33 to 1.0 for percentage roughness improvement value of 16.4 % to 62.4 % respectively. Hence, it is concluded that GRC value increases if material removal increase and percentage improvement of roughness increases. After GRC calculations, the deviation is found out and then at last MPCI value is calculated from Matlab fuzzy logic software. The MPCI values ranges from minimum 0.06 to maximum 0.64, i.e., it signifies the best combination of input parameters so as to get intermediate value of material removal and improvement of roughness value, i.e. optimized combined result, hence called multi objective optimization process. As shown in figure 6.6, the FIS variables are set as output variables of finishing operation and corresponding MPCI variables are generated. It is also shown that membership function plots are also set according to the input parameters, as low (L), very low (VL), medium (M), large (L) and very large (VL) based on the effect of input parameters, i.e., magnetic flux, electrolytic voltage and rotational speed.

Figure 6.6 Fuzzy logic operators alongwith membership plot and FIS variables

6.4 Magnetic Field and Electrolytic Voltage Results

In this section experimental results based on eletrochemo-magneto AFM process have been explained in detail. The table 6.6 and 6.7 gives the values of parameters and their levels and corresponding output response corresponding to magnetic, electrochemical voltage and rod size respectively.

Table 6.6 Parameters and their level values

| Symbol | Process Parameters | Unit | Level 1 | Level 2 | Level 3 |
| --- | --- | --- | --- | --- | --- |
| MV | Magnetic Voltage | V | 50 | 125 | 200 |
| ER | ECM Rod size | mm | 4 | 6 | 8 |
| EV | ECM Voltage | V | 6 | 12 | 18 |

The orthogonal array L9 table is given below as in table 6.7.

Table 6.7 The L9 (34) OA parameters and response

| Exp no. | Run order | Parameter conditions |  |  | Response output |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | MV | ER | EV | R1 | R2 | R3 |
|  |  | 1 | 2 | 3 |  |  |  |
| 1 | 1 | 1(50) | 1(4) | 1(6) | 0.17 | 0.18 | 0.17 |
| 2 | 4 | 1(50) | 2(6) | 2(12) | 2.44 | 1.94 | 1.77 |
| 3 | 7 | 1(50) | 3(8) | 3(18) | 3.33 | 3.67 | 4.54 |
| 4 | 5 | 2(125) | 1(4) | 2(12) | 0.45 | 0.54 | 0.26 |
| 5 | 8 | 2(125) | 2(6) | 3(18) | 2.9 | 2.77 | 2.53 |
| 6 | 2 | 2(125) | 3(8) | 1(6) | 1.36 | 1.81 | 1.49 |
| 7 | 9 | 3(200) | 1(4) | 3(18) | 0.65 | 0.71 | 0.63 |
| 8 | 3 | 3(200) | 2(6) | 1(6) | 1.39 | 1.46 | 1.53 |
| 9 | 6 | 3(200) | 3(8) | 2(12) | 5 | 6.57 | 6.96 |

6.4.1 Procedure of Experimental Work

Firstly, we fill the media into one of the cylinders of the two way AFM. Placing the workpiece between the two-piece fixture, we fix both the fixtures on the upper and lower jig such that they fit into the groove of the jig. We then fix this jig onto the AFM setup such that the cylinders are in line with the pistons with the help of the nut and bolt provision given. Subsequently, we set the pressure manually by using the handle for both the upper and lower side. After the pressure has been set, we manually operate the pistons with the help of the operating levers in accordance with the number of cycles required. Then electrolytic setup is installed which uses DC transformer in which the alternating current that reverses direction periodically is converted into direct current flowing in only one direction using rectifier device. In motor generated set the AC motor shaft is coupled to DC generator. The multi phase alternating current is produced in armature windings, commutator on the armature converts it into direct output current. A transformer contains two magnetically coupled windings, the primary winding is driven by input AC supply, while the secondary winding give supply to AC-DC converter.  After the machining is done, we unclamp and dismantle the fixture. We then remove the workpiece, clean it with cloth and in a toluene bath and the surface roughness and weight is measured. The difference in weight gives us the material removal. Clean setup after experimentation. Tabulate and analyse observations to get results.

fixes into the media cylinder.

6.4.2 Result Output

The output results in terms of material removal is explained below. In table 4, the three experimental runs of material removal of each workpiece is shown alongwith mean, variance and sum of squares. The L-9 OA is applied to optimise the result in which 9 experiments have been performed using different combination of 3 input parameters. The main effects of S/N ration i.e. SN ratio alongwith levels and iterations is shown in table 6.9. The three input variables are magnetic voltage, ECM voltage and rod size.

Table 6.8 Mean and variance of output results

| S.No. | R-1 | R-2 | R-3 | Mean | Variance | Sum of Squares of Reciprocals |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 0.17 | 0.18 | 0.17 | 0.173 | 3.33E-05 | 33.356 |
| 2 | 2.44 | 1.94 | 1.77 | 2.05 | 0.121 | 0.250 |
| 3 | 3.33 | 3.67 | 4.54 | 3.846 | 0.389 | 0.070 |
| 4 | 0.45 | 0.54 | 0.26 | 0.416 | 0.020 | 7.720 |
| 5 | 2.9 | 2.77 | 2.53 | 2.733 | 0.035 | 0.135 |
| 6 | 1.36 | 1.81 | 1.49 | 1.553 | 0.053 | 0.432 |
| 7 | 0.65 | 0.71 | 0.63 | 0.663 | 0.001 | 2.290 |
| 8 | 1.39 | 1.46 | 1.53 | 1.46 | 0.004 | 0.471 |
| 9 | 5 | 6.57 | 6.96 | 6.176 | 1.076 | 0.027 |
| Sum | 17.69 | 19.65 | 19.88 |  |  |  |
| Total Sum (T) |  | 57.22 |  |  |  |  |
| Average |  | 2.1193 |  |  |  |  |

It has been shown that the combined effect of magnetic field and electrolytic field increase the material removal and hence these magnetic and electric lines of forces result in increased velocity of impact of abrasive particles onto the internal walls of worpiece.

Table 6.9 S/N ratio table for response output

| Level | Magnet | ECM Rod | ECM volt |
| --- | --- | --- | --- |
| L1 | 0.753 | -9.235 | -2.773 |
| L2 | 1.153 | 5.987 | 4.222 |
| L3 | 5.068 | 10.223 | 5.527 |
| L2-L1 | 0.399 | 15.223 | 6.995 |
| L3-L2 | 3.915 | 4.236 | 1.305 |
| Difference | 3.516 | -10.987 | -5.690 |

Both the response tables i.e. for S/N ratio and for raw data have found to be significant. All the parameters are found suitable according to their given levels and their values. Hence the optimized results are found correct according to the given conditions. The ANOVA raw data data is given in table 6.10.

Table 6.10 ANOVA Raw Data

| Source | SS | DOF | V | P | F-Ratio | F-Ratio | Pooling |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Magnet | 6.592 | 2 | 3.296 | 7.198 | 4.223 | 19 | No (Significant) |
| ECM rod | 53.305 | 2 | 26.652 | 58.211 | 34.147 | 19 | No (Significant) |
| ECM volt | 16.063 | 2 | 8.031 | 17.542 | 10.29 | 19 | No (Significant) |
| Error | 15.61 | 20 | 0.78 | 17.046 |  |  |  |
| T | 91.571 | 26 |  | 100 |  |  |  |

6.4.3 Introduction to RSM

Response Surface Methodology (RSM) is amalgamation of statistical methods in which desired values are to be controlled. Here we forecast the properties of product, find out the factor level, relationships between variables and designation of individual and combined effect of input variables is done.

6.4.3.1 Procedure of RSM

It starts with problem recognition, objective formulation, definition of response characteristics and factors related. Then levels are selected, analysed using ANOVA and regression model is formulated and then optimization is done using central composite design (CCD). Optimal factor levels are identified and then experiments are performed. We find the optimum spot where response is maximised or minimised.

Table 6.11 Input variables

| Type of media | Pressure (bar) | Volume of media | Number of cycle |
| --- | --- | --- | --- |
| 1 | 10 | 175 | 4 |
| 2 | 15 | 200 | 6 |
| 3 | 20 | 225 | 8 |
| 4 | 25 | 250 | 10 |
| 5 | 30 | 275 | 12 |

The two models used are screening response and steepest ascent model. The steepest ascent model tells where to take new experiments and the response at those points are noted. It is a second order model that includes linear, cross product terms and second order term. The linear terms have one subscript and quadratic have two subscripts. There are k*(k-1)/2 interaction terms. The second order model is the base of response surface methodology. First of all, the values of parameters to be set are decided, based on their availability on the machine setup. Then experimentation is performed according to the design table. The table 6.11 shows the different input variables and their five levels and different factor values have been given in table 6.12.

Table 6.12 Values of factors and different points of cube

| Readings | Factors | Replicas | Runs | Base blocks | Blocks | Cube points | Center points | Axial points | Center points (axial) |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Value | 4 | 1 | 30 | 1 | 1 | 8 | 6 | 6 | 0 |

The design was set and graphs were obtained between different values as shown in table 6.13.

Table 6.13 Design table in terms of actual factors

| Run | Type of media | Pressure | No. of cycle | Volume of media | Material removal |
| --- | --- | --- | --- | --- | --- |
| 1 | 4 | 25 | 6 | 200 | 1.9543 |
| 2 | 3 | 20 | 8 | 225 | 2.6532 |
| 3 | 4 | 15 | 10 | 200 | 1.5329 |
| 4 | 2 | 25 | 10 | 200 | 1.3932 |
| 5 | 1 | 20 | 8 | 225 | 0.8032 |
| 6 | 4 | 15 | 6 | 200 | 1.8578 |
| 7 | 3 | 10 | 8 | 225 | 0.7593 |
| 8 | 3 | 30 | 8 | 225 | 0.8029 |
| 9 | 4 | 25 | 10 | 200 | 2.2076 |
| 10 | 2 | 25 | 6 | 250 | 1.1029 |
| 11 | 2 | 25 | 6 | 200 | 1.4191 |
| 12 | 3 | 20 | 4 | 225 | 1.1529 |
| 13 | 4 | 25 | 6 | 250 | 0.9043 |
| 14 | 4 | 15 | 10 | 250 | 1.2866 |
| 15 | 2 | 15 | 6 | 200 | 2.0546 |
| 16 | 3 | 20 | 12 | 225 | 1.2874 |
| 17 | 2 | 15 | 10 | 250 | 0.8031 |
| 18 | 3 | 20 | 8 | 225 | 2.0021 |
| 19 | 4 | 25 | 10 | 250 | 0.9041 |
| 20 | 3 | 20 | 8 | 225 | 2.5234 |
| 21 | 3 | 20 | 8 | 225 | 2.2872 |
| 22 | 3 | 20 | 8 | 275 | 2.3987 |
| 23 | 2 | 15 | 6 | 250 | 0.8155 |
| 24 | 2 | 25 | 10 | 250 | 1.1027 |
| 25 | 5 | 20 | 8 | 225 | 1.2874 |
| 26 | 3 | 20 | 8 | 175 | 2.0832 |
| 27 | 2 | 15 | 10 | 200 | 1.0571 |
| 28 | 3 | 20 | 8 | 225 | 2.7352 |
| 29 | 3 | 20 | 8 | 225 | 2.5229 |
| 30 | 4 | 15 | 6 | 250 | 1.2876 |

The table 6.14 gives values of static control terms.

Table 6.14 Statics control terminology

| Readings | Std. Dev. | Mean | CV% | Press | R-Sq | Adj R-Sq | Pred R-Sq | Adeq R-Sq |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Value | 0.36 | 1.57 | 22.74 | 9.40 | 0.8814 | 0.6934 | 0.2163 | 7.458 |

6.4.4 Effect of Electrolytic Force and Magnetic Assisted AFM on MR

The voltage supplied to the anode and cathode is in the range 6-18 V, and it affects MR during AFM process. The conventional AFM is made hybrid with the help of attachment of electrochemical electrodes and prepared electrolyte. For electrochemical action to occur, both anode (workpiece) and tool (ECM rod) must be conducting in nature and flow of current should be easy through the prepared electrolyte.

6.4.4.1 Effect of ECM Voltage and Rod Size on MR

The analysis of the effect of ECM rod and supplied voltage on material removal is done in an exhaustive manner in MiniTab software so that accurate result can be obtained and these results are compared with the actual values obtained after performing a large number of experiments on the prepared hybrid magnetic force assisted electrochemical abrasive flow finishing machine supporting in-house manufactured nylon fixture. The proper validation has been done for both experimental and analytical output results; so that we can obtain best optimized result i.e. higher material removal and lower surface roughness value. A number of analytical methods were applied so that the complete overview of the various input parameters’ effect on output responses can be understood, that included surface plot, interval plot, fitting line plot, pareto chart, contour plot. The detailed graphs and output results are discussed in the coming explanation.

6.4.4.2 Response Surface Methodology Results

The response surface methodology (RSM) technique is the optimization software employed in order to get best optimized results as shown in figure 6.7. The material removal is affected by both ECM rod size as well as supplied voltage. The different ECM voltage i.e. 5, 10, 15 V are shown one axis, rod size i.e. 4, 5, 6 mm are shown on another axis while the output response i.e. MR (gm) are clearly depicted in figure 6.7. If we increase supplied voltage the material removal decreases and if the large sized rod is taken, it resulted in lesser removal of material. This is due to the reason that the electrochemical generally works best if there is minimum gap.

(a) 						(b)

Figure 6.7 surface plot of MR vs (a) ECM voltage and (b) magnetic voltage

6.4.4.3 ANOVA Output and Fitted Line Plot Analysis

In the interval plot explained in figure 6.8(a) , the 3 intervals of rod size taken at 4, 5, 6 mm, the MR results obtained are about 0.17 gm at 4 and 5 mm rod size while 0.125 gm at 6 mm rod size. In the pooled analyses of variance, 95 % confidence interval is taken for the mean and standard deviation was used to calculate intervals.

Figure 6.8(a) ANOVA interval plot of MR vs rode size, (b) ANOVA interval plot of MR vs voltage

The 0.175 gm, 0.17 gm and 0.118 gm material removal was obtained at the input supplied electrochemical voltage of 6, 12 and 18 V respectively. The another method of analysis of the effect of input parameters on the output results is the technique of  fitted line having scattered points on the graphic line obtained and the points are above, on or below the line at the pre-decided three levels of the input parameter taken at the x-axis.

- (b)

Figure 6.9 Fitted line plot of (a) MR vs rod size, (b) MR vs ECM voltage

If the rod size is increased from 4 to 6 mm, then the material removal gradually decreases from about 0.167 gm to 0.135 gm and standard value ranges from 0.2397-0.01794 gm for rod size. The S value is 0.0653963, R-Sq is 5.4 % and R-Sq (adj) is 0.0 %. In case of supplied ECM voltage the fitted line plot is explained in figure 6.9, where material removal decreases from 0.175 gm to 0.12 gm as we increase voltage from 6 to 18 V.  The standard MR values ranges from 0.2021 to 0.004157 gm for ECM voltage parameter, the S value is 0.0683666, the R-Sq is 11.2 % and R-Sq (adj) is 3.1 % in this case.

6.3 Pareto and Contour Chart Detailed Explanation

In figure 6.10(a), the Pareto chart analysis of the effect of input parameters i.e. ECM voltage and ECM rod size on the output response i.e. MR (gm) is done.

- (b)

Figure 6.10(a) Pareto Chart of standardized effects, (b) Contour plot of MR vs rod size and voltage

The value of sensitivity α is 0.05, A is ECM voltage while B is rod size and the terms A, B, AA, BB, AB values are 1.0, 0.8, 0.4, 0.39 and 0.07 respectively, these standard effect values ranges from 0 to 2.5 and the dashed vertical line is shown at the standardized effect value of 2.365. 
The contour plot of MR vs rod size, ECM voltage is shown in figure 6.10(b) where voltage is taken at x-axis and rod size at y-axis and the output response are shown in terms of curves that are viewed moving away from the origin. If the MR values less than 0.1 it is lightest green in colour at the outermost distance from the origin.

(a) 						(b)

Figure 6.11 (a) pareto chart of standardized effects, (b) interaction plot for material removal

If the value ranges between 0.1-0.12, 0.12-0.14, 0.14-0.16, 0.16-0.18, the colour becomes dark green which indicates that more material removal occurs as we go towards the origin, if MR is greater than 0.18, the black shaded region enclosing the origin is shown in the contour plot. The interaction plot is as shown in figure 6.11(b).

## 6.5 Experimental Results Based on Taguchi Analysis

This involves making the table for 9 workpieces and their corresponding observations. A 3-level table was made of the L-9 type for the parameters, pressure, passes and abrasive to media ratio. Table 6.15 shows larger is better and response table for means results.

Table 6.15 Taguchi Analysis: MRR versus pressure, no. of cycles, abrasive media

| Larger is better |  |  |  |
| --- | --- | --- | --- |
| Level | Pressure | Cycles | Abrasive media |
| 1 | 7.44 | 7.94 | 7.90 |
| 2 | 8.06 | 8.62 | 7.95 |
| 3 | 8.51 | 7.45 | 0.26 |
| Delta | 1.06 | 1.16 | 0.26 |
| Rank | 2 | 1 | 3 |
| Response Table for Means |  |  |  |
| 1 | 2.36 | 2.50 | 2.50 |
| 2 | 2.53 | 2.70 | 2.50 |
| 3 | 2.66 | 2.36 | 2.56 |
| Delta | 0.30 | 0.33 | 0.06 |
| Rank | 2 | 1 | 3 |

In figure 6.12(a) the effect of pressure, number of cycles and media on MRR is shown and in figure 6.12(b) S/N ratio effect is depicted. Smaller is better effect of roughness on different parameters is given in table 6.16.

- (b)

Figure 6.12(a) Effect of different parameters on MRR, (b) Plot for the S/N ratio of MRR

Table 6.16 Taguchi analysis: surface roughness versus pressure, no. of cycles, media

| Smaller is better |  |  |  |
| --- | --- | --- | --- |
| Level | Pressure | No of cycles | Abrasive media |
| 1 | 18.20 | 6.31 | 10.94 |
| 2 | 7.24 | 11.20 | 10.73 |
| 3 | 3.32 | 11.25 | 7.09 |
| Delta | 14.89 | 4.94 | 3.85 |
| Rank | 1 | 2 | 3 |

In figure 6.13 (a) and (b) the effect of process parameters on Ra mean value and SN ratio effect is shown respectively.

- (b)

Figure 6.13(a) Plot for different process parameters effect on the mean Ra, (b) Plot for different process parameters effect on the SN Ratio of Ra

  - Experimental Results Based on ANOVA Analysis

ANOVA (Analysis of Variance) is a simulation platform that allows one to carefully give the process parameters effect on response values and also the mean and variance values can be achieved with ease. All the input parameters were: pressure, number of cycles and abrasive to media ratio, the corresponding response values include: material removal and surface finish. The graphs of MR and Ra against parameters based on ANOVA analysis are shown in figure 6.14 and 6.15 respectively.

- (b)                                                 (c)

Figure 6.14(a) One-way ANOVA: MRR versus (a) Pressure, (b) No. of Cycles, (c) media

Figure 6.15(a) One-way ANOVA: Ra versus (a) pressure, (b) no. of cycles, (c) media

It can be seen from the figure 6.16 that as cycles are increased initially the material removal increases but after level 2 as the number of cycle increased material removal decreases

Figure 6.16(a) Effect of (a) cycles, (b) pressure, (c) CNTs on S/N ratio

This is because abrasive particles became dull after level 2 and material removal was low. CNT particles are harder as compare to the aluminium oxide. CNT has very sharp cutting edges. Table 6.17 and 6.18 gives pooled ANOVA raw and SN ratio data based on MR respectively.

Table 6.17 Pooled ANOVA (Raw Data) (MR)

Table 6.18 Pooled ANOVA (S/N Data)

So when the extrusion pressure is applied it easily cuts the peak of the roughness and causes more MR. But when surface gets smooth, after that it will cause low material removal. The average values of percentage improvement in surface roughness and S/N ratio for each parameter at Level L1, L2 and L3 are calculated and given in table 6.19.

Table 6.19 Average values and main effects: % improvement in Ra

6.7 Experimental Results to Study the Effect of Magnetic Field

From the bar diagram (figure 6.18) it is observed that MRR increases with increasing pressure and the increase is more in transition from level-1 to level-2 than in level-2 to level -3 i.e. MRR increases with decreasing slope. Magnetic flux is the most dominant among the three variables. Increasing magnetic field intensity increases the MRR significantly. Applying magnetic field increase the normal cutting force on the ferromagnetic grains. The MRR increases with increasing pressure and the increase in MRR decreases continuously. The main effects of SN ratio and means against parameters based on Ra is shown in figure 6.17 (a) and (b) respectively. Table 6.20 gives values of response for SN ratio and means.

Figure 6.17 Surface roughness versus pressure, number of cycle, magnetic field strength (a) SN ratio, (b) means

Table 6.20 Response table for SN ratio and means

| Response Table for Signal to Noise Ratios |  |  |  |
| --- | --- | --- | --- |
| level | pressure | cycles | Magnetic flux |
| 1. | -26.33 | -22.21 | -29.26 |
| 2. | -20.68 | -25.79 | -16.69 |
| 3. | -26.17 | -25.0 | -24.02 |
| DELTA | 5.66 | 3.58 | 12.57 |
| RANK | 2 | 3 | 1 |
| Response Table for Means |  |  |  |
| level | pressure | cycles | Magnetic field |
| 1. | 15.073 | 18.680 | 29.083 |
| 2. | 15.157 | 13.730 | 5.927 |
| 3. | 21.020 | 18.840 | 16.240 |
| DELTA | 5.947 | 5.110 | 23.157 |
| RANK | 2 | 3 | 1 |

(a)                                           (b)                                                (c)

Figure 6.18 (a) Graph is plotted keeping magnetic field and number of cycles at level 2, (b) magnetic field and pressure at level 2, (c) pressure and number of cycles at level 2

The MRR increases with increasing no. of cycles and the increase in MRR is almost constant. This is because as the number of cycles increases the abrasive grains perform more cutting and hence further material removal occurs. For maximum improvement in surface finish, the pressure should be kept low, number of cycles should be moderate and the magnetic field strength should be kept low. For the following values of independent variables maximum improvement in surface finish is observed.

## 6.7.1 Material removal (MR)

The optimum MR mean is calculated as in eq. (2)

μ = N2 +P2 +C3  -2T 					       (2)

T= mean (overall) = 5.04 mg

N2 = second level of no. of cycle MR = 6.19mg

P2 = second level of Pressure MR = 6.16mg

C3 = third CNT level MR = 6.11 mg

Substituting these values, Mean MR = 8.38 mg

The confidence interval of confirmation experiments (ci) is found by eq. (3)

cice= fa 1, Feve 1Neff+1r  								       (3)

where

Fe = DOF = 20

r = size of sample = 3

ve = variance value = 0.74

Neff= =3.86

CICE = ± 1.24

CIPOP = ± 0.67

## 6.7.2 Confirmation Experiments

To obtain maximum MR, the optimum process parameters levels of are N2P2C3,whereas for the maximum % improvement surface roughness the optimal parameters settings are N3P1C3. The optimum response values based on confirmation experiments is given in table 6.21.

P1 = Extrusion Pressure at first level =13 MPa

P2 = Extrusion Pressure at second level =23 MPa

N2 = first level extrusion cycles =6

N3 = first level extrusion cycles =8

Table 6.21 Optimum values, ci and confirmation experiments

| Output Response | Optimum value | Predicted Value | CI 95% | Confirmation Exp |
| --- | --- | --- | --- | --- |
| MR | N2P2C3 | 8.38mg | CICE 7.26:<MR<9.50 CIPOP:7.71<MR<9.05 | 8.7 mg |
| %Improvement ∆Ra | N3P1C3 | 28.51 % | CICE:26.67<%ΔRa<30.35 CIPOP:27.3<%ΔRa<29.72 | 29.40% |

6.8 Surface Roughness Calculation

The abrasive flow machining was done on brass workpieces, initial weight and roughness and final was measured and the material removal and roughness improvement was analysed. Measurement involved assigning quantitative values to the parameters of weight and surface roughness of all the 130 pieces procured as explained earlier. The measurements will be later used for the sampling process. Figure 6.19 to 6.23 represents profile curve, R and W motifs, Rk, distance and step height measurements respectively.

Figure 6.19 Profile curve

The surface roughness of workpiece is measured  in which small diamond knobe  is made to pass through the hollow workpiece and made to touch the surface at different point both along its length as well as its diametral periphery. In figure 6.19 the profile curve has been obtained. The roughness value varies from -9 µm to 13 µm in the vertical direction whereas it varies from 0 to 3.8 mm on horizontal  axis.

Figure 6.20 R and  W motifs

R and W motifs is a portion of primary profile between highest points of two local peaks. In figure 6.20 this difference or the value of motifs is = 13.5-(-7)  = 20.5 mm.

Figure 6.21 Rk calculation profiles

Figure 6.22 Distance measurement

Figure 6.23 Step height measurement

- (b)

(c)                                                                              (d)

Figure 6.24 (a) Abbot firestone curve, (b) Interactive abbot curve, (c) Fractal analysis, (d) R and  W motifs

The stylus Rk parameter is derived from bearing ratio curve. It is the reduced peak height along (x,y) calculated from measurement of peak height above the roughness value. In figure 6.21, the curve generated varies along  x-axis having value ranging from 0.8 to 3.2 mm whereas its y component holds negative value throughout ranging from minimum 0 µm to -5.9 µm. As it is clear from the figure 6.22 showing distance measurement plot having two vertical interfaces at 1.6 and 2.4 mm. The horizontal distance 0.8 mm whereas vertical distance is 4.67 µm. The curve obtained has x-axis value ranging from 0 to 3.8 mm and vertical value ranging from minimum value of -8 µm to 11 µm.  The step height measurement has been done to get accurate surface integrity values of the inner walls of the workpiece. As clear from figure 6.23 the constant parameters taken are maximum depth, mean depth and width at five different locations. It has been obtained by the method of chromatic confocal that measure step height from 60 nm to 20 mm. The depth can be measured with range greater than 7 µm. The main concentration area lies between 1.9 mm to 3 mm. The minimum and maximum depth is 5.85 µm and 14.5 µm respectively whereas minimum and maximum width is 0.036 mm and 1.09 mm respectively. In figure 6.24 (a), (b), (c), (d) abbot firestone curve, interactive abbot curve, fractal analysis, R and  W motifs curves are shown respectively.

6.9 GRA and MPCI Output Results

In this section the results in terms of MR and Ra and the ranking of input parameters combination based on the best results is done according to fuzzy logic MPCI and GRA concepts. In table 6.22 the ranking is done based on MPCI technique and the input parameters taken are (a) MV, EV, RS, (b) MS, EP, RS, (c) EP, NC, WT, (d) AT, AM, AR, (e) EV, ER, ES respectively. The parameters details are given in table 6.27.

Table 6.22 Output results corresponding different parameters combination

| MV, EV and RS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ra | Normalised |  | MR |  |  | Normalised |  |  | MPCI |  |  |  | Rank |
| 20.37 | 0.09 |  | 4.2 |  |  | 0.00 |  |  | 0.06658 |  |  |  | 9 |
| 16.4 | 0.00 |  | 10.8 |  |  | 0.43 |  |  | 0.25 |  |  |  | 8 |
| 50.8 | 0.75 |  | 12.4 |  |  | 0.53 |  |  | 0.55 |  |  |  | 3 |
| 30.3 | 0.30 |  | 14.4 |  |  | 0.66 |  |  | 0.4271 |  |  |  | 6 |
| 38.1 | 0.47 |  | 19.6 |  |  | 1.00 |  |  | 0.65 |  |  |  | 1 |
| 62.4 | 1.00 |  | 10.2 |  |  | 0.39 |  |  | 0.6415 |  |  |  | 2 |
| 36.5 | 0.44 |  | 7.2 |  |  | 0.19 |  |  | 0.315 |  |  |  | 7 |
| 50.4 | 0.74 |  | 8.2 |  |  | 0.26 |  |  | 0.45 |  |  |  | 5 |
| 53.9 | 0.82 |  | 9.8 |  |  | 0.36 |  |  | 0.5484 |  |  |  | 4 |
| MS, EP and RS |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 8.37 |  | 0.07 |  | 3.7 |  |  | 0.00 |  |  | 0.0655 |  | 9 |  |
| 6.8 |  | 0.00 |  | 6.5 |  |  | 0.45 |  |  | 0.25 |  | 8 |  |
| 23.1 |  | 0.74 |  | 6.9 |  |  | 0.52 |  |  | 0.5443 |  | 2 |  |
| 11.33 |  | 0.21 |  | 8.1 |  |  | 0.71 |  |  | 0.4157 |  | 6 |  |
| 12.45 |  | 0.26 |  | 9.9 |  |  | 1.00 |  |  | 0.5557 |  | 1 |  |
| 16.1 |  | 0.42 |  | 6.5 |  |  | 0.45 |  |  | 0.45 |  | 4 |  |
| 28.89 |  | 1.00 |  | 4.7 |  |  | 0.16 |  |  | 0.4958 |  | 3 |  |
| 15.09 |  | 0.38 |  | 5 |  |  | 0.21 |  |  | 0.3181 |  | 7 |  |
| 22.19 |  | 0.70 |  | 5.5 |  |  | 0.29 |  |  | 0.445 |  | 5 |  |
| EP (1), NC (2) and WT (3) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 23.4 | 0.70 |  | 4.1 |  |  | 0.28 |  |  | 0.4403 |  |  |  | 6 |
| 16.9 | 0.41 |  | 4.13 |  |  | 0.29 |  |  | 0.3729 |  |  |  | 7 |
| 29.9 | 1.00 |  | 3.16 |  |  | 0.14 |  |  | 0.4819 |  |  |  | 4 |
| 17.01 | 0.41 |  | 5.14 |  |  | 0.44 |  |  | 0.45 |  |  |  | 5 |
| 13.69 | 0.26 |  | 8.95 |  |  | 1.00 |  |  | 0.5557 |  |  |  | 2 |
| 12.98 | 0.23 |  | 7.93 |  |  | 0.85 |  |  | 0.4955 |  |  |  | 3 |
| 24.91 | 0.77 |  | 6.01 |  |  | 0.57 |  |  | 0.5613 |  |  |  | 1 |
| 7.9 | 0.00 |  | 5.19 |  |  | 0.44 |  |  | 0.25 |  |  |  | 8 |
| 9.99 | 0.10 |  | 2.19 |  |  | 0.00 |  |  | 0.06718 |  |  |  | 9 |
| AT (1), AM(2) and AR (3) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 23.01 | 0.716 |  |  |  | 4.1 |  |  | 0.28 |  |  | 0.4482 |  | 6 |
| 15.4 | 0.355 |  |  |  | 4.13 |  |  | 0.29 |  |  | 0.3496 |  | 7 |
| 29 | 1 |  |  |  | 3.16 |  |  | 0.14 |  |  | 0.4819 |  | 3 |
| 17.8 | 0.469 |  |  |  | 5.14 |  |  | 0.44 |  |  | 0.45 |  | 5 |
| 13.33 | 0.257 |  |  |  | 8.95 |  |  | 1.00 |  |  | 0.554 |  | 1 |
| 12.1 | 0.199 |  |  |  | 7.93 |  |  | 0.85 |  |  | 0.479 |  | 4 |
| 24 | 0.763 |  |  |  | 6.01 |  |  | 0.57 |  |  | 0.5 |  | 2 |
| 7.9 | 0 |  |  |  | 5.19 |  |  | 0.44 |  |  | 0.25 |  | 8 |
| 9.9 | 0.094 |  |  |  | 2.19 |  |  | 0.00 |  |  | 0.067 |  | 9 |
| EV (1), ER (2) and ES (2) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 10.37 | 0.068 |  |  |  | 4.1 |  |  | 0.28 |  |  | 0.1989 |  | 9 |
| 8.8 | 0 |  |  |  | 4.13 |  |  | 0.29 |  |  | 0.2037 |  | 8 |
| 25.7 | 0.7322 |  |  |  | 3.16 |  |  | 0.14 |  |  | 0.3779 |  | 5 |
| 14.43 | 0.244 |  |  |  | 5.14 |  |  | 0.44 |  |  | 0.3466 |  | 6 |
| 15.57 | 0.2933 |  |  |  | 8.95 |  |  | 1.00 |  |  | 0.5748 |  | 3 |
| 19.02 | 0.443 |  |  |  | 7.93 |  |  | 0.85 |  |  | 0.6109 |  | 2 |
| 31.88 | 1 |  |  |  | 6.01 |  |  | 0.57 |  |  | 0.65 |  | 1 |
| 18.09 | 0.4025 |  |  |  | 5.19 |  |  | 0.44 |  |  | 0.45 |  | 4 |
| 25.2 | 0.7106 |  |  |  | 2.19 |  |  | 0.00 |  |  | 0.3274 |  | 7 |
| MT (1), MV (2) and ET(3) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 9.11 | 0.10 |  | 2.2 |  |  | 0.00 |  |  | 0.06718 |  |  |  | 9 |
| 7.01 | 0.00 |  | 5.2 |  |  | 0.51 |  |  | 0.25 |  |  |  | 8 |
| 24.17 | 0.78 |  | 6 |  |  | 0.65 |  |  | 0.6135 |  |  |  | 1 |
| 12 | 0.23 |  | 7.04 |  |  | 0.82 |  |  | 0.4756 |  |  |  | 6 |
| 13.47 | 0.29 |  | 8.09 |  |  | 1.00 |  |  | 0.5729 |  |  |  | 2 |
| 17.9 | 0.49 |  | 5.99 |  |  | 0.64 |  |  | 0.4819 |  |  |  | 5 |
| 29.1 | 1.00 |  | 3.79 |  |  | 0.27 |  |  | 0.5613 |  |  |  | 3 |
| 16.9 | 0.45 |  | 4.04 |  |  | 0.31 |  |  | 0.385 |  |  |  | 7 |
| 23.2 | 0.73 |  | 4.9 |  |  | 0.46 |  |  | 0.5387 |  |  |  | 4 |

The figure 6.25 shows the matlab fuzzy logic operator details.

Figure 6.25(a) MPCI fuzzy controller, (b) scope display

In table 6.23 different parameters combination based results are tabulated and their deviation and GRC values are shown for both Ra and MR. Here grey relational analysis optimization is done to get best output response.

Table 6.23 GRC based output results corresponding different combination of parameters

| MV, EV and RS |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Ra | Normalised | Deviation | GRC | MR | Normalised | Deviation | GRC |  |
| 20.37 | 0.09 | 0.81 | 0.3817 | 4.2 | 0.00 | 1.00 | 0.3333 |  |
| 16.4 | 0.00 | 1.00 | 0.3333 | 10.8 | 0.43 | 0.57 | 0.4673 |  |
| 50.8 | 0.75 | 0.25 | 0.6666 | 12.4 | 0.53 | 0.47 | 0.5155 |  |
| 30.3 | 0.30 | 0.70 | 0.4166 | 14.4 | 0.66 | 0.34 | 0.5952 |  |
| 38.1 | 0.47 | 0.53 | 0.4854 | 19.6 | 1.00 | 0.00 | 1.0000 |  |
| 62.4 | 1.00 | 0.00 | 1.0000 | 10.2 | 0.39 | 0.61 | 0.4505 |  |
| 36.5 | 0.44 | 0.56 | 0.4717 | 7.2 | 0.19 | 0.81 | 0.3817 |  |
| 50.4 | 0.74 | 0.36 | 0.5814 | 8.2 | 0.26 | 0.74 | 0.4032 |  |
| 53.9 | 0.82 | 0.28 | 0.6410 | 9.8 | 0.36 | 0.64 | 0.4386 |  |
| MV, EV and RS |  |  |  |  |  |  |  |
| 8.37 | 0.07 | 0.93 | 0.347 | 3.7 | 0.00 | 1.00 | 0.333 |
| 6.8 | 0.00 | 1.00 | 0.333 | 6.5 | 0.45 | 0.55 | 0.476 |
| 23.1 | 0.74 | 0.26 | 0.658 | 6.9 | 0.52 | 0.48 | 0.510 |
| 11.33 | 0.21 | 0.79 | 0.388 | 8.1 | 0.71 | 0.29 | 0.633 |
| 12.45 | 0.26 | 0.74 | 0.403 | 9.9 | 1.00 | 0.00 | 1.000 |
| 16.1 | 0.42 | 0.58 | 0.463 | 6.5 | 0.45 | 0.55 | 0.476 |
| 28.89 | 1.00 | 0.00 | 1.000 | 4.7 | 0.16 | 0.84 | 0.373 |
| 15.09 | 0.38 | 0.62 | 0.446 | 5 | 0.21 | 0.79 | 0.388 |
| 22.19 | 0.70 | 0.30 | 0.625 | 5.5 | 0.29 | 0.71 | 0.413 |
| MV, EV and RS |  |  |  |  |  |  |  |
| 23.4 | 0.70 | 0.30 | 0.625 | 4.1 | 0.28 | 0.72 | 0.409 |
| 16.9 | 0.41 | 0.59 | 0.458 | 4.13 | 0.29 | 0.71 | 0.413 |
| 29.9 | 1.00 | 0.00 | 1 | 3.16 | 0.14 | 0.86 | 0.367 |
| 17.01 | 0.41 | 0.59 | 0.458 | 5.14 | 0.44 | 0.56 | 0.471 |
| 13.69 | 0.26 | 0.74 | 0.403 | 8.95 | 1.00 | 0.00 | 1 |
| 12.98 | 0.23 | 0.77 | 0.393 | 7.93 | 0.85 | 0.15 | 0.769 |
| 24.91 | 0.77 | 0.23 | 0.684 | 6.01 | 0.57 | 0.43 | 0.537 |
| 7.9 | 0.00 | 1.00 | 0.333 | 5.19 | 0.44 | 0.56 | 0.471 |
| 9.99 | 0.10 | 0.90 | 0.357 | 2.19 | 0.00 | 1.00 | 0.333 |
| MV, EV and RS |  |  |  |  |  |  |  |
| 23.01 | 0.72 | 0.28 | 0.641 | 4.1 | 0.28 | 0.72 | 0.409 |
| 15.4 | 0.36 | 0.64 | 0.438 | 4.13 | 0.29 | 0.71 | 0.413 |
| 29 | 1 | 0 | 1 | 3.16 | 0.14 | 0.86 | 0.367 |
| 17.8 | 0.47 | 0.53 | 0.485 | 5.14 | 0.44 | 0.56 | 0.471 |
| 13.33 | 0.26 | 0.74 | 0.403 | 8.95 | 1.00 | 0.00 | 1 |
| 12.1 | 0.19 | 0.81 | 0.381 | 7.93 | 0.85 | 0.15 | 0.769 |
| 24 | 0.76 | 0.34 | 0.595 | 6.01 | 0.57 | 0.43 | 0.537 |
| 7.9 | 0 | 1 | 0.333 | 5.19 | 0.44 | 0.56 | 0.471 |
| 9.9 | 0.09 | 0.91 | 0.354 | 2.19 | 0.00 | 1.00 | 0.333 |
| MV, EV and RS |  |  |  |  |  |  |  |
| 10.37 | 0.06 | 0.94 | 0.94 | 4.1 | 0.28 | 0.72 | 0.409 |
| 8.8 | 0 | 1 | 1 | 4.13 | 0.29 | 0.71 | 0.413 |
| 25.7 | 0.73 | 0.27 | 0.27 | 3.16 | 0.14 | 0.86 | 0.367 |
| 14.43 | 0.24 | 0.76 | 0.76 | 5.14 | 0.44 | 0.56 | 0.471 |
| 15.57 | 0.29 | 0.71 | 0.71 | 8.95 | 1.00 | 0.00 | 1 |
| 19.02 | 0.44 | 0.56 | 0.56 | 7.93 | 0.85 | 0.15 | 0.769 |
| 31.88 | 1 | 0 | 0 | 6.01 | 0.57 | 0.43 | 0.537 |
| 18.09 | 0.40 | 0.60 | 0.6 | 5.19 | 0.44 | 0.56 | 0.471 |
| 25.2 | 0.71 | 0.29 | 0.29 | 2.19 | 0.00 | 1.00 | 0.333 |
| MV, EV and RS |  |  |  |  |  |  |  |
| 9.11 | 0.10 | 0.90 | 0.357 | 2.2 | 0.00 | 1.00 | 0.333 |
| 7.01 | 0.00 | 1.00 | 0.333 | 5.2 | 0.51 | 0.49 | 0.505 |
| 24.17 | 0.78 | 0.32 | 0.609 | 6 | 0.65 | 0.35 | 0.588 |
| 12 | 0.23 | 0.77 | 0.393 | 7.04 | 0.82 | 0.18 | 0.735 |
| 13.47 | 0.29 | 0.71 | 0.413 | 8.09 | 1.00 | 0.00 | 1 |
| 17.9 | 0.49 | 0.51 | 0.495 | 5.99 | 0.64 | 0.36 | 0.581 |
| 29.1 | 1.00 | 0.00 | 1 | 3.79 | 0.27 | 0.73 | 0.406 |
| 16.9 | 0.45 | 0.55 | 0.476 | 4.04 | 0.31 | 0.69 | 0.420 |
| 23.2 | 0.73 | 0.27 | 0.649 | 4.9 | 0.46 | 0.54 | 0.480 |

The table 6.24 gives the values of parameters and their levels taken.

Table 6.24. Parameters and their level values

| Symbol | Process Parameters | Unit | Level 1 | Level 2 | Level 3 |
| --- | --- | --- | --- | --- | --- |
| MV | Magnetic Voltage | V | 50 | 125 | 200 |
| ER | ECM Rod size | mm | 4 | 6 | 8 |
| EV | ECM Voltage | V | 6 | 12 | 18 |

The figure 6.26 (a), (b), (c) gives the details of time series plot, SN ratio main effects and matrix plot of parameters respectively.

Figure 6.26(a) Time series, (b) SN ratio data, (c) matrix plot

The orthogonal array L9 table is given below in table 6.25.

Table 6.25 The L9 (34) OA parameters and response

| Exp no. | Run order | Parameter conditions |  |  | Response output |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | MV | ER | EV | R1 | R2 | R3 |
|  |  | 1 | 2 | 3 |  |  |  |
| 1 | 1 | 1(50) | 1(4) | 1(6) | 0.17 | 0.18 | 0.17 |
| 2 | 4 | 1(50) | 2(6) | 2(12) | 2.44 | 1.94 | 1.77 |
| 3 | 7 | 1(50) | 3(8) | 3(18) | 3.33 | 3.67 | 4.54 |
| 4 | 5 | 2(125) | 1(4) | 2(12) | 0.45 | 0.54 | 0.26 |
| 5 | 8 | 2(125) | 2(6) | 3(18) | 2.9 | 2.77 | 2.53 |
| 6 | 2 | 2(125) | 3(8) | 1(6) | 1.36 | 1.81 | 1.49 |
| 7 | 9 | 3(200) | 1(4) | 3(18) | 0.65 | 0.71 | 0.63 |
| 8 | 3 | 3(200) | 2(6) | 1(6) | 1.39 | 1.46 | 1.53 |
| 9 | 6 | 3(200) | 3(8) | 2(12) | 5 | 6.57 | 6.96 |

In table 6.26 the Ra and MR results corresponding to three input parameters are tabulated.

Table 6.26 Output results corresponding to input parameters

| Variable parameters | AT (1), AM(2) and AR (3) |  | EP (1), NC (2) and WT (3) |  | MV (1), EV (2) and RS(3) |  |
| --- | --- | --- | --- | --- | --- | --- |
| Exp. Run | % imp. In Ra | MR (gm) | % imp. In Ra | MR (gm) | % imp. In Ra | MR (gm) |
| 1(111) | 23.01 | 4.8 | 23.4 | 4.1 | 20.37 | 4.2 |
| 2(122) | 15.4 | 4.03 | 16.9 | 4.13 | 16.4 | 10.8 |
| 3(133) | 29 | 3.86 | 29.9 | 3.16 | 50.8 | 12.4 |
| 4(212) | 17.8 | 5.64 | 17.01 | 5.14 | 30.3 | 14.4 |
| 5(223) | 13.33 | 8.19 | 13.69 | 8.95 | 38.1 | 19.6 |
| 6(231) | 12.1 | 7.14 | 12.98 | 7.93 | 62.4 | 10.2 |
| 7(313) | 24 | 6.1 | 24.91 | 6.01 | 36.5 | 7.2 |
| 8(321) | 7.9 | 5.5 | 7.9 | 5.19 | 50.4 | 8.2 |
| 9(332) | 9.9 | 9.5 | 9.99 | 2.19 | 53.9 | 9.8 |
| Average | 16.93 | 6.08 | 17.40 | 5.2 | 39.90 | 10.75 |
| Variable Parameters | MF (1), RS (2) and EP (3) |  | EV (1), ER (2) and ES (2) |  | MT (1), MV (2) and ET(3) |  |
| Exp. Run | % imp. in Ra | MR (gm) | % imp. In Ra | MR (gm) | % imp. In Ra | MR (gm) |
| 1(111) | 8.37 | 3.7 | 10.37 | 2.1 | 9.11 | 2.2 |
| 2(122) | 6.8 | 6.5 | 8.8 | 5.4 | 7.01 | 5.2 |
| 3(133) | 23.1 | 6.9 | 25.7 | 6.2 | 24.17 | 6 |
| 4(212) | 11.33 | 8.1 | 14.43 | 7.2 | 12 | 7.04 |
| 5(223) | 12.45 | 9.9 | 15.57 | 8.8 | 13.47 | 8.09 |
| 6(231) | 16.1 | 6.5 | 19.02 | 5.1 | 17.9 | 5.99 |
| 7(313) | 28.89 | 4.7 | 31.88 | 3.8 | 29.1 | 3.79 |
| 8(321) | 15.09 | 5 | 18.09 | 4.1 | 16.9 | 4.04 |
| 9(332) | 22.19 | 5.5 | 25.2 | 4.9 | 23.2 | 4.9 |
| Average | 16.03 | 6.31 | 18.78 | 5.28 | 16.98 | 5.25 |

Table 6.26 Input parameters and their levels and units

| S.No. | Symbol | Prameters | Unit | Level-1 | Level-2 | Level-3 |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | MF | Magnetic flux | Tesla | 0.5 | 1.0 | 1.5 |
| 2 | RS | Rotation speed | RPM | 100 | 150 | 200 |
| 3 | EP | Extrusion pressure | Bar | 15 | 30 | 45 |
| 4 | EV | ECM voltage | V | 6 | 12 | 18 |
| 5 | ER | ECM rod size | mm | 4 | 6 | 8 |
| 6 | ES | ECM rod shape | - | Round | Square | Drill-bit |
| 7 | MT | Media type | - | Natural | SBR | Nitrile |
| 8 | MV | Media volume | cm3 | 200 | 225 | 250 |
| 9 | ET | Electrolyte | - | NaCl | HNO3 | CaCl2 |
| 10 | AT | Abrasive type | - | Al2O3 | SiC | Al2O3+SiC |
| 11 | AM | Abrasive mesh size | # | 100 | 200 | 300 |
| 12 | AR | Abrasive ratio | - | 1:2 | 1:1 | 2:1 |
| 13 | NC | Number of cycles | No.’s | 3 | 6 | 9 |
| 14 | WT | Workpiece type | - | Brass | Aluminium | Mild Steel |
| 15 | MV | Magnetic voltage | V | 50 | 125 | 200 |

6.10 Characterization of Polymer Media

The prepared media is characterized using fourier transmission infra red microscopy technique alonwith scanning and transmission electron microscope images so as to understand the characteristics of the media and its suitability in AFM process. The TEM, SEM, and FTIR image and graphs are shown in figure 6.27 (a), (b) and (c) respectively. Figure 6.27(a) shows TEM images of iron filed CNTs, taken at 50 nm scale. It is clear from the micrograph that there is negligible amount of impurities such as carbon particles, soot and amorphous carbon, and CNTs seem to be growing at uniform rate. The prepared media resulted in improvement of conductivity upto 35% , hence material removal will be increased.

- (b)   				    (c)

Figure 6.27 (a) TEM image of CNTs, (b) SEM image of media, (c) FTIR graph of the media

FTIR/TGA analysis stands for fourier transform infrared spectroscopy/ thermogravity analysis. As depicted in figure 6.27(c), the FTIR output image results are shown, having transmittance (absorbance) on y-axis and wavenumber (cm-1) on x-axis.

Figure 6.28 FTIR image of the developed Nitrile rubber media

The figure 6.28 clearly shows the FTIR image of nitrile polymer media i.e. transmittance vs wavenumber plot. When the prepared sample of polymer media is installed on the FTIR/TGA apparatus, the infrared light falls on sample and the spectrum i.e. transmittance shows fingerprint which gives performance and quality of polymer sample media. As shown in figure 6.27, % transmittance varied from 0 to 100, whereas wavenumber decreased from 4000 to 500. The FTIR image or graph can be understood by dividing the whole region of the graph into different zones.

6.10.1 X-Ray Diffraction Methods and Images

The X-Ray Diffraction (XRD) method is used for the phase confirmation of the component whose XRD is to be done. In the XRD machine, the light comes from the source, which falls on the component, then ultimately deflects at an angle 2θ and ultimately falls on the detector plate. The principle of operation is thermionic emission. In case of crystalline material, good peaks are observed in XRD images as shown in figure 6.29. X-Ray diffraction is used to find density f(r) of electrons where are is position vector

f(r) = 403.22×10-3 f.expi.p.rdp

The length of p is around the circle 2π divided by wavelength. The Bragg formula of diffraction is used so that reflection is indexed with the help of miller indices i.e. reciprocal vector component of lattice.

- (b)

Figure 6.30 X-Ray Diffraction image of  (a) Nitrile Rubber, (b) SBR

6.10.1.1 Explanation of XRD Image Output Results

Basically XRD is used to find the crystal atomic structure with the help of X-Ray beam to diffract into different directions and by measuring the angle we can find 3-D picture of electro density, as shown in figure 6.30. In Brucker XRD machine as shown in figure 6.31, its different components i.e. light source, controller and detector are clearly mentioned. The machine is installed in precision engineering laboratory in an automation environment two quality and process control XRD and X-Ray fluorescence analysis (XRFA). The integration of machine production line is used to effectively optimize the process. Different softwares are used for analysis of these images such as High Score, Origin and Xpertise, etc. Figure 5 shows Bruker X-Ray Diffraction Machine (D-8 Advance).

6.10.1.2 Procedure of Polymer Media Analysis on Brucker Machine

Thin polymer film is prepared on glass slides and Si/SiO2 substrates by spin coating. Since it is a polymer therefore it has semi-crystalline and amorphous structure, our XRD analysis was used to assess phases i.e. polymorphism and poly types. During AFM process the prepared polymer media was extruded and molded through cylinders and after completion of machining process of inside walls of brass workpiece, the orientation of molecules was analyzed using diffraction technique. The inter space distance is given in equation (1).

d = λ2sinθ   = 0.1542sin⁡(22) = 2.01×10-7 mm 							       (1)

dh,k,l = a1h2  +k2  +l2   = 2.01×10-7 mm

The structure of our in-house prepared polymer media is face centered cubic (FCC) structure, the units cell width and atomic radius relationship is as follows in equation (2).

a = 2r2 (geometry) 										       (2)

r = 1.28 × 10-7 mm

Therefore a = 3.61 × 10-7 mm

h2  +k2  +l2  = adh,k,l

= 3.61 × 10-72.01×10-7

= 1.729 mm

h2  +k2  +l2  = 3.0

FCC primary diffraction planes are those planes whose indices are all even or all odd (e, o, (111), (200), (220)). If h = k = l = 1, it is close packed plane (CCP) i.e. hexagonal structure.

Controllers

Light source

2θ angle

Detector

Figure 6.31 Bruker X-Ray Diffraction Machine (D-8 Advance)

    - Prepared Media FTIR/TGA Image Discussion and Analysis

FTIR/TGA analysis stands for fourier transform infrared spectroscopy/ thermogravity analysis. As depicted in figure 6.29, the FTIR output image results are shown, having transmittance (absorbance) on y-axis and wavenumber (cm-1) on x-axis. The figure 6.29 clearly shows the FTIR image of nitrile polymer media i.e. transmittance vs wavenumber plot. When the prepared sample of polymer media is installed on the FTIR/TGA apparatus, the infrared light falls on sample and the spectrum i.e. transmittance shows fingerprint which gives performance and quality of polymer sample media. As shown in fig.6, % transmittance varied from 0 to 100, whereas wavenumber decreased from 4000 to 500. The FTIR image or graph can be understood by dividing the whole region of the graph into different zones. The left zone has peaks ranging from 3852.8 to 2958.8, but the inter space distance between these peaks is large. The middle zone ranges from value 2922.7 to 1736.6, whereas the right most zone has comparatively large number of peaks having very small interspacing, the value changing from 1639.1 to 911.4, the significance of the different peaks denoting  alcoholic, ether, ketonic groups etc. After thorough analysis it was found that the utilized media was successful in machining implementation and it was observed that it was qualitatively improved media.

Summary

- The effect of process parameters on output response MR and Ra was analysed.

- The results of matlab fuzzy logic and grey relational analysis optimization were analysed and compared with those of Taguchi based experimental results.

- Further characterization of prepared polymer media was done and analysed.

CHAPTER 7: CONCLUSIONS AND FUTURE SCOPE OF WORK

This chapter describes the conclusions obtained from the experimental investigation of EMR-AFM process and the mathematical model developed. The output results have been explained in brief and the scope of future work is discussed.

7.1 Conclusions

- The electrochemical and electromagnetic setup was employed successfully to make the traditional AFM setup hybrid in nature in order to improve the efficiency of the process. A machine setup alongwith electromagnet, media have been developed and characterized using FTIR and XRD analysis.

- The SBR media resulted in maximum material removal during experimentation, i.e., 3.88 mg when input parameters, i.e., electrolytic voltage, number of extrusion cycles and pressure were taken as 18 V, 4 and 10 bar respectively. The NR, NTR and SR media had intermediate effect of material removal but minimum removal of material was achieved in case of PBS media, i.e., 2.39 mg at 6 V voltage, 6 number of cycles and 30 bar pressure.

- The material removal was first increased with higher rod size but afterwards its increase was lesser. The surface plots obtained from RSM technique showed that MR obtained was 2.25 mg at 21 bar pressure and 7 number of cycles. As compared to conventional AFM setup, it was found that in EMR-AFM setup, 34.5 % and 17.8 % improvement in % Ra and material removal, respectively, was obtained. It was found that MR was approximately 2.9 mg on an average when machining was done on traditional AFM process, while it increased upto 4.5 mg in prepared hybrid machine setup.

- Both mathematical and computational modeling has been done successfully. The magnetic flux and voltage calculations and electrochemical action has been explained alongwith time derivatives of magnetic field using Maxwell equations. The flux φ of magnetic field was found to be 300 G/A, magnetic field equal to 10 Gauss and angular momentum of iron particle due to rotation provided by motor was found to be 0.75 rad/s.

- Analysis of media flow both mathematically by calculating different forces that are shown by drawing a model and by using SolidWorks software, the flow was analysed using computational flow dynamics.

- The different optimization techniques i.e. Taguchi L9 OA, RSM, Minitab fuzzy logic and grey relational analysis were employed and implemented to validate the results obtained from the hybrid machine setup experimentation. The objective of maximum material removal and minimum surface roughness was fulfilled consequently.

- The effect of different parameters viz. finishing cycles, different media, etc. on surface roughness improvement have been explained graphically in detail. It was found that 40 % more reduction in surface roughness was achieved in 20 % lesser number of cycles in hybrid EMR-AFM setup.

- Experiments were carried out for evaluating performance of newly developed media(carrier+Al2O3+CNTs) using the double acting, vertical type AFM setup to study its performance in terms of the improvement in material removal and surface finish of “cast iron” work pieces. It has been found that the use of CNTs with media led to an improvement in the response parameter of percentage improvement in surface finish and material removal.

- At selected parameters a maximum improvement of 8.38mg and 28.51% has been observed in the material removal and surface finish on the inner cylindrical surface of the cast iron work piece.

## Scope of Future Work

- CNTs filled with Fe, Co and Ni which is ferromagnetic in nature can be explored in MAFM for better result.

- Results can be analyzed for different industrial material.

- The set up can be optimized for many other process parameters like different shapes of work materials, different abrasives, flow rate of media etc.

References

- Amineh S.K, Tehrani A.F., Mohammadi A., Improving the surface quality in wire electrical discharge machined specimens by removing recast layer using magnetic abrasive finishing method, International Journal of Advanced Manufacturing Technology, (2013), 66, pp. 1793-1803.

- Aurich  J.C., Linke, B., Hauschild, M., Carrella, M., Kirsch, B., Sustainability of abrasive processes, CIRP Annals - Manufacturing Technology, (2013), 62, pp.653–672.

- Bahre D., Brunnet H, Swat M, Investigation of one way abrasive flow machining and in-process measurement of axial forces, 5th CIRP Conference on High Performance Cutting, (2012), pp.419-424.

- Barletta, Progress in abrasive fluidized bed machining, Journal of Materials Processing Technology, (2009), 209, pp.6087–6102.

- Brar B.S., Walia R.S., Singh V.P., Electrochemical aided abrasive flow machining (ECA2AFM) process: a hybrid machining process, International Journal of Advanced Manufacturing Technology, (2015), pp.1205-1217.

- Bin W, Wei C, Jin C, Xia C, A new type of nozzle AFM machine tool and control system research, International Conference on Mechatronics and automation, China, (2012) 23, pp.2314-2318.

- Chen K.Y., Cheng K.C., A study of helical passageways applied to polygon holes in abrasive flow machining, Int J Adv Manuf Technol, (2014), 74, pp.781-790.

- Chryssolouris g., Guillot m., Modelling of machining process using neural network, Trans. ASME J. Eng. Ind. , 1990, 112, pp. 122-131.

- Das M., Jain V. K., Ghoshdastidar, P.S., Analysis of magnetorheological abrasive flow finishing (MRAFF) process, Int J Adv Manuf Technol, (2008), 38, pp.613–621.

- Fang, L., Zhao, J., Li, B., Sun K., Movement patterns of ellipsoidal particle in abrasive flow machining, Journal of Materials Processing Technology, (2009), 209, pp.6048–6056.

- Fang, L., Zhao, J., Li, B., Sun K., Zheng D, Ma D., Temperature as sensitive monitor for efficiency of work in abrasive flow machining, Wear, (2009), 266, pp.678-687.

- Ghoshal, B., Bhattacharyya B., Investigation on profile of microchannel generated by electrochemical micromachining, Journal of Materials Processing Technology, (2015), 222, pp.410–421.

- Givi M, Tehrani A.F., Mohammadi A, Polishing of aluminium sheets with magnetic abrasive finishing method, Int J Adv Manuf Technol, (2012), 61, pp. 989-998.

- Gorana V.K., Jain V.K., Lal G.K., Forces prediction during material deformation in abrasive flow machining, Wear, (2006),  260, pp.128–139.

- Ibrahim A.F., Shather S.K., Hamdan W.K., Studying abrasive flow machining conditions by using Taguchi method, Engineering & Technology Journal, (2014), 32, pp. 1071-1082.

- Jahan M.P., Rahman M., Wong Y.S., A review on the conventional and micro-electrodischarge machining of tungsten carbide, International Journal of Machine Tools & Manufacture, (2011), 51, pp.837–858.

- Jain V. K., Abrasive-based nano-finishing techniques: an overview, Machining Science and Technology, An International Journal, (2008), 12(3), pp. 257-294.

- Jain R. K. and Jain V. K, Optimum selection of machining conditions in abrasive flow machining using neural networks”, Journal of Materials Processing Technology, 2000, 108, pp.62-67.

- Jain N.K., Jain V.K., Modeling of material removal in mechanical type advanced machining processes: a state-of-art review. International Journal of Machine Tools & Manufacture, (2001), 41, pp.1573–1635.

- Jain R.K., Jain V.K., Specific energy and temperature determination in abrasive flow machining process, International Journal of machine tools and manufacture, (2001), 41, pp.1689-1704.

- Jain R.K., Jain V.K., Dixit P.M., Modelling of material removal and surface roughness in abrasive flow machining process, International Journal of Machine Tools and Manufacture, (1999), 39, pp.1903-1923.

- Fang Liang, Zhao Jia, Sun Kun, Zheng Degang, Ma Dexin, Temperature as sensitive monitor for efficiency of work in abrasive flow machining, Wear, (2009), 266, pp. 678–687.

- Jang K.I., Seok J.S., Min B.K., Lee A.J., An electrochemical polishing process using magnetorheological fluid, International journal of machine tools and manufacture, (2010), 50, pp. 869-881.

- Jha S., Jain V.K., Modelling and simulation of surface roughness in magnetorheological abrasive flow finishing (MRAFF) process, Wear, (2006), 261, pp.856-866.

- Jha S., Jain V.K., Rheological characterization of magnetorheological polishing fluid for MRAFF, Int J Adv Manuf Technol, (2009), 42, pp.656-668.

- Jha S., Jain V.K., Komanduri R., Effect of extrusion pressure and number of cycles on surface roughness in magnetorheological abrasive flow finishing process, Int J Adv Manuf Technol, (2007), 33, pp.725-729.

- Jiang B.Y., Lan S.H., Ni J., Modeling and experimental investigation of gas film in micro-electrochemical discharge machining process, International Journal of Machine Tools & Manufacture, (2015), 90, pp.8–15.

- Judal K.B., Yadava V., Modeling and simulation of cylindrical electrochemical magnetic abrasive machining of AISI-420 magnetic steel, Journal of Materials Processing Technology, (2013), 213, pp.2089-2100.

- Jui,S.K., Kamaraj A.B., Sundaram M.M., High aspect ratio micromachining of glass by electrochemical discharge machining, Journal of Manufacturing Processes, (2013), 15, pp.460–466.

- Kala P., Pandey P.M., Comparison of finishing characteristics of two paramagnetic materials using double disc magnetic abrasive finishing, Journal of Manufacturing Processes, (2015), 17, pp.63–77.

- Kar K. K., Ravikumar N.L., Tailor P.B., Ramkumar J., Sathiyamoorthy D., Performance evaluation and rheological characterization of newly developed butyl rubber based media for abrasive flow machining process, Journal of Materials Processing Technology (2009) 209, pp. 2212-2221.

- Kenda J., Duhovnik J., Tavcar J., Kopac J., Abrasive flow machining applied to plastic gear matrix polishing, Int J Adv Manuf Technol, (2014), 71, pp.141-151.

- Kendaa J., Pusaveca F., Kermoucheb G., Kopaca J., Surface Integrity in Abrasive Flow Machining of Hardened Tool Steel AISI D2, 1st CIRP Conference on Surface Integrity (CSI), Procedia Engineering, (2011), 19, pp.172–177.

- Kenda J., Pusavec F., Kopac J., Modeling and Energy Efficiency of Abrasive Flow Machining on Tooling Industry Case Study, 2nd CIRP Conference on Surface Integrity, Procedia CIRP, (2014), 13, pp.13 – 18.

- Kozaka J., Oczos K.E., Selected problems of abrasive hybrid machining, Journal of Materials Processing Technology, (2001), 109, pp. 360-366.

- Kumar P., Tailor B., Agrawal A., Joshi S.S., Evolution of electrochemical finishing processes through cross innovations and modelling, International Journal of Machine Tools & Manufacture, (2013),  66, pp.15–36.

- Kurita T., Hattori M., A study of EDM and ECM/ECM-lapping complex machining technology, International Journal of Machine Tools & Manufacture, (2006), 46, pp.1804–1810.

- Li J., Liu W., Yang L., Li C., Liu, B.  Wu H., Sun X., Design and simulation for micro hole abrasive flow machining, Int J Adv Manuf Technol, (2009), 54, pp.789-796.

- J. Li, W. Liu, L. Yang, C. Tian, S. Zhang, A method of motion control about micro hole abrasive flow machining based on Delphi language, International Conference on Mechatronics and automation, China, (2009), 21: 1444-1448.

- Lin Y.C., & Lee, H.S., Optimization of machining parameters using magnetic-force-assisted EDM based on gray relational analysis, Int J Adv Manuf Technol, (2009),  42, pp.1052–1064.

- Lin C.T., Yang L.D., Chow H.M., Study of magnetic abrasive finishing in free-form surface operations using the Taguchi method, Int J Adv Manuf Technol, (2007), 34, pp.122–130.

- Liua J., Zhua D., Zhaoa L., Yang Z., Experimental Investigation on Electrochemical Machining of TiAl Intermetallic, 15th Machining Innovations Conference for Aerospace Industry, (2012), 45. pp.45-54.

- Mali H.S., Manna A., Optimum selection of abrasive flow machining conditions during fine finishing of Al/15 wt% SiC-MMC using Taguchi method, Int J Adv Manuf Technol ,(2010) ,50, pp.1013-1024.

- Mathew R., Sundaram M.M., Modeling and fabrication of micro tools by pulsed electrochemical machining, Journal of Materials Processing Technology, (2012), 212, pp.1567– 1572.

- Niranjana M.S., Jha S., Flow Behaviour Of Bidisperse MR Polishing Fluid And Ball End MR Finishing, 3rd International Conference on Materials Processing and Characterisation Procedia Materials Science, (2014), 6,pp.798 – 804.

- Paul L., Hiremath S.S., Response surface methodology of micro holes in electrochemical discharge machining process, International Conference on Design and Manufacturing, (2013), 64, pp.1395-1404.

- Paul L., Shekhar S., Hiremath S., Response surface modelling of micro holes in electrochemical discharge machining process, International conference on design and manufacturing, (2013).

- Pengfei H., Chunlin Q., Weidong L., Wenji S., Cleaning Technology of the Steel Tube Based on AFM., (2011).

- Pengfei H., Jiazhi G., A new cleaning technology based on AFM & its industry application, International Conference on Computer Application and System Modeling, (2010).

- Petri K. L., Billuo R. E., Bidando B., A neural network process model for abrasive flow machining operation”, Journal of manufacturing systems, 1998, 17(1).

- Perry W.B., Stackhouse J., Gas turbine applications of abrasive flow machining, The American Society of Mechanical Engineers, (1989), 45, pp.1-8.

- Rhoades L.J., Abrasive Flow Machining, Technical Paper of the Society of Manufacturing Engineers(SME), (1989), pp.89-145 .

- Sankara M., Babu A.G., Effect of reinforcement particles on the abrasive assisted electrochemical machining of Aluminium-Boron carbide-Graphite composite, 12th Global congress on manufacturing and management, Procedia Engineering, (2014), 97, pp.381 – 389.

- Sankar M.L., Ramkumar J., Jain V.K., Experimental investigation and mechanism of material removal in nano finishing of MMCs using abrasive flow finishing (AFF) process. Wear, (2009), 266, pp.688–698.

- Singh Sehijpal, Studies in metal finishing with magnetically assisted abrasive flow machining , Ph.D. Thesis. I IT Roorkee, (2002).

- Sharma A.K., Venkatesh G., Rajesha S., Kumar P., Experimental investigations into ultrasonic assisted abrasive flow machining (UAAFM) process, Int J Adv Manuf Technol (2015) 34, pp. 451-459.

- Shinmura T.  and Aizawa T., Study on magnetic abrasive finishing process, JSPE, 1986, 20(2), pp. 79-84.

- Sidpara, A.; Jain, V.K. Analysis of forces on the free form surface in magnetorheological fluid based finishing process. International Journal of Machine Tools & Manufacture, (2013)  69, pp.1–10.

- Sidpara, A.; Jain, V.K.,Theoretical analysis of forces in magnetorheological fluid based finishing process. International Journal of Mechanical Sciences, (2012)  56, pp.50–59.

- Silva A. K. M. D., Geough J. A. M., Computer applications in unconventional machining, Journal of Materials Processing Technology, 2000, 107, pp.276-282

- Simon T.M., Reitch F., Jolly M.R., Ito K. and Banks H.T., The effective magnetic properties of magnetorheological fluids, International journal of mathematical & computing modelling, 2001, 33, pp 273-284.

- Singh, A.K.; Jha, S.; Pandey, P.M., Nanofinishing of a typical 3D  ferromagnetic workpiece using ball end magnetorheological finishing process. International Journal of Machine Tools & Manufacture, (2012) 63, pp 21–31

- Singh D.K.; Jain, V.K.; Raghuram, V. Experimental investigations into forces acting during a magnetic abrasive finishing process. Int J Adv Manuf Technol , (2006) ,30, pp.652–662.

- Singh, S.; Shan, H.S. Development of magneto abrasive flow machining process. International Journal of Machine Tools & Manufacture , (2002), 42, pp.953–959

- Swata, M.; Brünneta, H.; Lyubenova, N.; Schmittb, J.; Diebels, S.; Bährea, D., Improved process control and model of axial forces of one-way abrasive flow machining, 6th CIRP International Conference on High Performance Cutting, HPC, Procedia CIRP, (2014)  14 pp.19 – 24.

- Tang B., Ji S., Tan D., Structural surface of mould softness abrasive flow precision polishing machining method based on VOF, International Conference on electrical and control engineering, (2010), 67, pp. 2001-2005

- Taweel, T.A.E., Modelling and analysis of hybrid electrochemical turning magnetic abrasive finishing of 6061 Al/Al2O3 composite. Int J Adv Manuf Technol, (2008), 37, pp.705–714

- Tzeng H.J, Yan B.H., Hsu R.T., Lin Y.C., Self modulating abrasive medium and its application to abrasive flow machining for finishing micro channel surfaces, Int J Adv Manuf Technol, (2007), 3. Pp.1163-1169

- Tzeng H.J., Yan B.H., Hsu R.T, Chow H.M., Finishing effect of abrasive flow machining on micro slit fabricated by wire-EDM, Int J Adv Manuf Technol, (2007), 34, pp. 649-656

- Tzeng, Yan, Hsu and Lin, Self-modulating abrasive medium and its application to abrasive flow machining for finishing micro channel surfaces, International Journal of Advanced Manufacturing Technology, (2007),  32, pp.1163-1169.

- Uhlmann, E.; Doits, M.; Schmiedel, C. Development of a material model for visco-elastic abrasive medium in Abrasive Flow Machining. 14th CIRP Conference on Modeling of Machining Operations (CIRP CMMO), Procedia CIRP, (2013),  8, pp. 351–356.

- Uhlmann, E.; Mihotovic, V; Coenen, A., Modelling the abrasive flow machining process on advanced ceramic materials. Journal of Materials Processing Technology, (2009), 209, pp.6062–6066.

- Uhlmann E., Schmiedel C., Wendler J., CFD simulation of the abrasive flow machining process, Procedia CIRP, 2015, .31, pp. 209-214.

- Venkatesh, G.; Sharma, A.K.; Singh, N., Simulation of media behaviour in vibration assisted abrasive flow machining. Simulation Modelling Practice and Theory, (2015), 51, pp.1–13.

- Venkatesh, G.; Sharmaa, A.K.; Singh, N; Kumar, P., Finishing of Bevel Gears using Abrasive Flow Machining. 12th Global Congress on Manufacturing and Management, GCMM, Procedia Engineering, (2014), 97, pp. 320 – 328.

- Vaishya, R.; Walia, R.S.; Kalra, P., Design and Development of hybrid electrochemical and centrifugal force assisted abrasive flow machining. 4th International Conference on Materials Processing and Characterization, Materials Today, Proceedings, (2015), 2, pp.3327 – 3341.

- Wan S., Ang Y.J., Sato T., Lim G.C., Process modelling and CFD simulation of two-way abrasive flow machining, Int J Adv Manuf Technol, (2014), 71, pp.1077-1086

- Wang A.C., Weng S.H., Developing the polymer abrasive gels in AFM process, Journal of Materials Processing Technology, (2007), 192, pp. 486-490

- Walia R.S., Shan H.S., Kumar P., Determining dynamically active abrasive particles in the media used in centrifugal force assisted abrasive flow machining process, International Journal of Advanced Manufacturing Technology, (2008), 38, pp. 1157-1164

- Wang, C.; Liu, C. H.; Liang, K. Z.; Pai, S. H., Study of the rheological properties and the finishing behavior of abrasive gels in abrasive flow machining. Journal of Mechanical Science and Technology, (2007), 22, pp.1593-1598.

- Wang, A.C.; Tsai, L.; Liang, K.Z., Uniform surface polished method of complex holes in abrasive flow machining. Trans non ferrous met scichina, (2009), 19, pp. 2225-2257.

- Wani A.M., Yadava V., Khatri A., Simulation for the prediction of surface roughness in magnetic abrasive flow finishing (MAFF), Journal of Materials Processing Technology, (2007), 190, pp.282-290

- Williams R. E., Acoustic emission characteristics of abrasive flow machining process, ASME J. Manuf. Sci. Eng., 1998, 20, pp.264-271.

- Williams, R.R.; Melton, V.L., Abrasive flow finishing of stereolithography prototypes. Rapid Prototyping Journal, (1998), 4(2), pp.56 – 87.

- Williams R.E., Walczyk D.F., Dang H.T., Using abrasive flow machining to seal and finish conformal channels in laminated tooling, Rapid prototyping Journal, (1998), 8(4), pp. 255-258

- Yamaguchi H., Srivastava A.K., Tan M.A., Riveros R.E., Hashimoto F., Magnetic abrasive finishing of cutting tools for machining of titanium alloys, CIRP- Annals- Manufacturing Technology, (2012), 61, pp.311-314.

- Yan, B.H.; Wang, C.C.; Lin, Y.C., Feasibility study of rotary electrical discharge machining with ball burnishing for Al2O3/6061Al composite. International Journal of Machine Tools & Manufacture, (2000), 40, pp.1403–1421

- Yan B.H., Chang G.W., Cheng T.J., Hsu R.T., Electrolytic magnetic abrasive finishing. International Journal of Machine Tools & Manufacture, (2003), 43, pp.1355–1366

- Yang Y., Natsub W., Zhao W.S., Realization of eco-friendly electrochemical micromachining using mineral water as an electrolyte. Precision Engineering, (2011), 35, pp.204–213

- Yang S., Sha L., Study on processing effect prediction system of AFM for injector hole of twin flapper nozzle valve, Second International Conference on Enterprise systems, (2014), 42, pp.196-200

- Yang L., Zhao L., The study of polishing and equipment of abrasive flow, Int J Adv Manuf Technol (2007), 56, pp.778-788

- Yoon S, Tu J.F., Lee J.H., Yang G.E., Mun S.D., Effect of magnetic pole arrangement on the surface roughness of STS 304 by magnetic abrasive machining, International Conference of precision engineering and manufacturing, (2014), 15(7), pp. 1275-1281

- Zaborski S., Łupak M., Poro D., Wear of cathode in abrasive electrochemical grinding of hardly machined materials, Journal of Materials Processing Technology, (2004), 149, pp.414–418

- Zhang W., Hao P., Liu, Y.  Dong Z., Research on cleaning technology of steel pipe based on AFM, Int J Adv Manuf Technol ,(2007), 32, pp.1130-1142

- Zhang S., Liu W., Yang L., Zhu C., Li C., Li J., Study On Abrasive Flow Ultra-Precision Polishing Technology of Small Hole, Proceedings of the IEEE, International Conference on Mechatronics and Automation, August 9 - 12, Changchun, China, (2009), 45, pp.4305-4309.

RESEARCH PUBLICATIONS

International Journal

| S.No. | Title of Paper | Name of the authors | Name of the Journal | Indexing status of journals with indexing agency |
| --- | --- | --- | --- | --- |
| 1 | Experimental, Computational and Mathematical Analysis of Hybrid Abrasive Flow Machining Process | Sachin Dhull, R.S. Walia, Q. Murtaza and M.S. Niranjan. | International Journal of Precision Engineering and Manufacturing. (accepted) | Springer (SCI) I.F. 2.2. |
| 2 | Electrochemo-magneto abrasive flow machine setup fabrication and experimental investigation of the process alongwith mathematical modeling and optimization | Sachin Dhull, R.S. Walia, Q. Murtaza, M.S.Niranjan | Independent Journal of Management & Production ISSN: 2236-269X, DOI: 10.14807/ijmp.v10i8.1045. 2019; vol.10, n.8, pp.1834-1849 | Emerging Sources Citation Index (Web of science group clarivate analytics) Inst Federal Educacao, Ciencia & Tecnologia Sao Paulo, Rua Pedro Vicente 625, Caninde, Sao Paulo, Brazil, 01109-010 |
| 3 | Development of Different Polymer Media and Experimental Investigation of Abrasive Flow Machining Process | Sachin Dhull, R.S. Walia, Q. Murtaza, M.S.Niranjan | International Journal of Engineering Research and Technology 2018; 11 (7): 1015-1024. | Scopus indexed International Research Publication House |
| 4 | Modeling and Simulation of AFM Experimentation of Brass Workpiece Using Different Media | Sachin Dhull, R.S. Walia, Q. Murtaza, M.S.Niranjan | International Journal of Latest Engineering and Management Research (IJLEMR) ISSN: 2455-4847 2019; 4 (3): 01-09. | NA |
| 5 | Experimental Investigation of Abrasive Flow Machining Process Alongwith Fuzzy Logic and Grey Relation Analysis | Sachin Dhull, R.S. Walia, Q. Murtaza, M.S.Niranjan | International Journal of Latest Engineering and Management Research (IJLEMR) ISSN: 2455-4847 2019; 4 (3): 01-08. | NA |
| 6 | Experimental Investigation and Preparation of Electromagnets and Their Effect on Surface Roughness in Abrasive Flow Machining Process | Sachin Dhull, R.S. Walia, Q. Murtaza | International Journal of Latest Engineering and Management Research (IJLEMR) ISSN: 2455-4847 2018; 3 (3): 74-79. | NA |

International/ National Conference/ Proceedings/ Book chapters

| S.No. | Title of Paper | Name of the authors | Name of the Conference Proceedings | Indexing status of journals with indexing agency |
| --- | --- | --- | --- | --- |
| 1 | Hybrid Abrasive Flow Machining for Nano Finishing-A Review | P Ali, S Dhull, RS Walia, Q Murtaza, M Tyagi | Materials Today: Proceedings 4 (8), 7208-7218 | Scopus indexed |
| 2 | Synthesis CNTs Particle Based Abrasive Media for Abrasive Flow Machining Process | S Kumar, Q Murtaza, RS Walia, S Dhull, PK Tyagi | IOP Conference Series: Materials Science and Engineering 115 (1), 012034 | Scopus indexed |
| 3 | Abrasive Flow Machining Process Hybridization with Other Non Traditional Machining Processes: A Review. | Sachin Dhull, R.S. Walia, Q. Murtaza, M.S.Niranjan, Saloni Vats | Proceedings of ICMET. Smart Innovation and Technology (Springer) | Scopus indexed |
| 4 | Study of CNT Particle based abrasive media used for finishing workpiece by abrasive flow machining. | Himmat, R S Walia, Qasim Murtaza, Sachin Dhull. | Processing and Fabrication of Advanced Materials – XXIII Procedia Materials Today. 4, 7208- 7218. | Scopus indexed |
| 5 | Development And Characterization Of Newly Developed Polymer Media And Its Computational Flow Dynamics In Electrochemo- Magneto-Rotational Abrasive Flow Machine Fixture | Sachin Dhull, R.S. Walia, Q. Murtaza and M.S. Niranjan. | International Conference on Advanced Production and Industrial Engineering (ICAPIE-2018), Delhi Technological University (DTU) Delhi, Oct 5-6, 2018 | NA |
| 6 | Hybrid abrasive flow machining process models and their computer and industrial applications. | Sachin Dhull, R.S. Walia, Q. Murtaza and M.S. Niranjan. | International Conference on Advanced Production and Industrial Engineering (ICAPIE-2016), Delhi Technological University (DTU) Delhi, 09-10 th December. pp. 101-114. | NA |